Table A1: Lattice parameters for the samples, synthesized by ceramic sintering.

| Sample | X(Al) | a (Å) | b (Å) | c (Å) | Volume (Å3) |
| --- | --- | --- | --- | --- | --- |
| C4AF_00 | 0,00 | 5,4260(5) | 14,7630(21) | 5,5970(6) | 448,34 |
| C4AF_10 | 0,10 | 5,4185(6) | 14,7320(22) | 5,5959(7) | 446,69 |
| C4AF_20 | 0,20 | 5,4119(6) | 14,7061(21) | 5,5951(8) | 445,30 |
| C4AF_30 | 0,30 | 5,4068(7) | 14,6921(23) | 5,5943(8) | 444,33 |
| C4AF_45 | 0,45 | 5,3968(6) | 14,6538(22) | 5,5919(9) | 442,23 |
| C4AF_50 | 0,50 | 5,3899(10) | 14,6404(21) | 5,5893(11) | 441,05 |
| C4AF_55 | 0,55 | 5,3863(11) | 14,6284(20) | 5,5853(12) | 440,08 |
| C4AF_60 | 0,60 | 5,3818(10) | 14,5932(20) | 5,5905(11) | 439,06 |
| C4AF_65 | 0,65 | 5,3717(13) | 14,5854(20) | 5,5861(9) | 437,66 |
| C4AF_70 | 0,70 | 5,3675(14) | 14,5720(21) | 5,5830(12) | 436,67 |
| C4AF_75 | 0,75 | 5,3630(11) | 14,5561(21) | 5,5794(12) | 435,56 |
| C4AF_80 | 0,80 | 5,3560(7) | 14,5348(20) | 5,5745(12) | 433,97 |
| C4AF_90 | 0,90 | 5,3476(12) | 14,5176(22) | 5,5670(11) | 432,19 |
| C4AF_100 | 1,00 | 5,3382(10) | 14,4946(21) | 5,5566(13) | 429,95 |
| C4AF_120 | 1,20 | 5,3172(15) | 14,4735(23) | 5,5316(16) | 425,70 |
| C4AF_130 | 1,30 | 5,3094(12) | 14,4513(21) | 5,5180(15) | 423,38 |
| C4AF_135 | 1,35 | 5,2998(13) | 14,4446(18) | 5,5144(13) | 422,14 |

Table A2: Acronyms for the single crystal samples of the Ca2(Fe2-xAlx)O5 series, studied here, together with their composition, the growth method and the space group. Fill structural data can be found in the corresponding Crystallographic Information File (CIF).

| Sample | X | growth method | space group |
| --- | --- | --- | --- |
| BX000_1 | 0.00 | sintering | Pnma |
| BHT005_2 | 0.115 | melt | Pnma |
| BHT015_1 | 0.204 | melt | Pnma |
| BF010_1 | 0.212 | flux | Pnma |
| BF060_1 | 0.257 | flux | Pnma |
| BF070_1 | 0.258 | flux | Pnma |
| BF020_2 | 0.259 | flux | Pnma |
| BF100_1 | 0.271 | flux | Pnma |
| BHT025_2 | 0.276 | melt | Pnma |
| BHT030_3 | 0.365 | melt | Pnma |
| BHT035_1 | 0.408 | melt | Pnma |
| BHT040_2 | 0.441 | melt | Pnma |
| BF65I_1 | 0.526 | flux | Pnma |
| BF120I_1 | 0.527 | flux | Pnma |
| BF90I_1 | 0.541 | flux | Pnma |
| BF80I_1 | 0.560 | flux | Pnma |
| BHT055_1 | 0.552 | melt | I2mb |
| BHT060_1 | 0.583 | melt | I2mb |
| BHT050_2 | 0.590 | melt | I2mb |
| BHT065_3 | 0.618 | melt | I2mb |
| BHT070_1 | 0.663 | melt | I2mb |
| BHT075_2 | 0.749 | melt | I2mb |
| bht120_6 | 0.789 | melt | I2mb |
| bht095_2 | 0.866 | melt | I2mb |
| bht110_3 | 0.880 | melt | I2mb |
| BHT100_2 | 0.909 | melt | I2mb |
| BHT110n1 | 0.986 | melt | I2mb |
| BHT120N2 | 1.078 | melt | I2mb |
| BHT130_2 | 1.259 | melt | I2mb |
| BHT140_2 | 1.356 | melt | I2mb |

Table A3: Lattice parameters for the all the single crystal samples, investigated here and obtained by powder diffraction on ground single crystals.

| sample | x (Al) | a (Å) | b (Å) | c (Å) | Volume (Å3) |
| --- | --- | --- | --- | --- | --- |
| bx000 | 0,000 | 5,4268(3) | 14,7631(5) | 5,5969(2) | 448,345 |
| bht005_2 | 0,114 | 5,4212(3) | 14,7432(6) | 5,5961(3) | 447,273 |
| bht015_1 | 0,204 | 5,4140(2) | 14,7163(5) | 5,5947(2) | 445,752 |
| bf010_2 | 0,212 | 5,4162(4) | 14,7155(7) | 5,5949(5) | 445,925 |
| bf060_1 | 0,257 | 5,4068(5) | 14,6973(9) | 5,5930(5) | 444,45 |
| bf070_1 | 0,259 | 5,4051(7) | 14,6969(11) | 5,5942(6) | 444,393 |
| bf020_2 | 0,259 | 5,4072(7) | 14,6996(11) | 5,5948(6) | 444,704 |
| bf100_2 | 0,271 | 5,4069(7) | 14,6974(11) | 5,5931(6) | 444,469 |
| bht025_2 | 0,276 | 5,4071(3) | 14,6949(8) | 5,5941(3) | 444,489 |
| bht030_3 | 0,365 | 5,4027(4) | 14,6779(9) | 5,5923(4) | 443,471 |
| bht035_1 | 0,408 | 5,3986(3) | 14,6631(7) | 5,5911(2) | 442,593 |
| bht040_2 | 0,441 | 5,3936(3) | 14,6476(7) | 5,5900(3) | 441,628 |
| bf65i_2 | 0,526 | 5,3859(4) | 14,6317(12) | 5,5871(5) | 440,291 |
| bf120i_1 | 0,527 | 5,3886(4) | 14,6314(13) | 5,5885(6) | 440,613 |
| bf90i_1 | 0,541 | 5,3880(4) | 14,6306(13) | 5,5863(5) | 440,366 |
| bf80i_1 | 0,560 | 5,3876(2) | 14,6302(6) | 5,5877(3) | 440,432 |
| bht055_1 | 0,552 | 5,3808(3) | 14,6130(8) | 5,5911(4) | 439,626 |
| bht060_1 | 0,583 | 5,3781(5) | 14,6020(12) | 5,5887(7) | 438,886 |
| bht050_2 | 0,590 | 5,3832(2) | 14,6210(7) | 5,5916(3) | 440,102 |
| bht065_3 | 0,618 | 5,3725(6) | 14,5830(13) | 5,5870(7) | 437,726 |
| bht070_1 | 0,663 | 5,3714(3) | 14,5804(7) | 5,5847(3) | 437,378 |
| bht075_2 | 0,749 | 5,3624(4) | 14,5526(8) | 5,5795(5) | 435,407 |
| bht120_6 | 0,789 | 5,3569(2) | 14,5407(7) | 5,5735(3) | 434,137 |
| bht095_2 | 0,866 | 5,3510(2) | 14,5256(8) | 5,5685(3) | 432,82 |
| bht110_3 | 0,881 | 5,3473(4) | 14,5156(9) | 5,5659(5) | 432,021 |
| bht100_2 | 0,909 | 5,3469(3) | 14,5149(8) | 5,5640(3) | 431,82 |
| bht110n1 | 0,986 | 5,3369(2) | 14,4945(7) | 5,5548(3) | 429,695 |
| bht120n2 | 1,078 | 5,3269(3) | 14,4687(9) | 5,5433(2) | 427,241 |
| bht130_2 | 1,259 | 5,3093(3) | 14,4534(8) | 5,5230(3) | 423,821 |
| bht140_2 | 1,356 | 5,2991(4) | 14,4434(9) | 5,5099(3) | 421,711 |