Table 5. List of observed and calculated structure factors

===================================================================

# h,k,l, Fc-squared, Fo-squared, sigma(Fo-squared) and status flag

===================================================================

data_jkb1

_shelx_title ' jkbf in C2/c'

_shelx_refln_list_code          4

_shelx_F_calc_maximum      142.81

_exptl_crystal_F_000       411.35

_reflns_d_resolution_high  0.7323

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-x, y, -z+1/2'

'x+1/2, y+1/2, z'

'-x+1/2, y+1/2, -z+1/2'

'-x, -y, -z'

'x, -y, z-1/2'

'-x+1/2, -y+1/2, -z'

'x+1/2, -y+1/2, z-1/2'

_cell_length_a     9.5792

_cell_length_b     8.7588

_cell_length_c     5.2610

_cell_angle_alpha  90.000

_cell_angle_beta  107.199

_cell_angle_gamma  90.000

_shelx_F_squared_multiplier     1.000

loop_

_refln_index_h

_refln_index_k

_refln_index_l

_refln_F_squared_calc

_refln_F_squared_meas

_refln_F_squared_sigma

_refln_observed_status

2   0   0      106.66       83.94      7.31 o

4   0   0       16.29       10.75      5.58 o

6   0   0     4656.01     4738.82    270.00 o

8   0   0     3077.85     2860.12    153.97 o

10   0   0     2254.30     2513.64    242.45 o

12   0   0      189.85      187.15     47.63 o

1   1   0       49.81       63.89      3.84 o

3   1   0     7068.62     7142.64     66.10 o

5   1   0     3642.32     3725.61     59.49 o

7   1   0     1655.89     1635.58     42.15 o

9   1   0        3.92        5.60      5.22 o

11   1   0      793.08      881.02     58.42 o

0   2   0     1657.74     1644.97     85.85 o

2   2   0     2705.82     2844.35     33.73 o

4   2   0      275.97      303.76     11.71 o

6   2   0      173.58      171.50     13.79 o

8   2   0      122.34      141.05     15.46 o

10   2   0       32.50       47.67     13.48 o

12   2   0      145.23      232.35     51.96 o

1   3   0        0.25       -0.17      2.13 o

3   3   0     2720.12     2892.01     28.04 o

5   3   0      762.48      695.40     20.50 o

7   3   0      287.68      268.11     18.86 o

9   3   0      433.85      434.79     26.21 o

11   3   0      132.28      169.85     30.94 o

0   4   0        3.39        4.60      4.73 o

2   4   0      144.65      122.36      9.91 o

4   4   0     4608.14     4625.36     49.62 o

6   4   0      473.14      476.34     17.74 o

8   4   0      128.56      136.76     15.84 o

10   4   0     1833.43     1871.86     68.02 o

1   5   0     5950.36     6153.01     78.84 o

3   5   0     4202.43     4031.64     59.07 o

5   5   0      236.60      215.43     10.59 o

7   5   0     8661.37     8319.20    107.20 o

9   5   0       12.77       12.76      9.10 o

0   6   0     9087.78     9339.42    284.55 o

2   6   0      647.40      629.77     24.50 o

4   6   0      468.76      506.16     23.74 o

6   6   0        3.66        2.52      3.50 o

8   6   0       98.16       85.55     16.40 o

10   6   0     1420.25     1421.33     83.37 o

1   7   0       73.11       65.21     10.14 o

3   7   0      150.47      145.79     14.80 o

5   7   0     1741.78     1746.20     48.96 o

7   7   0     1002.67      964.33     46.96 o

9   7   0      212.35      241.17     28.59 o

0   8   0       14.50        7.18      8.73 o

2   8   0      369.17      349.72     22.38 o

4   8   0      888.82      940.36     36.94 o

6   8   0       30.01       35.56     11.19 o

8   8   0        4.66        2.72      6.21 o

1   9   0       15.39        5.83      4.72 o

3   9   0      421.96      438.44     32.12 o

5   9   0      144.94      138.13     20.81 o

7   9   0      218.96      235.55     28.19 o

0  10   0     3459.12     3293.28    152.55 o

2  10   0        2.44        5.00      9.44 o

4  10   0     1783.69     1848.60     84.61 o

6  10   0      374.30      429.93     64.46 o

1  11   0        0.18       10.88      8.92 o

3  11   0     1087.17     1099.67     66.68 o

-11   1   1      152.31      149.24     26.37 o

-9   1   1       18.89       23.92      8.69 o

-7   1   1      778.70      695.89     29.31 o

-5   1   1      733.06      732.68     20.80 o

-3   1   1     5422.13     5554.34     46.00 o

-1   1   1      184.34      163.38      3.90 o

1   1   1        2.39        3.83      1.59 o

3   1   1     4733.50     5057.94     64.04 o

5   1   1      243.14      244.03     14.49 o

7   1   1      307.68      321.43     22.29 o

9   1   1      120.76      122.51     16.46 o

11   1   1      443.46      480.70     34.14 o

-12   2   1     2831.60     3211.84    115.52 o

-10   2   1       68.61       81.06     19.71 o

-8   2   1     1113.38     1155.94     35.83 o

-6   2   1     1469.57     1321.03     36.85 o

-4   2   1     2594.65     2775.65     41.24 o

-2   2   1    17725.52    17819.90    124.84 o

0   2   1     1891.32     2017.16     29.12 o

2   2   1     9901.16     9102.46    224.28 o

4   2   1      261.22      262.41     13.99 o

6   2   1     3848.52     3801.51     62.98 o

8   2   1     1392.18     1438.56     45.12 o

10   2   1      111.29      134.55     18.52 o

-11   3   1      348.04      342.69     38.91 o

-9   3   1     2939.07     2958.25     95.03 o

-7   3   1     2108.94     1929.87     62.99 o

-5   3   1    11438.99    11884.15    178.10 o

-3   3   1     5866.75     6615.85     65.14 o

-1   3   1     5507.36     5742.76     72.47 o

1   3   1      296.30      481.51     15.05 o

3   3   1      609.31      643.96     15.83 o

5   3   1    17158.48    16643.66    286.98 o

7   3   1      367.33      353.17     21.82 o

9   3   1     1579.74     1632.70     52.44 o

11   3   1        6.52        2.99      9.65 o

-10   4   1      536.18      587.55     45.06 o

-8   4   1       44.30       29.72      9.73 o

-6   4   1       39.40       34.96      6.15 o

-4   4   1        0.42        3.10      2.75 o

-2   4   1     1270.68     1332.52     27.96 o

0   4   1     7935.72     8196.82     67.22 o

2   4   1      479.48      476.27     15.94 o

4   4   1      659.60      628.82     14.86 o

6   4   1      159.66      154.09     15.13 o

8   4   1       20.42       29.37      8.72 o

10   4   1      592.65      653.80     41.43 o

-11   5   1       52.54       63.51     20.57 o

-9   5   1       18.02       26.62      9.78 o

-7   5   1        1.27       -0.93      3.09 o

-5   5   1      179.63      178.23     11.84 o

-3   5   1      269.49      267.92     14.90 o

-1   5   1      554.58      553.43     35.13 o

1   5   1       58.65       60.79      7.39 o

3   5   1      558.91      573.38     19.92 o

5   5   1      306.65      303.53     17.65 o

7   5   1       25.14       23.53      7.94 o

9   5   1       15.19       16.36      8.94 o

-10   6   1       90.40       66.35     19.64 o

-8   6   1       23.62       15.91      5.72 o

-6   6   1      380.76      366.60     21.41 o

-4   6   1      542.59      528.15     23.38 o

-2   6   1      199.81      158.47     13.39 o

0   6   1     1452.84     1405.56     35.54 o

2   6   1       54.26       63.78      8.49 o

4   6   1      202.36      199.17     14.36 o

6   6   1       11.40       10.17      5.12 o

8   6   1      114.73      102.21     18.89 o

10   6   1      105.70      126.19     40.15 o

-9   7   1      669.92      612.08     48.54 o

-7   7   1       10.52       19.41      6.14 o

-5   7   1     4913.85     4848.98     93.71 o

-3   7   1      168.79      146.82     14.41 o

-1   7   1     1946.51     1847.62     44.51 o

1   7   1     2939.31     2918.19     65.56 o

3   7   1        0.22       -2.44      3.69 o

5   7   1     1815.40     1772.56     45.71 o

7   7   1       11.04       12.32      6.66 o

9   7   1     1466.54     1485.52     98.42 o

-8   8   1     1171.23     1150.75     54.12 o

-6   8   1      385.16      369.56     31.39 o

-4   8   1      102.23      130.37     18.20 o

-2   8   1     6343.38     6409.46    123.03 o

0   8   1      216.01      201.82     20.80 o

2   8   1     3073.40     3091.31     76.17 o

4   8   1       40.48       29.28      9.61 o

6   8   1     1740.98     1774.93     56.93 o

8   8   1      442.27      424.58     46.07 o

-7   9   1     1712.88     1709.42     57.77 o

-5   9   1     1439.26     1367.76     66.52 o

-3   9   1       75.41       95.71     19.24 o

-1   9   1        6.74        5.24      5.05 o

1   9   1      140.55      143.06     19.90 o

3   9   1      148.09      140.28     20.48 o

5   9   1      891.64      892.34     47.11 o

7   9   1      729.16      720.83     54.69 o

-6  10   1       16.51       16.97     10.06 o

-4  10   1        1.20       -2.74      5.88 o

-2  10   1      846.74      816.46     44.06 o

0  10   1      445.27      433.39     34.28 o

2  10   1       26.27       35.85     11.78 o

4  10   1       18.11       41.96     14.52 o

-5  11   1      169.71      175.40     38.47 o

-3  11   1        7.69        3.29      9.64 o

-1  11   1       16.88       26.30     12.01 o

1  11   1      366.30      449.84     45.63 o

3  11   1       41.70       67.16     25.49 o

-12   0   2      393.27      381.30     58.33 o

-10   0   2     3699.76     3130.20    132.01 o

-8   0   2      411.27      356.63     38.14 o

-6   0   2     6934.21     6992.95    558.54 o

-4   0   2     8124.02     8155.54     90.79 o

-2   0   2     1923.67     2093.21     60.13 o

0   0   2    20395.11    19778.64    462.59 o

2   0   2     4163.47     4411.53     66.46 o

4   0   2    10848.32    10588.93    335.12 o

6   0   2       52.50       48.47     13.79 o

8   0   2      626.68      612.34     43.44 o

10   0   2     3405.18     3495.67    170.42 o

-11   1   2        6.06        9.00      8.43 o

-9   1   2      479.48      437.03     32.65 o

-7   1   2     9359.14     8876.45    229.65 o

-5   1   2      951.47      896.44     22.91 o

-3   1   2       24.44       69.52      3.41 o

-1   1   2       56.07       50.89      3.19 o

1   1   2     4377.31     4729.24     42.76 o

3   1   2      948.83      904.79     30.87 o

5   1   2     1326.95     1302.49     35.51 o

7   1   2     2460.58     2496.85     57.93 o

9   1   2      482.14      497.73     43.79 o

-12   2   2      562.60      527.09     44.72 o

-10   2   2      783.00      751.31     46.61 o

-8   2   2      325.89      319.42     26.36 o

-6   2   2     1603.91     1581.09     48.45 o

-4   2   2      705.70      732.15     20.80 o

-2   2   2      186.92      155.65      5.19 o

0   2   2     2949.83     3518.08     37.53 o

2   2   2     1242.36     1146.21     24.87 o

4   2   2     2211.28     2246.61     43.63 o

6   2   2     1088.71     1111.60     38.07 o

8   2   2      733.35      781.37     52.07 o

10   2   2      264.95      266.07     37.03 o

-11   3   2        4.03        0.77      8.09 o

-9   3   2       47.79       48.78     14.76 o

-7   3   2      436.95      421.78     20.49 o

-5   3   2      514.72      512.64     12.13 o

-3   3   2      342.00      392.13     12.23 o

-1   3   2     2221.06     2309.74     46.20 o

1   3   2     1447.85     1608.88     33.17 o

3   3   2       84.21       89.18      8.46 o

5   3   2      386.45      352.84     19.71 o

7   3   2      221.88      216.04     23.16 o

9   3   2       47.48       64.70     15.97 o

-10   4   2      444.74      441.54     39.18 o

-8   4   2        4.19        6.11      5.85 o

-6   4   2      425.22      397.23     15.69 o

-4   4   2      149.82      142.85      9.18 o

-2   4   2      401.16      412.39     13.52 o

0   4   2     3398.76     3421.83     47.21 o

2   4   2     1378.57     1426.82     44.88 o

4   4   2     1398.63     1285.59     38.10 o

6   4   2       22.20       26.64      8.95 o

8   4   2       14.72       13.86      8.01 o

10   4   2      128.54      180.74     44.79 o

-11   5   2      664.00      655.71     61.85 o

-9   5   2      125.97      111.87     17.53 o

-7   5   2     5297.12     5447.47     91.26 o

-5   5   2        3.05        0.21      3.46 o

-3   5   2    11050.13    11004.67    289.75 o

-1   5   2       26.78       23.58      4.91 o

1   5   2     2103.48     2167.84     37.77 o

3   5   2     9800.54     9403.81     94.80 o

5   5   2        0.77        2.49      4.57 o

7   5   2     2027.35     1995.89     66.86 o

9   5   2        2.83       16.13      9.46 o

-10   6   2      161.26      189.20     29.68 o

-8   6   2        6.94        9.97      5.73 o

-6   6   2     2779.19     2869.39     88.96 o

-4   6   2       14.24       33.26      9.22 o

-2   6   2     3841.97     3669.35    106.17 o

0   6   2     9380.48     9540.88    149.86 o

2   6   2       83.30       89.42     11.85 o

4   6   2      415.88      433.64     21.11 o

6   6   2       37.35       48.81     12.95 o

8   6   2      131.14      142.15     22.71 o

-9   7   2      113.08      140.30     26.28 o

-7   7   2      389.13      359.29     24.28 o

-5   7   2      750.42      701.83     34.95 o

-3   7   2      185.41      176.15     18.38 o

-1   7   2     1103.65     1146.42     41.94 o

1   7   2        9.71        7.94      5.26 o

3   7   2      545.29      561.05     27.32 o

5   7   2      846.94      823.42     36.63 o

7   7   2        2.32        5.94      7.18 o

-8   8   2      174.23      168.26     19.95 o

-6   8   2       97.53      106.22     21.45 o

-4   8   2       52.23       72.74     14.46 o

-2   8   2      155.25      160.53     18.84 o

0   8   2      339.69      346.84     27.66 o

2   8   2       41.25       37.30     10.14 o

4   8   2      236.56      248.78     25.95 o

6   8   2      144.23      147.47     19.59 o

-7   9   2      604.74      648.58     49.74 o

-5   9   2       86.11       69.89     19.17 o

-3   9   2       64.57       71.98     15.50 o

-1   9   2        3.04        8.80      6.23 o

1   9   2      151.24      182.53     23.05 o

3   9   2        7.02       10.28      6.95 o

5   9   2      148.42      154.75     19.94 o

-6  10   2      231.95      238.03     47.70 o

-4  10   2     1827.91     1876.04    124.18 o

-2  10   2      164.77      119.59     24.73 o

0  10   2     1600.48     1592.00     62.23 o

2  10   2        7.49       21.08      7.59 o

4  10   2     2929.45     2941.84    161.48 o

-3  11   2      654.60      720.71     79.36 o

-1  11   2       21.79       64.39     29.82 o

1  11   2      104.70       73.47     32.35 o

-11   1   3        0.34       -0.21      7.76 o

-9   1   3        8.08        4.96      6.92 o

-7   1   3      791.09      800.77     30.36 o

-5   1   3      952.30      808.31    105.72 o

-3   1   3     3919.97     3877.78     36.80 o

-1   1   3       15.97       22.94      3.61 o

1   1   3       99.61       90.93      6.19 o

3   1   3      860.48      828.42     26.29 o

5   1   3       42.83       42.29     13.64 o

7   1   3      318.06      353.25     36.12 o

9   1   3      409.02      401.76     43.14 o

-12   2   3     1905.87     1895.18    115.14 o

-10   2   3        1.00        7.94      7.76 o

-8   2   3     3309.78     3183.98     66.86 o

-6   2   3       20.69       28.30      7.32 o

-4   2   3      329.14      284.70     11.51 o

-2   2   3    11148.00    10693.16    131.62 o

0   2   3       20.58       19.05      3.99 o

2   2   3     5538.54     5703.22     75.09 o

4   2   3      196.79      166.67     16.98 o

6   2   3     2409.58     2322.02     81.52 o

8   2   3      781.42      777.18     54.08 o

-11   3   3      717.50      712.86     48.47 o

-9   3   3     3775.92     3717.01     81.97 o

-7   3   3      976.30      840.48     32.81 o

-5   3   3     4202.27     4196.66     76.15 o

-3   3   3      351.83      353.95     14.84 o

-1   3   3    11032.39    10807.97    194.26 o

1   3   3      259.55      254.32     13.51 o

3   3   3        0.04        5.42      4.17 o

5   3   3     4738.71     4440.95    108.11 o

7   3   3        6.00        7.71      8.56 o

-10   4   3      170.20      174.28     21.18 o

-8   4   3      448.42      443.53     23.45 o

-6   4   3     1049.75      954.79     26.38 o

-4   4   3      513.66      520.01     21.29 o

-2   4   3     2329.60     2329.97     49.66 o

0   4   3     1463.80     1466.61     85.05 o

2   4   3      106.88      101.63     11.08 o

4   4   3     1304.15     1266.83     61.15 o

6   4   3      250.27      261.27     31.45 o

8   4   3        0.54       10.77      8.16 o

-9   5   3       10.42       20.81      7.36 o

-7   5   3       52.92       52.69      9.05 o

-5   5   3      733.55      684.62     29.52 o

-3   5   3      406.25      397.83     21.89 o

-1   5   3        6.05        9.73      4.69 o

1   5   3      553.19      522.97     23.04 o

3   5   3       31.18       27.73      8.87 o

5   5   3       62.87       66.37     17.82 o

7   5   3        4.20       11.83     10.00 o

-10   6   3      176.03      151.66     22.07 o

-8   6   3        1.03        8.48      4.77 o

-6   6   3       85.11       81.40     16.67 o

-4   6   3      118.55      125.32     17.87 o

-2   6   3       50.00       47.97     10.62 o

0   6   3      697.14      688.81     31.77 o

2   6   3       89.14      112.16     15.81 o

4   6   3      454.46      433.35     28.97 o

6   6   3       27.04       20.74     12.56 o

-9   7   3      964.39      994.26     49.00 o

-7   7   3        0.03        4.15      5.87 o

-5   7   3     2600.25     2515.16    190.56 o

-3   7   3      166.20      168.05     21.99 o

-1   7   3     2557.68     2628.43     66.05 o

1   7   3      826.77      851.70     38.93 o

3   7   3       44.08       55.03     13.36 o

5   7   3     1145.15     1215.92     52.89 o

-8   8   3     1082.88     1094.52     44.07 o

-6   8   3      219.39      210.13     30.19 o

-4   8   3      245.14      198.90     26.19 o

-2   8   3     2242.45     2127.23     76.41 o

0   8   3        4.67        5.42      7.51 o

2   8   3     4089.76     4271.53    199.61 o

4   8   3      211.40      224.50     25.90 o

-5   9   3       48.53       41.50     17.15 o

-3   9   3      166.54      203.15     38.45 o

-1   9   3      991.90      953.39     55.50 o

1   9   3      437.24      378.50     54.94 o

3   9   3      449.57      526.43     37.19 o

-4  10   3        3.24       -1.97      9.01 o

-2  10   3      228.40      208.17     30.59 o

0  10   3       77.53       53.63     15.76 o

-10   0   4     1030.16     1094.28     72.64 o

-8   0   4      124.22      108.83     21.20 o

-6   0   4     9652.29     9582.94     99.67 o

-4   0   4     3410.98     3348.25    106.20 o

-2   0   4      443.02      445.00     27.94 o

0   0   4    10049.43     9688.90    141.15 o

2   0   4       82.32       93.81     16.14 o

4   0   4     4599.96     4524.77    148.60 o

6   0   4      174.19      169.35     38.62 o

-11   1   4      130.80      133.15     22.58 o

-9   1   4       84.17       84.68     15.61 o

-7   1   4      763.37      701.21     62.24 o

-5   1   4      241.64      251.32     20.59 o

-3   1   4     6485.43     6215.51     60.90 o

-1   1   4     1928.77     1836.48     43.01 o

1   1   4        0.14        3.22      4.06 o

3   1   4     1917.80     1875.95     71.64 o

5   1   4       19.04       36.07     13.48 o

7   1   4      302.60      327.47     38.23 o

-10   2   4        3.42       12.86      8.58 o

-8   2   4       83.41       94.42     13.36 o

-6   2   4       41.99       34.11      6.70 o

-4   2   4      435.94      410.04     17.31 o

-2   2   4      266.06      249.61     16.64 o

0   2   4      345.69      300.70     17.54 o

2   2   4     2117.17     2120.65     59.04 o

4   2   4       19.79       27.01      9.25 o

6   2   4        6.24       -0.94      6.99 o

-11   3   4       83.57       77.42     18.61 o

-9   3   4      295.69      267.04     20.64 o

-7   3   4      102.17      106.66     12.03 o

-5   3   4      286.59      284.22     16.11 o

-3   3   4      514.08      434.06     20.73 o

-1   3   4       97.51       99.89      9.60 o

1   3   4        4.64        7.93      5.65 o

3   3   4      521.28      506.35     28.59 o

5   3   4      259.74      267.30     31.09 o

-10   4   4     1575.87     1631.62     51.42 o

-8   4   4      218.72      234.75     18.56 o

-6   4   4        8.88        7.56      3.99 o

-4   4   4      707.15      692.69     23.82 o

-2   4   4      143.67      128.66     11.21 o

0   4   4      160.88      192.02     21.94 o

2   4   4     1152.55     1094.63     40.74 o

4   4   4     2305.63     2259.47     78.05 o

6   4   4       27.53       34.78     13.68 o

-9   5   4       20.30       25.71      8.76 o

-7   5   4     4849.50     4907.78    119.94 o

-5   5   4        1.81        1.72      5.37 o

-3   5   4     4826.23     4882.55     83.92 o

-1   5   4       95.73       97.66     13.46 o

1   5   4     2106.39     2020.51     56.48 o

3   5   4     1311.16     1307.43     48.75 o

5   5   4      134.64      113.46     23.28 o

-8   6   4      752.44      813.84     30.96 o

-6   6   4      823.80      793.88     41.97 o

-4   6   4     1504.56     1469.10     53.58 o

-2   6   4      589.06      546.52     28.68 o

0   6   4      549.55      576.56     31.27 o

2   6   4      130.43      151.72     19.40 o

4   6   4     2268.78     2205.97    124.78 o

-7   7   4      579.93      555.22     28.43 o

-5   7   4      178.52      212.65     24.88 o

-3   7   4       29.24       41.97     13.40 o

-1   7   4      581.92      564.96     32.15 o

1   7   4       22.47       36.81     11.26 o

3   7   4        0.54        1.93      6.67 o

5   7   4      220.96      276.13     52.75 o

-6   8   4        7.89       13.53      9.32 o

-4   8   4      257.04      260.61     29.76 o

-2   8   4      358.49      389.19     34.80 o

0   8   4        0.17        7.65      7.39 o

2   8   4        0.73        7.89      7.71 o

4   8   4      488.88      484.93     67.65 o

-5   9   4      103.34       82.96     25.15 o

-3   9   4      570.05      615.88     44.76 o

-1   9   4      124.68      154.52     26.52 o

1   9   4        9.78       27.81     19.57 o

-11   1   5        1.69        4.08      7.60 o

-9   1   5        1.99        1.61      6.04 o

-7   1   5      336.86      338.59     23.35 o

-5   1   5      708.59      690.36     21.41 o

-3   1   5     1498.36     1498.64     33.17 o

-1   1   5        0.02        2.60      3.78 o

1   1   5       13.97       12.87      5.65 o

3   1   5        3.24        4.74      6.22 o

5   1   5       27.58       30.95     13.28 o

-10   2   5      120.08      160.44     19.02 o

-8   2   5     2963.86     3223.62     77.36 o

-6   2   5       97.08       99.93     11.61 o

-4   2   5      301.44      301.41     15.96 o

-2   2   5     1597.48     1602.73     46.02 o

0   2   5        9.58       17.38      6.14 o

2   2   5     4610.24     4548.25     87.12 o

4   2   5      182.02      187.42     40.72 o

-11   3   5       98.92      102.87     25.01 o

-9   3   5     2399.85     2506.17    100.19 o

-7   3   5        8.46       17.59      8.46 o

-5   3   5     1752.41     1816.70     42.66 o

-3   3   5      360.68      328.20     20.22 o

-1   3   5     6055.91     6191.54     93.58 o

1   3   5      202.53      197.27     19.65 o

3   3   5       75.59       73.44     14.93 o

-10   4   5      338.75      436.40     65.60 o

-8   4   5      592.71      633.01     37.83 o

-6   4   5      166.30      182.73     21.26 o

-4   4   5      161.33      135.81     19.46 o

-2   4   5       36.65       53.06     14.78 o

0   4   5      375.91      389.84     27.40 o

2   4   5      757.87      806.09     38.65 o

4   4   5      969.75      982.81     46.88 o

-9   5   5       44.88       42.47     15.35 o

-7   5   5       19.66       27.55     11.23 o

-5   5   5      131.74      139.04     22.90 o

-3   5   5       90.19       79.61     18.35 o

-1   5   5       17.23       25.57      9.02 o

1   5   5       26.52       27.59      8.53 o

3   5   5       19.36       16.19      9.13 o

-6   6   5      206.31      228.06     39.73 o

-4   6   5       86.15      110.21     22.23 o

-2   6   5       12.26       16.79      7.05 o

0   6   5      320.28      308.41     25.58 o

2   6   5        9.28       23.35      8.56 o

-5   7   5     3027.15     2993.49    140.94 o

-3   7   5      224.06      248.25     22.19 o

-1   7   5      530.06      554.37     33.62 o

1   7   5      445.69      429.48     49.26 o

-4   8   5      128.90      180.36     28.61 o

-2   8   5     1117.49     1100.00     73.29 o

-8   0   6      594.11      556.94     68.13 o

-6   0   6     1007.51     1299.20     98.48 o

-4   0   6     2561.65     2618.80     95.24 o

-2   0   6      465.63      466.30     63.77 o

0   0   6     1101.67     1050.35     57.65 o

2   0   6        6.60       -9.08     10.39 o

-7   1   6      935.39      994.79     51.01 o

-5   1   6      361.59      369.92     24.36 o

-3   1   6     1140.00     1103.77     50.46 o

-1   1   6       76.23       94.60     14.98 o

1   1   6      434.08      424.17     27.62 o

3   1   6       27.95       19.50     11.05 o

-8   2   6      167.79      159.42     30.96 o

-6   2   6      166.21      164.66     17.60 o

-4   2   6        8.04       11.06      7.62 o

-2   2   6       12.70       11.61      6.86 o

0   2   6        7.55       16.70     10.64 o

2   2   6      763.43      764.04     39.18 o

-9   3   6        4.83        2.63     10.32 o

-7   3   6      166.17      196.27     19.72 o

-5   3   6      186.87      182.10     16.20 o

-3   3   6       96.36       90.77     13.89 o

-1   3   6      338.78      357.17     33.53 o

1   3   6      134.82      115.18     16.32 o

-8   4   6       27.18       51.96     20.30 o

-6   4   6      429.22      424.81     27.90 o

-4   4   6      157.23      159.00     18.24 o

-2   4   6        4.38        8.48      8.51 o

0   4   6     1362.22     1357.44     67.47 o

2   4   6      666.94      690.16     58.64 o

-7   5   6      643.77      683.30     59.92 o

-5   5   6       92.18      104.28     18.91 o

-3   5   6     4846.71     5120.63    181.68 o

-1   5   6        0.26       -1.45      7.79 o

-5   1   7      414.30      485.28     73.45 o