Appendix 1. Low-temperature PPMS-heat capacity measurements on synthetic pyrope-grossular garnets.

Sources: HW80: Haselton and Westrum (1980), Geiger: syntheses performed by C.A. Geiger. SW: sample weight [mg]; FW: Formula weight [g mol-1].

Numbers in parentheses are one standard deviation and refer to the last digit.

| Py #1 Source: HW80 |  | Py #2 Source: HW80 |  | Py #3 Source: Geiger |  | Py #4 Source: Geiger |  | Py90Gr10 #1 Source: Geiger |  | Py90Gr10 #2 Source: Geiger |  | Py90Gr10 #3 Source: Geiger |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FW | 403.129 | FW | 403.129 | FW | 403.129 | FW | 403.13 | FW | 407.955 | FW | 407.955 | FW | 407.955 |
| SW | 23.74 | SW | 23.74 | SW | 27.17 | SW | 27.17 | SW | 22.44 | SW | 22.44 | SW | 16.75 |
| XGr | 0.000 | XGr | 0.000 | XGr | 0.000 | XGr | 0.000 | XGr | 0.102 | XGr | 0.102 | XGr | 0.102 |
| T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] |
| 5.156 | 0.012(2) | 5.059 | 0.014(3) | 5.133 | 0.016(1) | 5.115 | 0.017(1) | 5.058 | 0.016(1) | 5.131 | 0.015(1) | 5.051 | 0.011(1) |
| 5.163 | 0.012(1) | 5.064 | 0.011(1) | 5.139 | 0.015(1) | 5.121 | 0.021(1) | 5.063 | 0.011(2) | 5.131 | 0.016(1) | 5.057 | 0.010(1) |
| 5.165 | 0.019(2) | 5.072 | 0.011(1) | 5.144 | 0.015(0) | 5.129 | 0.018(1) | 5.064 | 0.013(2) | 5.135 | 0.017(1) | 5.061 | 0.011(1) |
| 5.663 | 0.013(2) | 5.507 | 0.014(1) | 5.582 | 0.016(1) | 5.556 | 0.023(1) | 5.494 | 0.016(1) | 5.588 | 0.019(2) | 5.491 | 0.014(1) |
| 5.670 | 0.016(1) | 5.512 | 0.015(1) | 5.589 | 0.016(1) | 5.570 | 0.022(1) | 5.495 | 0.015(1) | 5.595 | 0.015(1) | 5.498 | 0.014(1) |
| 5.676 | 0.018(1) | 5.517 | 0.015(1) | 5.594 | 0.016(1) | 5.575 | 0.023(1) | 5.503 | 0.014(1) | 5.599 | 0.017(1) | 5.503 | 0.012(1) |
| 6.220 | 0.024(2) | 5.987 | 0.019(1) | 6.065 | 0.023(1) | 6.044 | 0.028(1) | 5.976 | 0.017(1) | 6.074 | 0.023(2) | 5.970 | 0.017(1) |
| 6.228 | 0.023(2) | 5.994 | 0.016(1) | 6.071 | 0.020(1) | 6.052 | 0.026(1) | 5.980 | 0.019(1) | 6.078 | 0.028(1) | 5.977 | 0.016(1) |
| 6.232 | 0.018(2) | 5.999 | 0.018(1) | 6.076 | 0.023(1) | 6.058 | 0.026(1) | 5.985 | 0.019(2) | 6.084 | 0.026(2) | 5.984 | 0.016(1) |
| 6.844 | 0.033(1) | 6.503 | 0.027(1) | 6.584 | 0.032(1) | 6.563 | 0.036(1) | 6.487 | 0.030(1) | 6.595 | 0.037(1) | 6.489 | 0.028(1) |
| 6.845 | 0.033(2) | 6.510 | 0.029(1) | 6.592 | 0.028(1) | 6.571 | 0.035(1) | 6.494 | 0.028(1) | 6.602 | 0.032(1) | 6.495 | 0.025(1) |
| 6.845 | 0.040(2) | 6.516 | 0.028(1) | 6.598 | 0.032(1) | 6.578 | 0.035(1) | 6.500 | 0.029(1) | 6.607 | 0.038(1) | 6.501 | 0.027(1) |
| 7.445 | 0.045(2) | 7.087 | 0.038(1) | 7.176 | 0.036(1) | 7.156 | 0.047(1) | 7.070 | 0.039(1) | 7.185 | 0.043(1) | 7.071 | 0.042(1) |
| 7.453 | 0.045(1) | 7.087 | 0.040(1) | 7.176 | 0.040(1) | 7.157 | 0.043(1) | 7.071 | 0.040(1) | 7.185 | 0.044(1) | 7.072 | 0.040(1) |
| 7.457 | 0.044(1) | 7.088 | 0.039(1) | 7.178 | 0.040(1) | 7.159 | 0.046(1) | 7.072 | 0.039(1) | 7.185 | 0.048(1) | 7.073 | 0.041(1) |
| 8.180 | 0.057(2) | 7.670 | 0.046(2) | 7.738 | 0.045(1) | 7.736 | 0.052(1) | 7.662 | 0.046(2) | 7.740 | 0.051(2) | 7.662 | 0.046(2) |
| 8.185 | 0.055(1) | 7.677 | 0.046(2) | 7.743 | 0.045(1) | 7.739 | 0.053(1) | 7.668 | 0.046(1) | 7.745 | 0.052(1) | 7.668 | 0.046(2) |
| 8.189 | 0.056(1) | 7.683 | 0.046(1) | 7.747 | 0.045(1) | 7.743 | 0.053(1) | 7.676 | 0.046(1) | 7.749 | 0.051(1) | 7.674 | 0.046(2) |
| 8.978 | 0.078(2) | 8.337 | 0.057(2) | 8.408 | 0.055(2) | 8.405 | 0.064(2) | 8.330 | 0.056(2) | 8.408 | 0.062(2) | 8.328 | 0.056(2) |
| 8.982 | 0.077(2) | 8.343 | 0.057(2) | 8.412 | 0.056(2) | 8.408 | 0.064(1) | 8.335 | 0.055(2) | 8.413 | 0.062(2) | 8.334 | 0.055(2) |
| 8.989 | 0.078(2) | 8.349 | 0.057(2) | 8.417 | 0.055(1) | 8.413 | 0.064(1) | 8.340 | 0.056(2) | 8.419 | 0.062(2) | 8.340 | 0.055(2) |
| 9.863 | 0.107(3) | 9.061 | 0.077(2) | 9.132 | 0.074(2) | 9.135 | 0.085(2) | 9.054 | 0.075(2) | 9.137 | 0.081(3) | 9.054 | 0.076(3) |
| 9.866 | 0.105(2) | 9.066 | 0.078(2) | 9.137 | 0.074(2) | 9.138 | 0.083(2) | 9.058 | 0.074(2) | 9.141 | 0.083(2) | 9.058 | 0.077(3) |
| 9.872 | 0.105(2) | 9.072 | 0.077(2) | 9.142 | 0.073(2) | 9.143 | 0.083(2) | 9.063 | 0.075(2) | 9.147 | 0.082(2) | 9.063 | 0.077(3) |
| 10.837 | 0.133(4) | 9.849 | 0.102(3) | 9.925 | 0.097(3) | 9.928 | 0.109(2) | 9.842 | 0.098(3) | 9.929 | 0.106(4) | 9.840 | 0.100(4) |
| 10.841 | 0.134(3) | 9.853 | 0.101(2) | 9.929 | 0.096(2) | 9.931 | 0.106(3) | 9.846 | 0.098(3) | 9.932 | 0.107(3) | 9.844 | 0.099(3) |
| 10.848 | 0.135(3) | 9.860 | 0.102(2) | 9.937 | 0.097(2) | 9.936 | 0.106(2) | 9.852 | 0.097(2) | 9.940 | 0.105(3) | 9.850 | 0.099(3) |
| 11.906 | 0.182(6) | 10.706 | 0.128(4) | 10.793 | 0.119(4) | 10.795 | 0.133(3) | 10.699 | 0.121(4) | 10.795 | 0.131(4) | 10.698 | 0.124(5) |
| 11.906 | 0.179(4) | 10.710 | 0.126(3) | 10.797 | 0.119(3) | 10.797 | 0.132(3) | 10.701 | 0.121(3) | 10.800 | 0.129(3) | 10.701 | 0.123(4) |
| 11.911 | 0.180(4) | 10.717 | 0.128(3) | 10.803 | 0.119(3) | 10.801 | 0.132(2) | 10.707 | 0.120(3) | 10.806 | 0.128(3) | 10.707 | 0.123(4) |
| 13.075 | 0.245(5) | 11.640 | 0.159(5) | 11.728 | 0.153(4) | 11.732 | 0.169(4) | 11.631 | 0.152(5) | 11.733 | 0.167(5) | 11.630 | 0.152(6) |
| 13.077 | 0.249(6) | 11.643 | 0.158(4) | 11.730 | 0.153(3) | 11.732 | 0.167(4) | 11.636 | 0.149(4) | 11.736 | 0.165(4) | 11.635 | 0.150(5) |
| 13.080 | 0.246(5) | 11.651 | 0.158(3) | 11.737 | 0.152(3) | 11.737 | 0.167(3) | 11.642 | 0.150(4) | 11.743 | 0.166(4) | 11.642 | 0.150(5) |
| 14.362 | 0.338(7) | 12.655 | 0.216(5) | 12.743 | 0.203(6) | 12.748 | 0.215(4) | 12.644 | 0.205(7) | 12.747 | 0.221(7) | 12.644 | 0.208(9) |
| 14.365 | 0.332(9) | 12.657 | 0.213(5) | 12.745 | 0.201(4) | 12.750 | 0.219(5) | 12.647 | 0.202(5) | 12.750 | 0.215(5) | 12.645 | 0.208(6) |
| 14.366 | 0.335(6) | 12.663 | 0.214(4) | 12.751 | 0.202(4) | 12.754 | 0.218(4) | 12.654 | 0.204(5) | 12.756 | 0.217(5) | 12.653 | 0.207(6) |
| 15.780 | 0.453(8) | 13.756 | 0.290(8) | 13.850 | 0.271(5) | 13.853 | 0.284(5) | 13.748 | 0.277(6) | 13.855 | 0.291(9) | 13.745 | 0.286(8) |
| 15.780 | 0.451(8) | 13.756 | 0.289(6) | 13.851 | 0.271(6) | 13.857 | 0.289(6) | 13.749 | 0.280(8) | 13.856 | 0.288(7) | 13.746 | 0.289(10) |
| 15.791 | 0.458(13) | 13.762 | 0.289(5) | 13.856 | 0.268(5) | 13.858 | 0.285(5) | 13.753 | 0.277(5) | 13.862 | 0.293(6) | 13.751 | 0.288(7) |
| 17.322 | 0.628(11) | 14.955 | 0.375(8) | 15.054 | 0.357(7) | 15.058 | 0.369(7) | 14.943 | 0.363(8) | 15.059 | 0.384(9) | 14.942 | 0.377(10) |
| 17.323 | 0.627(11) | 14.957 | 0.379(9) | 15.056 | 0.353(9) | 15.063 | 0.371(7) | 14.946 | 0.371(11) | 15.064 | 0.388(12) | 14.946 | 0.377(13) |
| 17.339 | 0.634(14) | 14.958 | 0.375(6) | 15.059 | 0.353(6) | 15.066 | 0.380(9) | 14.948 | 0.366(7) | 15.064 | 0.387(7) | 14.948 | 0.374(9) |
| 19.025 | 0.863(15) | 16.254 | 0.497(9) | 16.363 | 0.471(8) | 16.371 | 0.486(9) | 16.244 | 0.493(10) | 16.372 | 0.522(10) | 16.243 | 0.503(13) |
| 19.027 | 0.865(15) | 16.258 | 0.498(9) | 16.365 | 0.465(8) | 16.371 | 0.489(8) | 16.249 | 0.492(10) | 16.374 | 0.523(10) | 16.247 | 0.506(12) |
| 19.055 | 0.887(17) | 16.259 | 0.505(13) | 16.372 | 0.471(12) | 16.382 | 0.499(11) | 16.249 | 0.494(14) | 16.382 | 0.525(13) | 16.249 | 0.510(18) |
|  |  | 17.671 | 0.675(12) | 17.785 | 0.627(11) | 17.794 | 0.647(11) | 17.660 | 0.680(13) | 17.792 | 0.708(13) | 17.659 | 0.700(17) |
|  |  | 17.672 | 0.675(11) | 17.786 | 0.628(11) | 17.795 | 0.650(12) | 17.663 | 0.677(12) | 17.794 | 0.704(13) | 17.661 | 0.700(16) |
|  |  | 17.678 | 0.679(16) | 17.802 | 0.641(15) | 17.812 | 0.664(14) | 17.668 | 0.690(18) | 17.809 | 0.715(18) | 17.666 | 0.709(24) |
|  |  | 19.203 | 0.892(15) | 19.318 | 0.842(14) | 19.332 | 0.864(15) | 19.193 | 0.918(16) | 19.327 | 0.952(17) | 19.192 | 0.936(20) |
|  |  | 19.204 | 0.894(15) | 19.319 | 0.839(14) | 19.333 | 0.865(15) | 19.195 | 0.915(16) | 19.327 | 0.952(17) | 19.194 | 0.938(20) |
|  |  | 19.219 | 0.904(20) | 19.345 | 0.857(17) | 19.360 | 0.884(17) | 19.209 | 0.927(22) | 19.354 | 0.956(19) | 19.207 | 0.955(29) |
| 20.89 | 1.20(2) | 20.86 | 1.21(2) | 20.99 | 1.14(2) | 21.009 | 1.156(20) | 20.85 | 1.25(2) | 21.00 | 1.29(2) | 20.85 | 1.28(3) |
| 20.90 | 1.21(2) | 20.87 | 1.20(2) | 21.00 | 1.14(2) | 21.01 | 1.16(2) | 20.86 | 1.25(2) | 21.01 | 1.29(2) | 20.86 | 1.28(3) |
| 20.94 | 1.23(3) | 20.90 | 1.22(3) | 21.03 | 1.16(2) | 21.05 | 1.18(2) | 20.89 | 1.27(3) | 21.04 | 1.29(3) | 20.89 | 1.30(4) |
| 22.94 | 1.68(3) | 22.68 | 1.61(3) | 22.81 | 1.55(3) | 22.83 | 1.57(3) | 22.67 | 1.68(3) | 22.82 | 1.75(3) | 22.67 | 1.70(4) |
| 22.95 | 1.69(3) | 22.69 | 1.61(3) | 22.81 | 1.55(3) | 22.83 | 1.57(3) | 22.68 | 1.69(3) | 22.82 | 1.75(3) | 22.68 | 1.72(4) |
| 22.99 | 1.71(4) | 22.71 | 1.64(4) | 22.85 | 1.56(3) | 22.87 | 1.59(3) | 22.71 | 1.72(4) | 22.86 | 1.77(4) | 22.70 | 1.74(5) |
| 25.20 | 2.46(4) | 24.65 | 2.21(4) | 24.78 | 2.14(4) | 24.81 | 2.18(4) | 24.65 | 2.36(4) | 24.79 | 2.42(4) | 24.64 | 2.36(5) |
| 25.20 | 2.48(4) | 24.65 | 2.20(4) | 24.79 | 2.13(4) | 24.82 | 2.15(4) | 24.65 | 2.35(4) | 24.80 | 2.36(4) | 24.64 | 2.36(5) |
| 25.24 | 2.53(5) | 24.69 | 2.24(5) | 24.82 | 2.15(5) | 24.85 | 2.24(4) | 24.68 | 2.38(5) | 24.84 | 2.47(5) | 24.68 | 2.41(7) |
| 27.68 | 3.47(6) | 26.80 | 3.02(5) | 26.94 | 2.93(5) | 26.96 | 2.99(6) | 26.80 | 3.20(6) | 26.95 | 3.32(6) | 26.79 | 3.24(8) |
| 27.68 | 3.48(6) | 26.81 | 2.99(5) | 26.95 | 2.82(6) | 26.97 | 2.97(5) | 26.81 | 3.21(5) | 26.95 | 3.34(7) | 26.81 | 3.11(13) |
| 27.72 | 3.64(8) | 26.84 | 3.20(10) | 26.99 | 2.95(7) | 27.01 | 3.07(6) | 26.84 | 3.40(11) | 27.00 | 3.26(7) | 26.84 | 3.05(11) |
| 30.38 | 4.67(8) | 29.14 | 4.07(6) | 29.27 | 3.90(6) | 29.30 | 3.96(6) | 29.13 | 4.32(7) | 29.28 | 4.37(7) | 29.13 | 4.36(9) |
| 30.39 | 4.72(7) | 29.14 | 4.06(7) | 29.28 | 3.89(6) | 29.30 | 3.95(6) | 29.14 | 4.31(7) | 29.28 | 4.38(7) | 29.13 | 4.36(9) |
| 30.39 | 4.71(7) | 29.20 | 4.12(7) | 29.33 | 3.94(8) | 29.36 | 4.11(9) | 29.19 | 4.36(8) | 29.34 | 4.38(9) | 29.18 | 4.42(11) |
| 31.83 | 5.47(9) | 31.69 | 5.39(8) | 31.81 | 5.22(8) | 31.85 | 5.27(8) | 31.68 | 5.69(9) | 31.82 | 5.81(9) | 31.67 | 5.74(12) |
| 31.83 | 5.49(9) | 31.69 | 5.39(9) | 31.81 | 5.23(8) | 31.85 | 5.30(8) | 31.68 | 5.69(9) | 31.82 | 5.80(9) | 31.68 | 5.73(12) |
| 31.89 | 5.54(10) | 31.74 | 5.46(10) | 31.87 | 5.31(10) | 31.91 | 5.38(9) | 31.74 | 5.75(11) | 31.88 | 5.89(11) | 31.73 | 5.81(13) |
| 34.59 | 7.35(11) | 34.45 | 7.23(11) | 34.58 | 7.05(10) | 34.61 | 7.07(10) | 34.45 | 7.58(12) | 34.59 | 7.74(12) | 34.45 | 7.66(15) |
| 34.59 | 7.35(11) | 34.46 | 7.24(11) | 34.58 | 7.03(10) | 34.61 | 7.08(11) | 34.45 | 7.60(12) | 34.59 | 7.74(12) | 34.45 | 7.68(16) |
| 34.65 | 7.46(12) | 34.52 | 7.34(12) | 34.64 | 7.16(11) | 34.68 | 7.20(12) | 34.52 | 7.71(13) | 34.64 | 7.87(13) | 34.51 | 7.78(16) |
| 37.60 | 9.66(14) | 37.47 | 9.48(14) | 37.58 | 9.30(13) | 37.62 | 9.29(14) | 37.47 | 9.87(15) | 37.59 | 10.14(15) | 37.46 | 10.00(19) |
| 37.60 | 9.65(14) | 37.47 | 9.53(14) | 37.58 | 9.29(13) | 37.62 | 9.32(13) | 37.47 | 9.88(15) | 37.59 | 10.15(15) | 37.47 | 10.00(20) |
| 37.65 | 9.80(15) | 37.54 | 9.65(15) | 37.64 | 9.44(14) | 37.69 | 9.49(16) | 37.54 | 10.03(16) | 37.65 | 10.28(16) | 37.53 | 10.14(20) |
| 40.86 | 12.56(17) | 40.75 | 12.27(17) | 40.84 | 12.09(16) | 40.89 | 12.06(17) | 40.75 | 12.71(19) | 40.85 | 13.05(18) | 40.74 | 12.85(24) |
| 40.86 | 12.54(17) | 40.75 | 12.31(17) | 40.85 | 12.09(16) | 40.89 | 12.05(17) | 40.75 | 12.71(19) | 40.86 | 13.04(18) | 40.74 | 12.84(24) |
| 40.92 | 12.71(19) | 40.82 | 12.42(18) | 40.91 | 12.27(17) | 40.96 | 12.27(19) | 40.82 | 12.87(20) | 40.92 | 13.16(20) | 40.82 | 13.01(25) |
| 44.41 | 15.86(21) | 44.30 | 15.85(21) | 44.39 | 15.34(19) | 44.45 | 15.28(20) | 44.31 | 16.30(23) | 44.40 | 16.38(22) | 44.30 | 16.46(29) |
| 44.41 | 15.85(21) | 44.31 | 15.87(21) | 44.40 | 15.34(19) | 44.45 | 15.31(20) | 44.31 | 16.26(23) | 44.41 | 16.33(22) | 44.30 | 16.48(30) |
| 44.48 | 16.00(22) | 44.39 | 16.09(23) | 44.46 | 15.53(21) | 44.51 | 15.50(21) | 44.39 | 16.48(26) | 44.47 | 16.50(23) | 44.38 | 16.78(32) |
| 48.27 | 19.98(25) | 48.17 | 19.99(25) | 48.26 | 19.34(23) | 48.31 | 19.30(24) | 48.17 | 20.45(26) | 48.26 | 20.48(26) | 48.16 | 20.71(34) |
| 48.27 | 19.95(25) | 48.17 | 20.03(25) | 48.26 | 19.32(23) | 48.31 | 19.29(24) | 48.17 | 20.43(27) | 48.27 | 20.45(26) | 48.17 | 20.73(34) |
| 48.34 | 20.14(26) | 48.26 | 20.27(26) | 48.33 | 19.55(24) | 48.39 | 19.53(24) | 48.26 | 20.66(28) | 48.33 | 20.66(27) | 48.25 | 20.97(36) |
| 52.47 | 24.51(29) | 52.37 | 24.62(29) | 52.45 | 23.74(27) | 52.51 | 23.72(28) | 52.38 | 25.08(31) | 52.46 | 24.89(30) | 52.36 | 25.25(40) |
| 52.47 | 24.44(28) | 52.37 | 24.58(28) | 52.45 | 23.75(27) | 52.52 | 23.73(27) | 52.38 | 25.02(29) | 52.47 | 24.90(29) | 52.37 | 25.19(37) |
| 52.55 | 24.71(30) | 52.46 | 24.90(31) | 52.52 | 24.04(28) | 52.59 | 23.97(29) | 52.47 | 25.28(34) | 52.54 | 25.12(31) | 52.46 | 25.58(43) |
| 57.04 | 30.07(32) | 56.94 | 30.33(33) | 57.02 | 29.32(31) | 57.09 | 29.23(31) | 56.94 | 30.67(35) | 57.03 | 30.52(33) | 56.93 | 30.90(42) |
| 57.05 | 30.06(32) | 56.94 | 30.25(31) | 57.03 | 29.33(30) | 57.09 | 29.31(31) | 56.95 | 30.67(33) | 57.04 | 30.50(34) | 56.93 | 30.93(45) |
| 57.12 | 30.32(34) | 57.04 | 30.59(36) | 57.11 | 29.61(32) | 57.17 | 29.55(32) | 57.04 | 30.96(38) | 57.11 | 30.68(34) | 57.03 | 31.24(48) |
| 62.01 | 36.67(36) | 61.91 | 36.72(34) | 61.99 | 35.77(32) | 62.07 | 35.77(34) | 61.90 | 37.14(36) | 62.00 | 37.16(38) | 61.90 | 37.43(51) |
| 62.01 | 36.66(33) | 61.91 | 36.77(37) | 61.99 | 35.79(33) | 62.07 | 35.81(37) | 61.91 | 37.17(39) | 62.00 | 37.05(34) | 61.90 | 37.33(46) |
| 62.10 | 36.72(38) | 62.01 | 37.10(39) | 62.09 | 35.84(36) | 62.16 | 35.87(38) | 62.01 | 37.44(42) | 62.09 | 37.15(40) | 62.00 | 37.72(53) |
| 67.41 | 44.28(40) | 67.29 | 44.28(37) | 67.40 | 43.33(38) | 67.48 | 43.48(41) | 67.29 | 44.61(39) | 67.41 | 44.53(38) | 67.29 | 45.00(50) |
| 67.41 | 44.30(43) | 67.29 | 44.21(37) | 67.40 | 43.41(35) | 67.48 | 43.36(38) | 67.29 | 44.55(40) | 67.41 | 44.61(37) | 67.30 | 44.94(56) |
| 67.49 | 44.80(43) | 67.40 | 44.76(43) | 67.50 | 43.67(40) | 67.58 | 43.75(42) | 67.41 | 44.85(44) | 67.50 | 45.22(44) | 67.40 | 45.20(57) |
| 73.26 | 52.59(41) | 73.16 | 52.59(41) | 73.26 | 51.57(41) | 73.35 | 51.71(45) | 73.17 | 53.04(42) | 73.27 | 52.71(40) | 73.16 | 52.97(51) |
| 73.26 | 52.33(40) | 73.16 | 52.69(43) | 73.26 | 51.41(40) | 73.35 | 51.38(41) | 73.17 | 53.16(41) | 73.27 | 52.77(45) | 73.16 | 53.12(59) |
| 73.36 | 53.04(44) | 73.27 | 52.99(43) | 73.36 | 52.29(44) | 73.45 | 52.22(45) | 73.28 | 52.99(48) | 73.37 | 53.36(46) | 73.27 | 53.70(61) |
| 79.63 | 62.90(46) | 79.55 | 62.36(43) | 79.63 | 61.82(41) | 79.73 | 61.65(46) | 79.56 | 62.35(42) | 79.63 | 62.92(45) | 79.55 | 62.60(56) |
| 79.63 | 62.52(44) | 79.55 | 62.42(42) | 79.64 | 61.39(44) | 79.73 | 61.33(45) | 79.56 | 62.47(45) | 79.64 | 62.96(45) | 79.55 | 62.64(58) |
| 79.74 | 63.09(52) | 79.67 | 62.70(50) | 79.75 | 61.89(46) | 79.84 | 62.11(47) | 79.68 | 62.57(49) | 79.74 | 63.29(51) | 79.67 | 63.18(68) |
| 86.55 | 73.61(48) | 86.47 | 72.85(45) | 86.56 | 72.09(46) | 86.62 | 72.63(47) | 86.48 | 72.55(47) | 86.56 | 74.02(47) | 86.48 | 73.01(60) |
| 86.56 | 73.62(46) | 86.48 | 72.40(44) | 86.56 | 72.44(45) | 86.62 | 72.53(47) | 86.49 | 72.85(46) | 86.56 | 73.82(48) | 86.49 | 72.66(58) |
| 86.66 | 73.88(53) | 86.60 | 73.06(50) | 86.67 | 72.75(51) | 86.73 | 72.96(52) | 86.61 | 72.98(53) | 86.67 | 74.23(52) | 86.61 | 73.11(69) |
| 94.08 | 84.59(48) | 94.02 | 84.47(46) | 94.09 | 83.31(46) | 94.16 | 84.16(47) | 94.02 | 84.73(49) | 94.09 | 85.18(48) | 94.02 | 84.23(60) |
| 94.09 | 84.50(46) | 94.02 | 84.40(47) | 94.09 | 83.58(47) | 94.16 | 83.87(50) | 94.02 | 84.76(48) | 94.09 | 85.30(50) | 94.02 | 84.58(59) |
| 94.20 | 85.03(53) | 94.15 | 84.80(53) | 94.21 | 83.68(52) | 94.27 | 84.67(55) | 94.15 | 85.20(58) | 94.20 | 85.55(54) | 94.15 | 84.90(71) |
| 102.28 | 98.02(51) | 102.21 | 97.82(50) | 102.29 | 96.71(49) | 102.36 | 97.06(52) | 102.22 | 98.20(49) | 102.29 | 98.75(49) | 102.21 | 97.77(61) |
| 102.28 | 98.03(52) | 102.21 | 97.81(47) | 102.29 | 96.72(49) | 102.36 | 97.42(54) | 102.22 | 97.99(51) | 102.29 | 98.66(49) | 102.21 | 98.25(64) |
| 102.40 | 98.56(54) | 102.34 | 98.18(57) | 102.41 | 97.01(55) | 102.48 | 97.63(57) | 102.36 | 98.34(58) | 102.41 | 98.95(57) | 102.35 | 98.59(78) |
| 111.19 | 112.22(53) | 111.12 | 111.54(54) | 111.20 | 110.62(52) | 111.28 | 111.39(56) | 111.12 | 111.95(54) | 111.20 | 112.87(52) | 111.12 | 112.22(65) |
| 111.19 | 112.11(51) | 111.12 | 111.74(55) | 111.21 | 110.62(53) | 111.28 | 111.42(55) | 111.13 | 112.16(54) | 111.20 | 112.95(51) | 111.12 | 111.90(67) |
| 111.31 | 112.53(60) | 111.25 | 112.15(63) | 111.33 | 110.89(58) | 111.40 | 111.76(61) | 111.26 | 112.62(61) | 111.32 | 113.20(60) | 111.25 | 112.47(80) |
| 120.88 | 128.20(56) | 120.81 | 127.13(51) | 120.89 | 126.41(56) | 120.97 | 127.57(63) | 120.82 | 127.83(56) | 120.89 | 128.87(56) | 120.82 | 128.24(67) |
| 120.89 | 127.72(55) | 120.81 | 127.20(50) | 120.89 | 126.16(56) | 120.97 | 127.53(59) | 120.83 | 128.23(50) | 120.89 | 128.79(53) | 120.82 | 128.01(62) |
| 121.01 | 127.89(61) | 120.96 | 127.76(63) | 121.02 | 126.77(65) | 121.11 | 127.75(65) | 120.96 | 128.22(56) | 121.02 | 129.25(63) | 120.96 | 128.42(80) |
| 131.42 | 142.91(50) | 131.35 | 143.36(55) | 131.43 | 141.97(54) | 131.52 | 143.04(59) | 131.37 | 144.35(53) | 131.42 | 144.05(50) | 131.36 | 144.56(68) |
| 131.42 | 143.31(50) | 131.35 | 143.31(56) | 131.43 | 141.72(55) | 131.52 | 143.53(61) | 131.37 | 144.46(55) | 131.42 | 144.39(47) | 131.36 | 144.48(67) |
| 131.54 | 143.48(65) | 131.49 | 143.64(59) | 131.56 | 142.21(64) | 131.66 | 143.29(64) | 131.50 | 144.56(59) | 131.55 | 144.83(58) | 131.50 | 144.27(71) |
| 142.88 | 160.10(54) | 142.81 | 159.91(57) | 142.90 | 158.67(60) | 142.99 | 160.36(65) | 142.84 | 161.20(55) | 142.89 | 161.76(53) | 142.83 | 160.90(68) |
| 142.89 | 160.58(55) | 142.82 | 160.10(56) | 142.90 | 158.58(59) | 142.99 | 160.20(64) | 142.84 | 161.19(56) | 142.89 | 161.65(52) | 142.83 | 160.63(66) |
| 143.00 | 161.68(67) | 142.97 | 160.18(68) | 143.01 | 159.88(67) | 143.11 | 161.41(71) | 142.98 | 161.35(71) | 143.00 | 163.12(65) | 142.97 | 161.30(93) |
| 155.32 | 177.84(57) | 155.28 | 177.13(56) | 155.34 | 176.41(61) | 155.44 | 178.20(68) | 155.30 | 178.59(54) | 155.33 | 179.80(55) | 155.29 | 177.59(66) |
| 155.33 | 177.95(56) | 155.28 | 176.91(55) | 155.35 | 176.20(59) | 155.44 | 178.27(67) | 155.30 | 178.28(51) | 155.33 | 179.30(53) | 155.30 | 177.84(64) |
| 155.44 | 178.12(69) | 155.41 | 179.44(69) | 155.46 | 176.45(67) | 155.56 | 178.63(75) | 155.42 | 181.13(67) | 155.44 | 180.09(66) | 155.43 | 180.56(85) |
| 168.86 | 196.31(61) | 168.82 | 195.80(57) | 168.88 | 194.97(66) | 168.99 | 196.34(68) | 168.86 | 198.20(54) | 168.85 | 198.19(55) | 168.83 | 197.49(66) |
| 168.87 | 196.26(57) | 168.82 | 195.88(56) | 168.88 | 195.05(64) | 168.99 | 196.38(68) | 168.86 | 198.10(56) | 168.85 | 197.97(52) | 168.83 | 197.13(69) |
| 168.97 | 196.77(71) | 168.96 | 196.24(70) | 168.99 | 195.27(73) | 169.10 | 196.47(77) | 168.97 | 198.61(71) | 168.96 | 198.48(72) | 168.97 | 197.50(96) |
| 183.64 | 216.20(58) | 183.60 | 215.94(58) | 183.66 | 215.88(59) | 183.79 | 216.29(67) | 183.63 | 217.68(57) | 183.66 | 218.66(52) | 183.61 | 217.78(69) |
| 183.64 | 216.68(59) | 183.61 | 215.96(58) | 183.66 | 215.83(59) | 183.79 | 216.09(63) | 183.63 | 217.67(55) | 183.66 | 217.99(52) | 183.61 | 217.90(71) |
| 183.73 | 216.25(71) | 183.73 | 216.16(73) | 183.77 | 216.29(74) | 183.89 | 216.36(74) | 183.73 | 217.80(73) | 183.74 | 218.69(70) | 183.73 | 218.75(89) |
| 199.62 | 234.85(64) | 199.60 | 234.86(59) | 199.64 | 234.54(62) | 199.77 | 235.52(66) | 199.63 | 236.99(56) | 199.64 | 237.24(55) | 199.61 | 237.42(67) |
| 199.62 | 235.11(64) | 199.60 | 235.40(56) | 199.64 | 234.66(62) | 199.77 | 235.38(68) | 199.63 | 237.34(56) | 199.64 | 237.06(53) | 199.61 | 237.79(73) |
| 199.68 | 234.85(76) | 199.69 | 235.34(67) | 199.71 | 234.40(72) | 199.86 | 235.55(78) | 199.70 | 237.55(64) | 199.71 | 237.65(69) | 199.69 | 237.54(81) |
| 216.98 | 253.91(65) | 216.99 | 254.09(62) | 217.01 | 254.44(71) | 217.15 | 255.03(73) | 217.02 | 256.40(57) | 217.01 | 256.51(58) | 217.00 | 256.45(71) |
| 216.98 | 254.40(66) | 216.99 | 253.91(63) | 217.01 | 254.32(69) | 217.15 | 255.03(75) | 217.02 | 256.16(58) | 217.01 | 256.92(58) | 217.00 | 256.47(69) |
| 217.00 | 253.96(76) | 217.03 | 253.85(75) | 217.04 | 254.16(84) | 217.20 | 255.17(85) | 217.06 | 256.55(76) | 217.04 | 257.20(79) | 217.04 | 256.58(96) |
| 235.86 | 270.66(86) | 235.90 | 270.45(63) | 235.90 | 271.40(72) | 236.05 | 271.63(87) | 235.93 | 273.32(72) | 235.86 | 273.53(76) | 235.90 | 272.93(87) |
| 235.87 | 271.46(70) | 235.90 | 270.39(62) | 235.90 | 271.03(85) | 236.05 | 271.59(77) | 235.93 | 272.87(62) | 235.89 | 273.73(62) | 235.91 | 272.21(69) |
| 235.88 | 270.46(74) | 235.90 | 270.39(73) | 235.91 | 271.46(74) | 236.05 | 271.68(74) | 235.93 | 272.58(64) | 235.90 | 273.76(62) | 235.91 | 272.49(73) |
| 256.33 | 288.22(79) | 256.39 | 288.68(74) | 256.37 | 289.37(78) | 256.56 | 289.82(89) | 256.42 | 291.27(66) | 256.35 | 291.66(67) | 256.38 | 290.41(68) |
| 256.39 | 288.67(71) | 256.44 | 288.43(57) | 256.43 | 289.81(72) | 256.59 | 289.75(80) | 256.46 | 291.56(58) | 256.43 | 291.79(56) | 256.45 | 290.83(68) |
| 256.41 | 288.48(74) | 256.45 | 288.86(65) | 256.44 | 289.81(72) | 256.61 | 289.83(83) | 256.48 | 291.34(60) | 256.44 | 292.24(57) | 256.47 | 290.63(66) |
| 278.53 | 307.30(109) | 278.62 | 308.90(77) | 278.60 | 308.45(111) | 278.79 | 307.99(100) | 278.65 | 312.39(113) | 278.58 | 311.79(102) | 278.61 | 311.90(141) |
| 278.68 | 307.31(84) | 278.74 | 308.92(74) | 278.72 | 308.73(85) | 278.90 | 308.34(95) | 278.76 | 312.10(73) | 278.72 | 311.39(72) | 278.74 | 311.58(91) |
| 278.70 | 307.31(84) | 278.75 | 309.15(74) | 278.74 | 308.92(86) | 278.91 | 308.11(92) | 278.77 | 311.81(69) | 278.73 | 311.53(75) | 278.76 | 311.68(89) |
| 302.80 | 323.99(88) | 302.80 | 325.12(81) | 302.79 | 325.99(97) | 302.99 | 325.31(110) | 302.80 | 327.58(89) | 302.80 | 328.63(86) | 302.82 | 328.12(102) |
| 302.94 | 324.71(83) | 303.00 | 325.79(72) | 302.97 | 325.96(92) | 303.17 | 326.50(95) | 303.04 | 328.65(70) | 302.97 | 328.67(73) | 303.02 | 327.62(85) |
| 302.95 | 324.68(81) | 303.01 | 325.58(72) | 302.99 | 326.50(91) | 303.18 | 326.21(96) | 303.05 | 328.93(76) | 302.98 | 328.95(73) | 303.02 | 328.84(136) |

APPENDIX. Continued

| Py75Gr25 #1 Source: Geiger |  | Py60Gr40 #1 Source: HW80 |  | Py60Gr40 #2 Source: Geiger |  | Py50Gr50 #1 Source: Geiger |  | Py25Gr75 #1 Source: Geiger |  | Py10Gr90 #1 Source: Geiger |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FW | 415.716 | FW | 422.059 | FW | 422.059 | FW | 427.358 | FW | 439.094 | FW | 445.722 |
| SW | 21.220 | SW | 24.050 | SW | 21.911 | SW | 23.220 | SW | 21.023 | SW | 25.012 |
| XGr | 0.264 | XGr | 0.400 | XGr | 0.414 | XGr | 0.512 | XGr | 0.760 | XGr | 0.904 |
| T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] |
| 5.133 | 0.002(1) | 5.055 | 0.008(1) | 5.060 | 0.015(1) | 5.055 | 0.015(1) | 5.139 | 0.026(3) | 5.131 | 0.031(3) |
| 5.136 | 0.012(1) | 5.062 | 0.010(4) | 5.067 | 0.011(1) | 5.062 | 0.012(1) | 5.147 | 0.025(2) | 5.136 | 0.028(1) |
| 5.138 | 0.011(1) | 5.065 | 0.013(1) | 5.071 | 0.014(1) | 5.067 | 0.012(1) | 5.150 | 0.017(2) | 5.142 | 0.021(1) |
| 5.580 | 0.019(1) | 5.494 | 0.010(1) | 5.498 | 0.013(1) | 5.498 | 0.015(1) | 5.582 | 0.029(1) | 5.580 | 0.033(1) |
| 5.588 | 0.011(1) | 5.500 | 0.015(1) | 5.504 | 0.014(1) | 5.504 | 0.017(1) | 5.582 | 0.024(1) | 5.590 | 0.029(2) |
| 5.592 | 0.014(1) | 5.504 | 0.010(2) | 5.510 | 0.013(1) | 5.510 | 0.014(1) | 5.588 | 0.030(2) | 5.592 | 0.029(4) |
| 6.064 | 0.022(1) | 5.973 | 0.014(1) | 5.978 | 0.017(2) | 5.981 | 0.019(1) | 6.066 | 0.040(2) | 6.059 | 0.042(3) |
| 6.070 | 0.021(1) | 5.979 | 0.016(1) | 5.991 | 0.022(1) | 5.987 | 0.022(1) | 6.074 | 0.035(1) | 6.069 | 0.041(2) |
| 6.076 | 0.021(2) | 5.985 | 0.014(1) | 5.991 | 0.018(1) | 5.992 | 0.021(1) | 6.078 | 0.038(2) | 6.074 | 0.039(4) |
| 6.585 | 0.033(3) | 6.487 | 0.023(1) | 6.499 | 0.029(1) | 6.497 | 0.031(1) | 6.589 | 0.064(2) | 6.585 | 0.068(1) |
| 6.594 | 0.032(4) | 6.495 | 0.023(1) | 6.505 | 0.027(1) | 6.504 | 0.032(1) | 6.598 | 0.057(2) | 6.593 | 0.068(1) |
| 6.598 | 0.032(1) | 6.502 | 0.024(1) | 6.511 | 0.028(1) | 6.511 | 0.031(1) | 6.603 | 0.061(1) | 6.600 | 0.063(1) |
| 7.177 | 0.039(2) | 7.070 | 0.034(1) | 7.080 | 0.040(1) | 7.080 | 0.046(1) | 7.180 | 0.083(2) | 7.175 | 0.087(1) |
| 7.178 | 0.038(1) | 7.074 | 0.035(1) | 7.082 | 0.040(1) | 7.082 | 0.044(1) | 7.182 | 0.083(1) | 7.177 | 0.088(3) |
| 7.178 | 0.035(2) | 7.074 | 0.034(1) | 7.084 | 0.039(1) | 7.082 | 0.043(1) | 7.183 | 0.081(2) | 7.179 | 0.089(1) |
| 7.737 | 0.044(2) | 7.664 | 0.040(2) | 7.667 | 0.047(2) | 7.669 | 0.055(2) | 7.740 | 0.106(2) | 7.739 | 0.116(2) |
| 7.741 | 0.046(2) | 7.669 | 0.040(1) | 7.674 | 0.047(2) | 7.674 | 0.055(1) | 7.745 | 0.106(2) | 7.744 | 0.114(2) |
| 7.746 | 0.046(1) | 7.676 | 0.040(1) | 7.680 | 0.047(2) | 7.680 | 0.055(1) | 7.750 | 0.105(2) | 7.748 | 0.116(2) |
| 8.408 | 0.056(3) | 8.330 | 0.051(2) | 8.336 | 0.058(3) | 8.336 | 0.071(2) | 8.409 | 0.142(3) | 8.406 | 0.150(3) |
| 8.410 | 0.057(2) | 8.335 | 0.051(2) | 8.341 | 0.057(2) | 8.340 | 0.071(2) | 8.415 | 0.141(3) | 8.411 | 0.149(2) |
| 8.416 | 0.056(2) | 8.343 | 0.052(2) | 8.347 | 0.057(2) | 8.346 | 0.072(2) | 8.418 | 0.139(2) | 8.415 | 0.147(2) |
| 9.132 | 0.077(3) | 9.055 | 0.073(3) | 9.061 | 0.081(3) | 9.061 | 0.101(3) | 9.140 | 0.194(3) | 9.137 | 0.198(3) |
| 9.135 | 0.076(2) | 9.060 | 0.074(2) | 9.064 | 0.080(2) | 9.064 | 0.100(2) | 9.143 | 0.192(3) | 9.140 | 0.195(2) |
| 9.142 | 0.076(2) | 9.067 | 0.073(2) | 9.071 | 0.081(2) | 9.070 | 0.101(2) | 9.146 | 0.193(3) | 9.142 | 0.196(2) |
| 9.926 | 0.101(3) | 9.842 | 0.102(3) | 9.848 | 0.110(3) | 9.848 | 0.141(3) | 9.930 | 0.261(5) | 9.927 | 0.253(3) |
| 9.929 | 0.102(3) | 9.848 | 0.101(3) | 9.851 | 0.108(3) | 9.850 | 0.140(3) | 9.933 | 0.258(4) | 9.929 | 0.253(3) |
| 9.936 | 0.102(3) | 9.855 | 0.102(2) | 9.857 | 0.110(3) | 9.857 | 0.140(3) | 9.936 | 0.258(3) | 9.933 | 0.254(3) |
| 10.792 | 0.128(5) | 10.698 | 0.134(4) | 10.705 | 0.142(4) | 10.705 | 0.189(4) | 10.800 | 0.333(6) | 10.793 | 0.315(4) |
| 10.795 | 0.126(3) | 10.705 | 0.135(4) | 10.708 | 0.143(4) | 10.707 | 0.188(4) | 10.800 | 0.334(4) | 10.794 | 0.315(3) |
| 10.802 | 0.126(3) | 10.712 | 0.134(3) | 10.714 | 0.143(3) | 10.713 | 0.188(3) | 10.804 | 0.334(4) | 10.799 | 0.314(3) |
| 11.726 | 0.165(5) | 11.631 | 0.181(6) | 11.641 | 0.191(5) | 11.641 | 0.254(5) | 11.730 | 0.438(6) | 11.728 | 0.393(5) |
| 11.729 | 0.166(4) | 11.639 | 0.181(4) | 11.644 | 0.188(4) | 11.643 | 0.253(4) | 11.731 | 0.437(6) | 11.729 | 0.394(4) |
| 11.736 | 0.165(4) | 11.647 | 0.182(4) | 11.650 | 0.189(4) | 11.649 | 0.253(4) | 11.735 | 0.437(5) | 11.733 | 0.390(4) |
| 12.741 | 0.227(7) | 12.656 | 0.264(6) | 12.653 | 0.271(8) | 12.653 | 0.361(7) | 12.752 | 0.571(6) | 12.747 | 0.494(6) |
| 12.743 | 0.227(6) | 12.657 | 0.261(5) | 12.655 | 0.270(5) | 12.654 | 0.359(6) | 12.754 | 0.568(6) | 12.749 | 0.491(8) |
| 12.750 | 0.224(5) | 12.661 | 0.263(4) | 12.662 | 0.270(5) | 12.660 | 0.360(5) | 12.754 | 0.569(7) | 12.749 | 0.491(5) |
| 13.847 | 0.315(10) | 13.755 | 0.377(6) | 13.753 | 0.390(9) | 13.753 | 0.506(7) | 13.855 | 0.739(7) | 13.850 | 0.611(7) |
| 13.848 | 0.309(7) | 13.757 | 0.381(8) | 13.754 | 0.384(6) | 13.753 | 0.508(9) | 13.857 | 0.738(7) | 13.851 | 0.609(6) |
| 13.854 | 0.308(6) | 13.760 | 0.377(6) | 13.760 | 0.385(6) | 13.759 | 0.507(6) | 13.861 | 0.741(12) | 13.852 | 0.609(10) |
| 15.052 | 0.426(9) | 14.949 | 0.523(8) | 14.951 | 0.527(9) | 14.952 | 0.686(9) | 15.058 | 0.929(10) | 15.053 | 0.747(8) |
| 15.056 | 0.423(11) | 14.952 | 0.527(11) | 14.954 | 0.534(11) | 14.955 | 0.692(12) | 15.060 | 0.933(10) | 15.054 | 0.745(9) |
| 15.057 | 0.421(8) | 14.955 | 0.523(7) | 14.957 | 0.530(8) | 14.955 | 0.685(8) | 15.066 | 0.937(11) | 15.062 | 0.753(10) |
| 16.362 | 0.585(11) | 16.251 | 0.727(10) | 16.252 | 0.732(11) | 16.251 | 0.929(11) | 16.365 | 1.173(12) | 16.359 | 0.911(11) |
| 16.365 | 0.585(11) | 16.254 | 0.724(9) | 16.256 | 0.728(10) | 16.253 | 0.932(11) | 16.367 | 1.182(13) | 16.361 | 0.918(11) |
| 16.372 | 0.590(15) | 16.256 | 0.734(15) | 16.258 | 0.739(16) | 16.256 | 0.936(16) | 16.378 | 1.184(16) | 16.372 | 0.917(14) |
| 17.784 | 0.815(14) | 17.666 | 1.010(14) | 17.667 | 1.011(14) | 17.668 | 1.253(15) | 17.782 | 1.467(16) | 17.777 | 1.103(14) |
| 17.784 | 0.816(15) | 17.667 | 1.009(13) | 17.671 | 1.013(14) | 17.669 | 1.258(14) | 17.789 | 1.466(16) | 17.782 | 1.103(14) |
| 17.801 | 0.814(19) | 17.673 | 1.017(19) | 17.675 | 1.024(20) | 17.676 | 1.267(20) | 17.803 | 1.474(22) | 17.796 | 1.111(18) |
| 19.321 | 1.107(18) | 19.198 | 1.359(16) | 19.202 | 1.359(18) | 19.200 | 1.640(18) | 19.317 | 1.808(21) | 19.312 | 1.325(17) |
| 19.321 | 1.103(19) | 19.198 | 1.361(16) | 19.204 | 1.358(18) | 19.201 | 1.639(18) | 19.319 | 1.803(20) | 19.315 | 1.330(17) |
| 19.347 | 1.123(22) | 19.214 | 1.376(24) | 19.220 | 1.372(24) | 19.215 | 1.661(24) | 19.342 | 1.831(25) | 19.336 | 1.346(22) |
| 21.00 | 1.50(2) | 20.87 | 1.82(2) | 20.86 | 1.82(3) | 20.86 | 2.14(2) | 20.99 | 2.22(3) | 20.98 | 1.61(2) |
| 21.00 | 1.51(3) | 20.87 | 1.82(2) | 20.87 | 1.82(2) | 20.87 | 2.13(3) | 21.00 | 2.22(3) | 20.99 | 1.61(2) |
| 21.03 | 1.55(3) | 20.89 | 1.85(3) | 20.89 | 1.84(3) | 20.90 | 2.16(3) | 21.03 | 2.21(3) | 21.02 | 1.61(3) |
| 22.81 | 2.04(3) | 22.67 | 2.40(3) | 22.68 | 2.38(3) | 22.67 | 2.72(3) | 22.81 | 2.65(4) | 22.80 | 1.94(3) |
| 22.81 | 2.05(3) | 22.68 | 2.39(3) | 22.68 | 2.38(3) | 22.68 | 2.72(3) | 22.82 | 2.71(4) | 22.81 | 1.94(3) |
| 22.85 | 2.07(4) | 22.71 | 2.42(4) | 22.71 | 2.40(4) | 22.71 | 2.75(4) | 22.85 | 2.71(4) | 22.85 | 1.98(4) |
| 24.79 | 2.79(5) | 24.66 | 3.08(8) | 24.65 | 3.14(4) | 24.65 | 3.50(4) | 24.79 | 3.36(5) | 24.78 | 2.43(4) |
| 24.79 | 2.78(6) | 24.67 | 3.07(10) | 24.66 | 3.12(4) | 24.65 | 3.50(5) | 24.80 | 3.26(5) | 24.78 | 2.46(4) |
| 24.83 | 2.81(5) | 24.68 | 3.21(5) | 24.69 | 3.17(5) | 24.69 | 3.54(5) | 24.83 | 3.36(6) | 24.82 | 2.44(5) |
| 26.94 | 3.86(7) | 26.80 | 4.11(6) | 26.80 | 4.07(5) | 26.80 | 4.43(5) | 26.94 | 4.06(7) | 26.93 | 3.00(6) |
| 26.95 | 3.61(6) | 26.80 | 4.11(5) | 26.81 | 4.19(11) | 26.81 | 4.42(5) | 26.94 | 4.07(7) | 26.94 | 2.99(6) |
| 26.99 | 3.83(9) | 26.85 | 4.15(7) | 26.84 | 4.35(12) | 26.84 | 4.69(11) | 26.98 | 4.15(9) | 26.97 | 3.15(8) |
| 29.28 | 4.85(8) | 29.14 | 5.24(7) | 29.14 | 5.23(7) | 29.14 | 5.55(7) | 29.27 | 4.91(8) | 29.27 | 3.67(6) |
| 29.28 | 4.84(8) | 29.14 | 5.26(7) | 29.14 | 5.22(7) | 29.14 | 5.55(7) | 29.27 | 4.89(8) | 29.27 | 3.67(7) |
| 29.33 | 4.88(10) | 29.19 | 5.32(8) | 29.19 | 5.30(8) | 29.19 | 5.63(8) | 29.33 | 4.93(10) | 29.32 | 3.70(8) |
| 31.82 | 6.31(10) | 31.69 | 6.64(9) | 31.68 | 6.57(9) | 31.68 | 6.85(9) | 31.81 | 6.02(11) | 31.81 | 4.59(9) |
| 31.82 | 6.33(10) | 31.69 | 6.63(9) | 31.69 | 6.58(10) | 31.69 | 6.88(9) | 31.81 | 6.01(11) | 31.81 | 4.61(9) |
| 31.87 | 6.37(12) | 31.74 | 6.70(9) | 31.74 | 6.65(10) | 31.74 | 6.95(10) | 31.87 | 6.07(12) | 31.86 | 4.67(10) |
| 34.58 | 8.26(13) | 34.46 | 8.44(11) | 34.46 | 8.38(12) | 34.46 | 8.59(12) | 34.57 | 7.49(13) | 34.57 | 5.95(11) |
| 34.58 | 8.24(13) | 34.46 | 8.45(11) | 34.46 | 8.39(12) | 34.46 | 8.60(12) | 34.57 | 7.50(13) | 34.57 | 5.94(11) |
| 34.63 | 8.36(14) | 34.52 | 8.55(12) | 34.52 | 8.50(13) | 34.52 | 8.72(13) | 34.63 | 7.63(14) | 34.62 | 6.03(12) |
| 37.58 | 10.61(16) | 37.47 | 10.60(14) | 37.47 | 10.51(15) | 37.47 | 10.70(15) | 37.58 | 9.34(17) | 37.57 | 7.62(14) |
| 37.58 | 10.59(16) | 37.47 | 10.59(14) | 37.48 | 10.49(16) | 37.47 | 10.64(15) | 37.58 | 9.36(17) | 37.57 | 7.60(14) |
| 37.64 | 10.71(17) | 37.54 | 10.75(15) | 37.54 | 10.66(16) | 37.54 | 10.78(16) | 37.64 | 9.51(18) | 37.63 | 7.73(15) |
| 40.85 | 13.44(20) | 40.75 | 13.14(18) | 40.74 | 13.08(19) | 40.75 | 13.16(19) | 40.84 | 11.63(21) | 40.84 | 9.79(18) |
| 40.85 | 13.43(20) | 40.75 | 13.18(18) | 40.75 | 13.09(20) | 40.75 | 13.13(19) | 40.84 | 11.66(21) | 40.84 | 9.78(18) |
| 40.91 | 13.59(21) | 40.83 | 13.31(19) | 40.82 | 13.23(20) | 40.82 | 13.28(19) | 40.90 | 11.82(22) | 40.90 | 9.94(19) |
| 44.40 | 16.60(23) | 44.31 | 16.40(22) | 44.31 | 16.32(23) | 44.30 | 16.25(23) | 44.39 | 14.25(24) | 44.39 | 12.29(21) |
| 44.40 | 16.62(23) | 44.31 | 16.45(21) | 44.31 | 16.35(24) | 44.30 | 16.29(23) | 44.39 | 14.23(25) | 44.39 | 12.28(21) |
| 44.46 | 16.82(25) | 44.39 | 16.61(24) | 44.39 | 16.56(26) | 44.38 | 16.50(25) | 44.46 | 14.44(26) | 44.45 | 12.44(23) |
| 48.26 | 20.62(27) | 48.17 | 20.21(25) | 48.17 | 20.15(27) | 48.17 | 19.95(26) | 48.25 | 17.62(29) | 48.25 | 15.55(25) |
| 48.26 | 20.56(28) | 48.17 | 20.19(25) | 48.17 | 20.14(28) | 48.17 | 19.97(27) | 48.25 | 17.63(29) | 48.25 | 15.60(25) |
| 48.33 | 20.81(30) | 48.26 | 20.40(27) | 48.26 | 20.39(30) | 48.25 | 20.16(28) | 48.32 | 17.90(31) | 48.32 | 15.81(26) |
| 52.45 | 24.83(32) | 52.37 | 24.41(30) | 52.37 | 24.28(32) | 52.37 | 24.01(29) | 52.45 | 21.34(33) | 52.44 | 19.28(28) |
| 52.46 | 24.89(32) | 52.37 | 24.34(27) | 52.37 | 24.28(30) | 52.37 | 24.01(31) | 52.45 | 21.36(33) | 52.45 | 19.36(29) |
| 52.53 | 25.07(33) | 52.47 | 24.59(31) | 52.47 | 24.61(35) | 52.46 | 24.27(34) | 52.53 | 21.62(34) | 52.52 | 19.50(30) |
| 57.02 | 30.20(36) | 56.94 | 29.54(31) | 56.94 | 29.52(34) | 56.94 | 29.12(33) | 57.02 | 26.34(38) | 57.02 | 24.21(34) |
| 57.03 | 30.25(36) | 56.94 | 29.60(33) | 56.94 | 29.50(37) | 56.94 | 29.16(35) | 57.02 | 26.36(39) | 57.02 | 24.21(34) |
| 57.11 | 30.51(38) | 57.03 | 29.83(36) | 57.04 | 29.84(39) | 57.03 | 29.46(38) | 57.09 | 26.53(39) | 57.10 | 24.39(35) |
| 61.99 | 36.51(37) | 61.90 | 35.51(37) | 61.91 | 35.48(38) | 61.90 | 35.16(40) | 61.99 | 32.22(44) | 61.98 | 30.04(38) |
| 61.99 | 36.62(40) | 61.90 | 35.50(34) | 61.91 | 35.55(41) | 61.90 | 35.03(37) | 61.99 | 32.11(40) | 61.98 | 29.96(35) |
| 62.08 | 36.55(43) | 62.00 | 35.72(39) | 62.01 | 35.84(43) | 62.00 | 35.49(42) | 62.08 | 32.15(45) | 62.08 | 30.05(40) |
| 67.40 | 43.77(46) | 67.29 | 42.46(37) | 67.30 | 42.56(41) | 67.30 | 41.89(39) | 67.39 | 39.36(44) | 67.39 | 37.21(38) |
| 67.40 | 43.80(42) | 67.30 | 42.53(41) | 67.30 | 42.57(40) | 67.30 | 42.09(40) | 67.39 | 39.51(45) | 67.39 | 36.91(36) |
| 67.49 | 44.47(50) | 67.40 | 42.98(42) | 67.41 | 42.82(47) | 67.41 | 42.34(44) | 67.49 | 39.38(50) | 67.48 | 37.55(44) |
| 73.26 | 51.73(46) | 73.17 | 50.57(40) | 73.16 | 50.49(47) | 73.16 | 50.01(41) | 73.25 | 46.78(48) | 73.25 | 44.84(41) |
| 73.26 | 51.78(48) | 73.17 | 50.62(45) | 73.17 | 50.18(45) | 73.16 | 50.05(41) | 73.26 | 46.72(47) | 73.25 | 44.93(38) |
| 73.36 | 52.54(50) | 73.29 | 50.82(47) | 73.29 | 51.08(49) | 73.28 | 50.16(48) | 73.36 | 47.53(52) | 73.35 | 45.45(46) |
| 79.63 | 62.31(48) | 79.56 | 59.80(44) | 79.56 | 59.43(45) | 79.55 | 59.16(47) | 79.63 | 57.18(52) | 79.63 | 54.70(45) |
| 79.64 | 61.69(51) | 79.56 | 59.63(42) | 79.56 | 59.59(46) | 79.55 | 59.20(45) | 79.63 | 56.99(54) | 79.63 | 55.09(47) |
| 79.74 | 62.30(54) | 79.67 | 60.03(49) | 79.68 | 60.10(57) | 79.67 | 59.65(53) | 79.73 | 57.42(56) | 79.73 | 55.38(52) |
| 86.55 | 73.06(55) | 86.47 | 69.82(46) | 86.49 | 69.85(49) | 86.49 | 69.21(49) | 86.55 | 67.28(54) | 86.55 | 65.16(46) |
| 86.55 | 72.65(53) | 86.48 | 69.59(45) | 86.50 | 70.02(52) | 86.49 | 69.42(47) | 86.55 | 67.39(54) | 86.55 | 65.88(49) |
| 86.66 | 72.95(53) | 86.60 | 70.23(53) | 86.62 | 70.47(57) | 86.61 | 69.74(54) | 86.66 | 67.62(60) | 86.66 | 65.84(49) |
| 94.09 | 83.72(51) | 94.02 | 81.37(47) | 94.04 | 81.41(52) | 94.02 | 80.94(48) | 94.08 | 78.46(55) | 94.08 | 76.91(49) |
| 94.09 | 83.75(52) | 94.02 | 81.39(49) | 94.04 | 81.56(52) | 94.02 | 81.03(50) | 94.09 | 78.19(53) | 94.08 | 76.87(50) |
| 94.20 | 83.92(57) | 94.15 | 81.72(53) | 94.17 | 81.99(63) | 94.15 | 81.41(59) | 94.20 | 78.59(61) | 94.20 | 77.16(55) |
| 102.28 | 97.34(53) | 102.21 | 94.67(50) | 102.22 | 95.19(55) | 102.21 | 94.27(51) | 102.28 | 92.30(58) | 102.27 | 90.67(48) |
| 102.28 | 97.12(53) | 102.21 | 94.74(49) | 102.23 | 94.84(54) | 102.22 | 94.39(52) | 102.28 | 91.95(56) | 102.27 | 90.69(50) |
| 102.40 | 97.65(61) | 102.34 | 95.01(56) | 102.36 | 95.42(62) | 102.35 | 94.88(60) | 102.40 | 92.36(66) | 102.39 | 91.03(56) |
| 111.20 | 111.44(58) | 111.12 | 108.66(52) | 111.14 | 109.05(57) | 111.13 | 108.56(55) | 111.19 | 106.66(61) | 111.19 | 105.37(55) |
| 111.20 | 111.24(56) | 111.12 | 108.71(51) | 111.14 | 108.94(57) | 111.13 | 108.51(53) | 111.19 | 106.55(60) | 111.19 | 105.09(53) |
| 111.31 | 111.62(64) | 111.25 | 109.06(61) | 111.28 | 109.42(68) | 111.26 | 109.10(68) | 111.31 | 107.24(64) | 111.31 | 105.65(60) |
| 120.88 | 127.26(59) | 120.81 | 124.97(52) | 120.84 | 124.91(57) | 120.82 | 124.79(56) | 120.88 | 123.04(63) | 120.88 | 122.03(55) |
| 120.88 | 127.49(60) | 120.81 | 124.68(52) | 120.84 | 124.97(57) | 120.82 | 124.61(54) | 120.88 | 122.58(66) | 120.88 | 122.00(57) |
| 121.01 | 127.44(67) | 120.95 | 124.94(60) | 120.98 | 125.84(73) | 120.96 | 125.48(67) | 121.01 | 123.98(68) | 121.01 | 122.40(62) |
| 131.42 | 142.84(54) | 131.35 | 140.82(52) | 131.38 | 141.49(60) | 131.36 | 141.27(56) | 131.42 | 139.15(58) | 131.41 | 138.67(53) |
| 131.42 | 142.72(56) | 131.35 | 140.95(53) | 131.39 | 141.79(60) | 131.36 | 141.30(56) | 131.42 | 139.65(61) | 131.42 | 138.58(53) |
| 131.54 | 143.03(68) | 131.49 | 141.57(66) | 131.53 | 141.97(72) | 131.50 | 141.71(71) | 131.55 | 139.53(68) | 131.54 | 138.86(65) |
| 142.89 | 160.03(58) | 142.82 | 158.22(56) | 142.86 | 159.20(62) | 142.83 | 158.72(59) | 142.88 | 157.21(65) | 142.88 | 156.52(57) |
| 142.89 | 160.18(56) | 142.82 | 157.96(55) | 142.87 | 158.84(61) | 142.83 | 158.84(59) | 142.89 | 157.30(68) | 142.88 | 156.56(58) |
| 143.00 | 161.54(72) | 142.96 | 158.44(67) | 143.00 | 159.45(77) | 142.96 | 159.23(74) | 143.00 | 158.55(78) | 142.99 | 158.57(68) |
| 155.32 | 178.08(61) | 155.28 | 175.47(56) | 155.34 | 176.76(58) | 155.29 | 176.78(57) | 155.33 | 176.25(63) | 155.32 | 175.79(58) |
| 155.33 | 177.78(58) | 155.28 | 175.75(55) | 155.34 | 176.87(60) | 155.29 | 177.00(58) | 155.33 | 176.26(59) | 155.32 | 175.92(57) |
| 155.44 | 178.21(74) | 155.40 | 178.28(62) | 155.46 | 179.42(72) | 155.41 | 179.07(67) | 155.44 | 176.39(79) | 155.44 | 175.89(69) |
| 168.88 | 197.02(57) | 168.83 | 195.84(54) | 168.89 | 196.75(64) | 168.83 | 197.19(58) | 168.86 | 195.78(70) | 168.84 | 195.76(61) |
| 168.88 | 197.32(62) | 168.83 | 195.98(54) | 168.89 | 197.06(65) | 168.83 | 197.09(63) | 168.86 | 195.49(67) | 168.85 | 195.80(60) |
| 168.99 | 197.80(73) | 168.95 | 196.39(70) | 169.00 | 196.92(78) | 168.94 | 196.94(71) | 168.97 | 195.76(78) | 168.95 | 196.00(75) |
| 183.65 | 217.68(58) | 183.61 | 215.90(57) | 183.64 | 215.75(62) | 183.62 | 216.30(61) | 183.65 | 216.45(67) | 183.64 | 216.22(56) |
| 183.66 | 217.86(58) | 183.62 | 215.80(57) | 183.64 | 216.13(63) | 183.62 | 215.63(61) | 183.66 | 216.14(63) | 183.64 | 216.33(55) |
| 183.74 | 218.36(78) | 183.73 | 216.13(70) | 183.73 | 216.20(78) | 183.72 | 216.41(74) | 183.74 | 216.17(84) | 183.74 | 216.53(71) |
| 199.63 | 236.90(61) | 199.61 | 236.16(57) | 199.64 | 235.96(64) | 199.62 | 235.79(60) | 199.63 | 235.79(69) | 199.62 | 236.22(57) |
| 199.63 | 236.80(61) | 199.61 | 235.50(55) | 199.64 | 235.39(66) | 199.63 | 235.84(63) | 199.63 | 235.93(65) | 199.62 | 236.27(57) |
| 199.69 | 237.23(70) | 199.68 | 235.74(65) | 199.71 | 235.75(74) | 199.71 | 236.46(69) | 199.70 | 235.69(86) | 199.68 | 236.39(72) |
| 217.00 | 256.36(66) | 217.00 | 255.11(60) | 217.03 | 255.09(71) | 217.02 | 255.64(65) | 217.00 | 256.33(76) | 216.98 | 257.12(66) |
| 217.00 | 256.44(66) | 217.00 | 255.09(55) | 217.03 | 255.13(71) | 217.02 | 255.28(66) | 217.00 | 256.75(76) | 216.99 | 256.46(67) |
| 217.01 | 256.78(85) | 217.04 | 255.37(74) | 217.08 | 255.66(91) | 217.05 | 255.84(85) | 217.01 | 256.68(90) | 217.01 | 257.38(81) |
| 235.86 | 273.44(86) | 235.90 | 272.03(65) | 235.93 | 272.25(83) | 235.92 | 272.21(69) | 235.86 | 274.00(89) | 235.87 | 275.16(81) |
| 235.89 | 273.55(74) | 235.90 | 272.17(78) | 235.94 | 272.09(67) | 235.92 | 272.42(66) | 235.89 | 274.26(74) | 235.87 | 274.79(64) |
| 235.89 | 273.02(70) | 235.91 | 271.91(61) | 235.95 | 272.22(67) | 235.93 | 272.50(84) | 235.90 | 274.35(77) | 235.87 | 275.01(68) |
| 256.34 | 291.52(79) | 256.37 | 290.97(68) | 256.42 | 291.12(77) | 256.43 | 291.41(75) | 256.35 | 292.96(85) | 256.33 | 294.40(74) |
| 256.42 | 291.50(71) | 256.43 | 291.09(62) | 256.48 | 291.30(74) | 256.47 | 291.57(66) | 256.42 | 293.43(78) | 256.40 | 294.47(63) |
| 256.43 | 291.45(71) | 256.45 | 291.25(60) | 256.50 | 291.21(71) | 256.48 | 291.76(69) | 256.44 | 292.86(72) | 256.41 | 294.28(65) |
| 278.59 | 311.42(126) | 278.60 | 312.33(102) | 278.64 | 311.55(111) | 278.66 | 311.94(88) | 278.57 | 313.33(114) | 278.56 | 314.90(116) |
| 278.71 | 311.18(82) | 278.72 | 312.11(75) | 278.78 | 311.69(86) | 278.77 | 312.35(83) | 278.71 | 313.43(88) | 278.69 | 314.76(83) |
| 278.72 | 310.91(86) | 278.75 | 312.42(104) | 278.80 | 311.80(81) | 278.78 | 312.42(83) | 278.73 | 313.21(88) | 278.70 | 314.72(86) |
| 302.80 | 328.57(102) | 302.79 | 328.68(91) | 302.85 | 329.65(97) | 302.79 | 328.97(97) | 302.79 | 331.51(99) | 302.77 | 332.10(95) |
| 302.96 | 328.76(86) | 302.99 | 328.83(77) | 303.05 | 329.29(82) | 303.03 | 329.66(84) | 302.97 | 331.28(91) | 302.93 | 333.03(79) |
| 302.98 | 328.89(86) | 303.00 | 328.88(78) | 303.06 | 329.23(85) | 303.05 | 329.84(83) | 302.99 | 331.50(84) | 302.95 | 332.59(82) |

APPENDIX. Continued

| Py10Gr90 #2 Source: Geiger |  | Gr #1 Source: HW80 |  | Gr #2 Source: HW80 |  |
| --- | --- | --- | --- | --- | --- |
| FW | 445.722 | FW | 450.452 | FW | 450.452 |
| SW | 25.012 | SW | 25.809 | SW | 25.809 |
| XGr | 0.904 | XGr | 1.000 | XGr | 1.000 |
| T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] | T [K] | Cp [J/(mol.K)] |
| 5.119 | 0.026(1) | 5.140 | 0.016(1) | 5.052 | 0.009(1) |
| 5.122 | 0.025(1) | 5.142 | 0.015(1) | 5.068 | 0.009(1) |
| 5.125 | 0.027(1) | 5.148 | 0.018(1) | 5.068 | 0.010(1) |
| 5.580 | 0.031(1) | 5.593 | 0.015(1) | 5.488 | 0.010(1) |
| 5.586 | 0.037(1) | 5.600 | 0.020(1) | 5.495 | 0.012(1) |
| 5.591 | 0.034(1) | 5.604 | 0.015(1) | 5.500 | 0.010(1) |
| 6.062 | 0.047(2) | 6.075 | 0.017(2) | 5.965 | 0.014(2) |
| 6.068 | 0.045(1) | 6.080 | 0.022(1) | 5.980 | 0.015(3) |
| 6.073 | 0.047(1) | 6.085 | 0.019(1) | 5.981 | 0.014(1) |
| 6.586 | 0.069(1) | 6.587 | 0.031(2) | 6.488 | 0.024(1) |
| 6.592 | 0.069(1) | 6.598 | 0.031(2) | 6.494 | 0.023(1) |
| 6.599 | 0.069(1) | 6.608 | 0.028(1) | 6.500 | 0.022(2) |
| 7.174 | 0.094(1) | 7.165 | 0.040(3) | 7.066 | 0.036(2) |
| 7.175 | 0.090(1) | 7.169 | 0.045(4) | 7.070 | 0.036(1) |
| 7.175 | 0.096(1) | 7.187 | 0.046(2) | 7.081 | 0.030(3) |
| 7.736 | 0.117(2) | 7.745 | 0.049(2) | 7.662 | 0.042(2) |
| 7.740 | 0.118(2) | 7.753 | 0.050(1) | 7.667 | 0.042(1) |
| 7.744 | 0.118(2) | 7.757 | 0.049(1) | 7.674 | 0.042(1) |
| 8.404 | 0.152(2) | 8.413 | 0.062(2) | 8.329 | 0.053(2) |
| 8.407 | 0.151(2) | 8.419 | 0.059(2) | 8.334 | 0.052(2) |
| 8.413 | 0.152(2) | 8.423 | 0.061(2) | 8.341 | 0.053(2) |
| 9.131 | 0.200(3) | 9.142 | 0.080(2) | 9.053 | 0.073(2) |
| 9.135 | 0.200(3) | 9.146 | 0.078(3) | 9.059 | 0.072(2) |
| 9.142 | 0.199(2) | 9.149 | 0.082(2) | 9.065 | 0.073(2) |
| 9.923 | 0.259(4) | 9.935 | 0.103(4) | 9.840 | 0.096(3) |
| 9.927 | 0.255(3) | 9.937 | 0.103(3) | 9.846 | 0.096(3) |
| 9.933 | 0.257(3) | 9.941 | 0.106(2) | 9.853 | 0.096(2) |
| 10.793 | 0.321(5) | 10.800 | 0.128(4) | 10.698 | 0.121(4) |
| 10.796 | 0.318(4) | 10.801 | 0.130(3) | 10.704 | 0.120(3) |
| 10.801 | 0.320(3) | 10.808 | 0.129(3) | 10.709 | 0.119(3) |
| 11.722 | 0.403(6) | 11.741 | 0.167(4) | 11.627 | 0.154(5) |
| 11.726 | 0.399(5) | 11.741 | 0.167(4) | 11.637 | 0.151(4) |
| 11.732 | 0.400(4) | 11.744 | 0.166(3) | 11.644 | 0.150(3) |
| 12.744 | 0.501(7) | 12.752 | 0.219(6) | 12.651 | 0.207(6) |
| 12.744 | 0.498(6) | 12.753 | 0.216(4) | 12.653 | 0.203(5) |
| 12.750 | 0.501(5) | 12.758 | 0.217(4) | 12.658 | 0.203(4) |
| 13.847 | 0.625(9) | 13.859 | 0.280(6) | 13.752 | 0.276(6) |
| 13.848 | 0.619(7) | 13.860 | 0.285(8) | 13.752 | 0.278(8) |
| 13.853 | 0.621(7) | 13.862 | 0.287(5) | 13.756 | 0.275(5) |
| 15.052 | 0.755(9) | 15.064 | 0.368(8) | 14.948 | 0.354(8) |
| 15.054 | 0.758(8) | 15.066 | 0.371(7) | 14.950 | 0.359(10) |
| 15.056 | 0.766(12) | 15.068 | 0.375(10) | 14.952 | 0.353(7) |
| 16.359 | 0.918(11) | 16.371 | 0.477(9) | 16.249 | 0.463(10) |
| 16.360 | 0.926(10) | 16.373 | 0.475(9) | 16.252 | 0.462(9) |
| 16.367 | 0.926(14) | 16.381 | 0.493(14) | 16.254 | 0.472(13) |
| 17.779 | 1.121(14) | 17.792 | 0.624(12) | 17.663 | 0.617(13) |
| 17.781 | 1.108(14) | 17.795 | 0.618(12) | 17.665 | 0.617(12) |
| 17.794 | 1.122(18) | 17.811 | 0.642(16) | 17.667 | 0.627(17) |
| 19.315 | 1.351(17) | 19.324 | 0.815(16) | 19.196 | 0.792(15) |
| 19.317 | 1.346(17) | 19.326 | 0.805(16) | 19.196 | 0.793(15) |
| 19.339 | 1.357(20) | 19.353 | 0.823(19) | 19.212 | 0.805(23) |
| 20.99 | 1.62(2) | 21.00 | 1.05(2) | 20.86 | 1.03(2) |
| 20.99 | 1.62(2) | 21.01 | 1.05(2) | 20.87 | 1.03(2) |
| 21.02 | 1.62(3) | 21.04 | 1.05(3) | 20.89 | 1.05(3) |
| 22.81 | 1.96(3) | 22.82 | 1.37(3) | 22.67 | 1.33(3) |
| 22.81 | 1.95(3) | 22.82 | 1.36(3) | 22.68 | 1.33(3) |
| 22.84 | 1.99(4) | 22.86 | 1.39(4) | 22.69 | 1.35(4) |
| 24.78 | 2.48(7) | 24.79 | 1.82(4) | 24.66 | 1.78(6) |
| 24.78 | 2.44(4) | 24.80 | 1.80(6) | 24.66 | 1.69(8) |
| 24.82 | 2.47(5) | 24.84 | 1.87(5) | 24.68 | 1.81(5) |
| 26.94 | 3.01(5) | 26.95 | 2.41(5) | 26.80 | 2.35(5) |
| 26.94 | 3.02(6) | 26.95 | 2.41(5) | 26.81 | 2.35(5) |
| 26.98 | 3.01(7) | 26.99 | 2.41(6) | 26.85 | 2.43(7) |
| 29.27 | 3.69(7) | 29.28 | 3.11(7) | 29.14 | 3.10(6) |
| 29.27 | 3.70(7) | 29.28 | 3.11(7) | 29.14 | 3.10(7) |
| 29.32 | 3.80(8) | 29.33 | 3.20(8) | 29.19 | 3.15(7) |
| 31.81 | 4.61(9) | 31.82 | 4.10(9) | 31.68 | 4.04(8) |
| 31.81 | 4.61(9) | 31.82 | 4.08(9) | 31.69 | 4.03(9) |
| 31.86 | 4.68(11) | 31.88 | 4.20(10) | 31.74 | 4.13(9) |
| 34.57 | 5.94(11) | 34.58 | 5.51(11) | 34.46 | 5.45(11) |
| 34.57 | 5.93(11) | 34.58 | 5.51(11) | 34.46 | 5.43(11) |
| 34.63 | 6.05(12) | 34.64 | 5.62(12) | 34.52 | 5.52(12) |
| 37.58 | 7.63(14) | 37.59 | 7.31(14) | 37.47 | 7.17(14) |
| 37.58 | 7.65(14) | 37.59 | 7.29(14) | 37.48 | 7.18(14) |
| 37.64 | 7.75(15) | 37.65 | 7.42(15) | 37.54 | 7.32(15) |
| 40.84 | 9.75(18) | 40.85 | 9.59(17) | 40.75 | 9.41(18) |
| 40.84 | 9.82(17) | 40.85 | 9.59(18) | 40.76 | 9.42(18) |
| 40.90 | 9.92(19) | 40.91 | 9.73(19) | 40.83 | 9.55(19) |
| 44.39 | 12.31(21) | 44.40 | 12.24(21) | 44.31 | 12.35(21) |
| 44.39 | 12.28(21) | 44.40 | 12.22(21) | 44.31 | 12.36(22) |
| 44.46 | 12.47(22) | 44.46 | 12.44(22) | 44.40 | 12.57(24) |
| 48.25 | 15.63(24) | 48.26 | 15.52(25) | 48.18 | 15.91(25) |
| 48.25 | 15.66(25) | 48.26 | 15.65(25) | 48.18 | 15.91(26) |
| 48.32 | 15.80(26) | 48.33 | 15.85(27) | 48.27 | 16.14(27) |
| 52.45 | 19.32(29) | 52.46 | 19.48(29) | 52.38 | 19.89(30) |
| 52.45 | 19.37(28) | 52.46 | 19.51(30) | 52.38 | 19.89(28) |
| 52.53 | 19.51(30) | 52.53 | 19.74(31) | 52.47 | 20.17(33) |
| 57.02 | 24.26(33) | 57.03 | 24.51(34) | 56.95 | 25.01(32) |
| 57.02 | 24.22(33) | 57.03 | 24.56(33) | 56.95 | 25.08(34) |
| 57.10 | 24.41(34) | 57.10 | 24.71(35) | 57.04 | 25.35(37) |
| 61.99 | 30.11(36) | 62.00 | 30.56(38) | 61.91 | 30.97(38) |
| 61.99 | 30.11(34) | 62.00 | 30.51(35) | 61.91 | 30.93(35) |
| 62.08 | 30.05(39) | 62.09 | 30.58(40) | 62.02 | 31.27(39) |
| 67.39 | 37.15(39) | 67.40 | 37.54(38) | 67.31 | 38.08(39) |
| 67.39 | 37.13(40) | 67.40 | 37.56(39) | 67.31 | 38.09(40) |
| 67.49 | 37.67(44) | 67.50 | 37.85(45) | 67.42 | 38.54(45) |
| 73.25 | 44.83(41) | 73.27 | 45.31(43) | 73.18 | 46.36(46) |
| 73.26 | 44.80(40) | 73.27 | 45.77(44) | 73.18 | 46.28(45) |
| 73.35 | 45.61(44) | 73.37 | 46.25(47) | 73.30 | 46.78(49) |
| 79.63 | 55.14(47) | 79.63 | 55.59(48) | 79.56 | 55.37(46) |
| 79.63 | 54.59(50) | 79.64 | 55.64(45) | 79.57 | 55.80(47) |
| 79.74 | 55.17(49) | 79.74 | 56.19(52) | 79.69 | 56.08(53) |
| 86.55 | 65.31(49) | 86.56 | 66.64(53) | 86.50 | 66.21(47) |
| 86.55 | 65.46(48) | 86.56 | 66.37(49) | 86.50 | 66.14(49) |
| 86.66 | 66.04(54) | 86.67 | 66.56(55) | 86.62 | 66.59(55) |
| 94.08 | 76.99(48) | 94.09 | 77.73(53) | 94.03 | 77.97(50) |
| 94.08 | 76.75(46) | 94.09 | 77.66(52) | 94.04 | 77.89(51) |
| 94.20 | 77.20(52) | 94.20 | 78.05(59) | 94.16 | 78.55(59) |
| 102.28 | 90.26(49) | 102.28 | 91.29(55) | 102.23 | 91.81(51) |
| 102.28 | 90.67(47) | 102.29 | 91.31(53) | 102.23 | 91.64(52) |
| 102.40 | 91.08(57) | 102.40 | 91.77(61) | 102.37 | 92.05(61) |
| 111.19 | 105.14(54) | 111.20 | 105.88(58) | 111.14 | 106.19(58) |
| 111.20 | 105.19(52) | 111.20 | 105.70(58) | 111.15 | 106.28(65) |
| 111.32 | 105.77(58) | 111.32 | 106.26(63) | 111.27 | 106.59(65) |
| 120.88 | 122.20(54) | 120.89 | 122.47(61) | 120.83 | 122.30(59) |
| 120.88 | 121.78(55) | 120.89 | 122.45(63) | 120.83 | 122.41(59) |
| 121.01 | 122.29(66) | 121.03 | 122.78(68) | 120.98 | 123.11(66) |
| 131.42 | 138.30(54) | 131.43 | 138.21(59) | 131.37 | 139.45(61) |
| 131.42 | 138.15(53) | 131.43 | 138.49(62) | 131.37 | 139.31(59) |
| 131.55 | 138.63(63) | 131.57 | 138.69(66) | 131.51 | 139.87(71) |
| 142.88 | 156.41(54) | 142.90 | 156.62(61) | 142.84 | 156.92(65) |
| 142.89 | 156.74(56) | 142.90 | 156.87(65) | 142.84 | 156.83(64) |
| 143.00 | 157.82(61) | 143.01 | 158.33(73) | 142.97 | 157.15(72) |
| 155.31 | 175.05(56) | 155.34 | 175.45(68) | 155.30 | 175.10(63) |
| 155.31 | 175.32(56) | 155.34 | 175.25(70) | 155.30 | 175.08(63) |
| 155.43 | 175.84(67) | 155.46 | 175.55(75) | 155.42 | 177.43(73) |
| 168.93 | 195.40(57) | 168.87 | 194.29(67) | 168.85 | 195.00(71) |
| 168.93 | 195.60(57) | 168.87 | 195.02(67) | 168.85 | 194.73(71) |
| 169.03 | 195.91(74) | 168.98 | 195.35(79) | 168.96 | 195.09(76) |
| 183.64 | 215.70(58) | 183.66 | 214.72(71) | 183.63 | 216.66(71) |
| 183.64 | 215.79(57) | 183.66 | 214.72(73) | 183.63 | 216.30(68) |
| 183.73 | 216.19(73) | 183.75 | 214.58(84) | 183.73 | 216.77(81) |
| 199.61 | 236.06(60) | 199.63 | 234.38(74) | 199.62 | 236.74(70) |
| 199.62 | 235.82(62) | 199.64 | 234.32(74) | 199.63 | 236.88(67) |
| 199.68 | 236.25(70) | 199.71 | 234.13(83) | 199.70 | 237.00(81) |
| 216.98 | 257.25(63) | 217.01 | 254.79(79) | 217.01 | 256.86(80) |
| 216.99 | 256.66(62) | 217.01 | 254.73(81) | 217.01 | 256.89(80) |
| 217.02 | 256.86(82) | 217.03 | 254.52(92) | 217.05 | 256.64(92) |
| 235.84 | 274.47(78) | 235.88 | 271.90(96) | 235.91 | 273.78(91) |
| 235.87 | 274.56(70) | 235.90 | 272.22(83) | 235.91 | 273.91(79) |
| 235.88 | 274.29(68) | 235.90 | 272.19(82) | 235.92 | 273.77(80) |
| 256.33 | 293.56(81) | 256.37 | 290.06(94) | 256.38 | 292.45(87) |
| 256.40 | 293.69(65) | 256.43 | 290.67(84) | 256.44 | 292.76(80) |
| 256.41 | 293.77(65) | 256.45 | 291.12(79) | 256.46 | 292.84(78) |
| 278.56 | 314.08(121) | 278.59 | 310.37(125) | 278.60 | 312.99(123) |
| 278.69 | 313.80(81) | 278.72 | 310.22(98) | 278.73 | 313.48(100) |
| 278.70 | 313.75(79) | 278.75 | 310.25(94) | 278.75 | 313.45(97) |
| 302.78 | 331.69(90) | 302.83 | 329.14(103) | 302.80 | 330.01(107) |
| 302.93 | 331.71(86) | 302.98 | 329.53(94) | 302.99 | 329.98(95) |
| 302.94 | 332.26(84) | 303.00 | 329.59(89) | 303.00 | 330.20(99) |