Table 5b: Refined isotropic displacement parameters of zoisite [100*Uiso]

| sample | Au32 | Au40 | Au45 | # Pt4 | Au31 | Au34 | # Au30 | Au42 | # Pt3 | Pt36 | # Pt2 | Au23 | Au22 | # Au33 | Au44 | # Au21 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A1 | 0.43(68) | 0.86(27) | 0.34(64) | 1.16(16) | 0.22(72) | -0.03(51) | 0.36(32) | 0.25(80) | 0.94(16) | 0.92(15) | 0.13(14) | 0.58(16) | 0.06(20) | 1.27(21) | -0.17(12) | 0.86(4) |
| A2 | 0.35(68) | 1.00(24) | 0.63(48) | 1.46(12) | 0.63(52) | 0.71(39) | 0.98(22) | 0.80(96) | 0.94(10) | 1.04(8) | 0.18(10) | 0.55(12) | 0.14(17) | 2.54(21) | -0.02(12) | 1.31(5) |
| M1 | -0.39(76) | -0.34(15) | -0.35(40) | 0.79(11) | -0.43(44) | 0.37(39) | 0.16(22) | -0.61(52) | 0.65(13) | 0.51(12) | 0.46(16) | 0.35(17) | -0.02(24) | 1.00(30) | -0.05(16) | 0.54(8) |
| M2 | 0.32(76) | 0.28(28) | 0.90(80) | 1.08(20) | 1.18(98) | 0.46(63) | 0.38(40) | -0.74(88) | 0.97(22) | 1.28(23) | 0.52(26) | 0.63(29) | 0.62(44) | 1.09(39) | 0.29(27) | 0.55(13) |
| T1 | -0.07(68) | 0.12(28) | 1.00(80) | 0.47(17) | 0.37(88) | 0.03(57) | 0.14(38) | -0.97(80) | 0.38(18) | 0.79(20) | -0.13(22) | -0.22(24) | -0.04(37) | 0.65(45) | 0.30(26) | 0.67(12) |
| T2 | 0.83(76) | -0.31(26) | -0.18(60) | 0.74(17) | -0.51(72) | -0.03(54) | 0.76(38) | -0.21(88) | 0.82(20) | 0.67(19) | 0.38(24) | 0.34(25) | -0.50(34) | 1.17(45) | -0.06(22) | 0.51(11) |
| T3 | -0.75(64) | -0.17(26) | -0.14(64) | 0.58(17) | -0.80(68) | -0.07(54) | 0.91(40) | -0.19(98) | 0.62(20) | 0.41(20) | 0.36(24) | 0.02(26) | 0.36(42) | 0.46(45) | -0.27(24) | 0.39(11) |
| O1 | -0.36(96) | -0.17(40) | -0.53(92) | 0.91(25) | -0.97(100) | -0.44(75) | -0.05(52) | -1.76(108) | 0.71(30) | 0.68(28) | -0.09(32) | -0.44(32) | -0.76(48) | 1.36(63) | 0.18(36) | 1.44(19) |
| O2 | 0.20(88) | 0.40(40) | 0.20(88) | 1.12(25) | 0.58(112) | 0.57(75) | 0.47(51) | 2.03(148) | 0.94(28) | 1.02(27) | -0.15(30) | 0.82(35) | -0.59(46) | 1.70(62) | 0.18(32) | 0.92(16) |
| O3 | -0.50(92) | 0.30(44) | -0.19(24) | 1.11(28) | -1.15(112) | -0.24(87) | 0.23(60) | -0.79(128) | 1.21(35) | 0.96(34) | 0.88(40) | 0.80(42) | -0.84(52) | 0.40(63) | -0.01(36) | 0.96(19) |
| O4 | -0.59(144) | -0.44(60) | -0.22(144) | 1.04(40) | -0.30(160) | 0.08(115) | 1.04(84) | -0.51(180) | 0.48(40) | 1.96(47) | -0.04(47) | 1.71(63) | -0.45(74) | 0.54(84) | 0.65(52) | 0.18(24) |
| O5 | -0.94(120) | 0.71(60) | -0.16(120) | 1.14(32) | -1.00(128) | 0.35(105) | 0.73(74) | -1.04(160) | 0.97(40) | 0.66(40) | 0.11(47) | 1.94(59) | 0.59(76) | 1.13(84) | 0.27(48) | 0.52(25) |
| O6 | 0.19(144) | 0.91(56) | 1.03(132) | 1.39(35) | -0.40(132) | 0.96(111) | -0.03(66) | -0.97(159) | 0.70(37) | 1.14(40) | 0.23(42) | 1.82(51) | -0.10(62) | 0.44(72) | 0.19(42) | 0.42(21) |
| O7 | 0.68(164) | 0.06(64) | -0.23(144) | 1.15(40) | -0.37(168) | 0.59(129) | -0.09(80) | -2.52(152) | 2.36(54) | 0.92(46) | 0.51(55) | -0.64(49) | 0.67(88) | 1.57(101) | 1.27(61) | 1.07(28) |
| O8 | 1.20(176) | 0.66(66) | 2.2(16) | 1.12(40) | 2.28(212) | 1.35(129) | 0.91(84) | -0.74(180) | 1.16(45) | 1.92(48) | 1.33(58) | 1.62(65) | 0.12(84) | 1.02(96) | 1.44(60) | 0.56(27) |
| O9 | 0.14(150) | 1.01(62) | 0.27(140) | 2.6(4) | 0.25(168) | 0.67(120) | 1.03(84) | -2.5(13) | 2.29(50) | 2.84(51) | 1.54(56) | 2.89(69) | 1.03(84) | 2.15(98) | 1.37(56) | 0.57(25) |
| O10 | -0.59(124) | -0.26(54) | 0.02(128) | 0.97(34) | 0.37(148) | 0.48(115) | 2.5(8) | 0.56(178) | 2.08(45) | 0.65(39) | -0.26(44) | -0.57(45) | -0.99(66) | 0.19(75) | 0.23(47) | 0.15(22) |

Note: In general, isotropic displacement parameters obtained from Powder-XRD-data are afflicted with errors, especially when more than one phase is present in the powder-pattern. The values given in this table were obtained from the Rietveld-analysis with structure-refinement. Negative values are physically implausible; these values are caused by peak-overlap with other phases and are influenced strongly by peak shape parameters in the structure refinement.

Table 6b: Refined isotropic displacement parameters of clinozoisite [100*Uiso]

| sample | Au32 | Au45 | Au31 | Au35 | Au34 | Pt8 | Au42 | Pt35 | Au43 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A1 | 1.49(88) | 1.05(40) | -0.06(51) | 0.18(40) | -0.21(54) | 1.77(37) | 0.36(38) | -0.05(22) | 0.03(19) |
| A2 | 1.28(84) | 1.19(40) | 1.07(40) | -0.30(26) | -0.10(35) | 0.53(16) | -0.12(20) | 0.24(12) | 0.32(11) |
| M1 | 0.46(72) | 0.13(42) | -1.58(40) | -0.45(38) | 0.45(56) | 0.77(28) | 0.17(40) | -1.05(20) | 0.23(22) |
| M2 | 0.97(84) | 2.24(60) | 1.74(64) | 1.09(48) | 0.96(61) | 1.57(32) | 0.34(41) | 1.21(30) | 1.62(28) |
| M3 | 1.56(100) | 0.63(54) | -1.88(43) | -0.10(44) | 0.50(64) | 2.34(38) | -0.15(40) | 0.14(50) | 0.99(52) |
| T1 | 0.58(84) | -0.13(45) | -0.95(48) | -0.13(42) | -0.29(54) | 0.59(27) | -0.02(38) | -0.26(44) | 0.38(23) |
| T2 | 0.30(80) | -0.36(40) | -0.94(46) | -0.48(38) | -0.69(50) | 0.33(26) | -0.52(34) | -1.30(40) | -0.41(29) |
| T3 | 0.61(88) | 0.76(54) | 2.39(73) | 0.24(44) | 0.70(61) | 0.55(29) | 0.01(39) | -1.06(44) | 0.63(25) |
| O1 | 2.62(136) | 1.49(74) | 2.32(94) | 0.46(60) | 0.52(78) | 1.09(42) | 0.29(56) | -0.67(64) | 1.42(33) |
| O2 | -0.92(96) | -0.65(64) | -2.85(56) | -1.36(54) | -1.36(70) | -0.04(40) | -0.04(58) | -0.94(60) | -0.15(30) |
| O3 | 0.54(112) | -0.62(60) | -0.37(70) | 0.51(64) | 0.66(86) | 1.10(42) | 0.19(58) | -0.40(62) | 1.38(38) |
| O4 | 0.22(160) | -0.21(90) | 2.33(152) | 0.07(86) | 0.37(116) | 0.54(55) | -0.20(80) | -1.54(82) | -1.76(37) |
| O5 | 0.94(160) | 2.6(12) | -0.18(106) | 1.4(11) | -1.20(101) | 2.30(72) | 0.57(90) | 2.5(12) | 0.36(48) |
| O6 | 13(4) | 10(2) | 25(5) | 7(2) | 5(2) | 2.39(85) | -1.9(7) | 1.6(8) | 0.68(52) |
| O7 | 2(2) | 2.6(13) | 4(2) | 2(1) | 2.2(14) | 1.25(64) | 1.26(92) | 3.3(14) | 2.17(55) |
| O8 | 0.97(42) | 0.36(94) | -0.26(110) | 2(1) | 4.4(16) | 2.05(68) | 2.4(10) | 1.2(12) | 3.9(7) |
| O9 | 6(2) | 5.9(16) | 8.5(22) | 4.5(14) | 4.6(18) | 3.46(82) | 2.9(11) | 1.1(12) | 2.9(6) |
| O10 | 5(3) | 10(2) | 7.3(22) | 3.4(12) | 4.8(18) | 2.31(74) | 0.4(8) | 0.64(121) | 0.68(5) |

Note: In general, isotropic displacement parameters obtained from Powder-XRD-data are afflicted with errors, especially when more than one phase is present in the powder-pattern. The values given in this table were obtained from the Rietveld-analysis with structure-refinement. Negative values are physically implausible; these negative values are caused by peak-overlap with other phases and are influenced strongly by peak shape parameters in the structure refinement.

Table A1: Interatomic distances in zoisite [Å]

| Run no. |  | Au32 | Au40 | Au45 | Pt4 | Au31 | Au34 | Au30 | Pt3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| XSrzo |  | 0.06 | 0.13 | 0.16 | 0.22 | 0.25 | 0.24 | 0.32 | 0.42 |
| Distances A1 |  |  |  |  |  |  |  |  |  |
| -O1 | x 2 | 2.526(8) | 2.541(7) | 2.548(8) | 2.528(5) | 2.542(8) | 2.551(4) | 2.541(1) | 2.539(5) |
| -O3 | x 2 | 2.443(9) | 2.432(8) | 2.455(9) | 2.440(5) | 2.451(9) | 2.417(3) | 2.461(1) | 2.441(6) |
| -O5 |  | 2.570(12) | 2.547(12) | 2.552(12) | 2.577(7) | 2.518(13) | 2.552(4) | 2.588(1) | 2.595(7) |
| -O6 |  | 2.595(12) | 2.581(10) | 2.607(12) | 2.562(6) | 2.611(12) | 2.610(4) | 2.585(1) | 2.564(6) |
| -O7 |  | 2.314(14) | 2.258(11) | 2.305(13) | 2.270(7) | 2.299(14) | 2.296(3) | 2.299(1) | 2.273(8) |
|  | Mean (7) | 2.49 | 2.48 | 2.50 | 2.48 | 2.49 | 2.49 | 2.50 | 2.48 |
| -O9 | x2 | 2.917(4) | 2.912(3) | 2.912(4) | 2.903(2) | 2.912(4) | 2.908(4) | 2.912(1) | 2.898(2) |
| Distances A2 |  |  |  |  |  |  |  |  |  |
| -O2 | x2 | 2.548(9) | 2.543(7) | 2.574(8) | 2.584(5) | 2.605(10) | 2.620(3) | 2.631(1) | 2.620(5) |
| -O2 | x2 | 2.810(7) | 2.787(6) | 2.779(7) | 2.763(4) | 2.782(9) | 2.766(4) | 2.763(2) | 2.745(4) |
| -O3 | x2 | 2.492(8) | 2.472(7) | 2.494(8) | 2.519(5) | 2.490(9) | 2.469(2) | 2.484(1) | 2.551(5) |
| -O7 |  | 2.357(13) | 2.357(10) | 2.329(12) | 2.384(7) | 2.372(13) | 2.383(4) | 2.367(2) | 2.470(8) |
|  | Mean (7) | 2.58 | 2.57 | 2.57 | 2.59 | 2.59 | 2.59 | 2.59 | 2.61 |
| -O8 | x2 | 3.047(7) | 3.032(5) | 3.049(7) | 3.022(3) | 3.041(7) | 3.041(4) | 3.046(2) | 3.028(3) |
| -O10 |  | 3.054(12) | 3.042(10) | 3.057(12) | 3.066(6) | 3.128(14) | 3.086(5) | 3.079(2) | 3.110(7) |
| Distances M1,2 |  |  |  |  |  |  |  |  |  |
| Al1-O1 |  | 1.965(7) | 1.991(6) | 1.972(7) | 2.000(4) | 1.973(8) | 1.969(3) | 1.996(1) | 1.990(5) |
| Al1-O3 |  | 1.885(7) | 1.874(7) | 1.885(8) | 1.874(4) | 1.884(8) | 1.908(3) | 1.882(1) | 1.867(5) |
| Al1-O4 |  | 1.822(7) | 1.820(7) | 1.836(8) | 1.817(5) | 1.867(9) | 1.816(2) | 1.796(1) | 1.824(5) |
| Al1-O5 |  | 1.947(8) | 1.924(7) | 1.957(9) | 1.927(5) | 1.976(9) | 1.954(2) | 1.946(1) | 1.924(5) |
| Al1-O6 |  | 1.898(8) | 1.931(8) | 1.879(9) | 1.928(5) | 1.854(9) | 1.875(2) | 1.891(1) | 1.953(6) |
| Al1-O10 |  | 1.812(7) | 1.814(6) | 1.797(8) | 1.825(4) | 1.786(9) | 1.814(2) | 1.806(1) | 1.835(5) |
|  | Mean (6) | 1.89 | 1.89 | 1.89 | 1.90 | 1.89 | 1.89 | 1.89 | 1.90 |
| Distances M3 |  |  |  |  |  |  |  |  |  |
| Al2-O1 | x2 | 2.070(9) | 2.067(8) | 2.070(9) | 2.112(5) | 2.093(10) | 2.089(2) | 2.091(1) | 2.097(6) |
| Al2-O2 | x2 | 1.962(9) | 1.963(7) | 1.970(8) | 1.953(5) | 1.989(10) | 1.987(2) | 1.989(1) | 1.974(6) |
| Al2-O4 |  | 1.825(13) | 1.815(12) | 1.824(13) | 1.825(7) | 1.893(16) | 1.884(3) | 1.860(1) | 1.837(7) |
| Al2-O8 |  | 1.638(15) | 1.743(12) | 1.659(16) | 1.749(7) | 1.669(18) | 1.718(3) | 1.737(1) | 1.771(8) |
|  | Mean (6) | 1.92 | 1.94 | 1.93 | 1.95 | 1.95 | 1.96 | 1.96 | 1.96 |
| Distances T1 |  |  |  |  |  |  |  |  |  |
| Si1-O1 | x2 | 1.654(8) | 1.637(7) | 1.645(8) | 1.634(4) | 1.641(9) | 1.653(2) | 1.639(1) | 1.643(4) |
| Si1-O7 |  | 1.561(12) | 1.594(10) | 1.577(12) | 1.555(6) | 1.575(13) | 1.544(2) | 1.551(1) | 1.526(7) |
| Si1-O9 |  | 1.644(13) | 1.584(11) | 1.552(13) | 1.613(8) | 1.537(15) | 1.610(3) | 1.566(1) | 1.651(9) |
|  | Mean (4) | 1.63 | 1.61 | 1.60 | 1.61 | 1.60 | 1.62 | 1.60 | 1.62 |
| ## Distances T2 |  |  |  |  |  |  |  |  |  |
| Si2-O3 | x2 | 1.602(9) | 1.613(7) | 1.599(9) | 1.592(4) | 1.635(9) | 1.608(2) | 1.600(1) | 1.594(5) |
| Si2-O8 |  | 1.679(14) | 1.618(12) | 1.638(15) | 1.611(7) | 1.641(17) | 1.626(2) | 1.604(1) | 1.611(8) |
| Si2-O9 |  | 1.584(12) | 1.660(11) | 1.698(13) | 1.638(8) | 1.675(15) | 1.654(3) | 1.691(1) | 1.615(8) |
|  | Mean (4) | 1.62 | 1.63 | 1.63 | 1.61 | 1.65 | 1.62 | 1.62 | 1.60 |
| Distances T3 |  |  |  |  |  |  |  |  |  |
| Si3-O2 | x2 | 1.577(8) | 1.604(7) | 1.591(8) | 1.604(4) | 1.544(10) | 1.562(2) | 1.555(1) | 1.604(4) |
| Si3-O5 |  | 1.589(12) | 1.632(11) | 1.597(13) | 1.619(7) | 1.624(14) | 1.638(2) | 1.618(1) | 1.613(8) |
| Si3-O6 |  | 1.735(13) | 1.682(11) | 1.725(14) | 1.679(7) | 1.773(14) | 1.721(2) | 1.744(1) | 1.668(7) |
|  | Mean (4) | 1.62 | 1.63 | 1.63 | 1.63 | 1.62 | 1.62 | 1.62 | 1.62 |

(Continued)

(Table A1, continued)

| Run no. |  | Au42 | Pt36 | Pt2 | Au23 | Au22 | Au33 | Au44 | Au21 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| XSrzo |  | 0.37 | 0.52 | 0.63 | 0.66 | 0.77 | 0.86 | 0.87 | 1 |
| Distances A1 |  |  |  |  |  |  |  |  |  |
| -O1 | x 2 | 2.541(10) | 2.536(4) | 2.530(6) | 2.567(11) | 2.565(8) | 2.551(6) | 2.558(5) | 2.562(6) |
| -O3 | x 2 | 2.453(12) | 2.475(5) | 2.478(6) | 2.487(13) | 2.518(8) | 2.528(6) | 2.529(6) | 2.562(6) |
| -O5 |  | 2.578(15) | 2.545(6) | 2.594(8) | 2.605(19) | 2.622(13) | 2.579(9) | 2.621(8) | 2.617(8) |
| -O6 |  | 2.618(15) | 2.562(6) | 2.577(8) | 2.611(17) | 2.563(11) | 2.637(8) | 2.624(8) | 2.651(8) |
| -O7 |  | 2.233(15) | 2.253(7) | 2.312(8) | 2.271(18) | 2.300(15) | 2.334(10) | 2.314(10) | 2.416(9) |
|  | Mean (7) | 2.49 | 2.48 | 2.50 | 2.51 | 2.52 | 2.53 | 2.53 | 2.56 |
| -O9 | x2 | 2.899(4) | 2.905(2) | 2.895(2) | 2.898(5) | 2.895(3) | 2.902(2) | 2.902(2) | 2.900(2) |
| Distances A2 |  |  |  |  |  |  |  |  |  |
| -O2 | x2 | 2.657(13) | 2.649(4) | 2.650(6) | 2.698(13) | 2.670(8) | 2.682(6) | 2.668(6) | 2.690(6) |
| -O2 | x2 | 2.753(12) | 2.765(4) | 2.771(5) | 2.782(12) | 2.794(8) | 2.784(6) | 2.796(5) | 2.790(6) |
| -O3 | x2 | 2.482(12) | 2.533(5) | 2.539(6) | 2.561(13) | 2.561(8) | 2.550(6) | 2.535(6) | 2.539(6) |
| -O7 |  | 2.451(13) | 2.458(6) | 2.446(8) | 2.440(16) | 2.477(13) | 2.494(9) | 2.477(8) | 2.474(9) |
|  | Mean (7) | 2.61 | 2.62 | 2.62 | 2.65 | 2.65 | 2.65 | 2.64 | 2.65 |
| -O8 | x2 | 3.044(7) | 3.0539(29) | 3.065(4) | 3.073(8) | 3.084(6) | 3.085(4) | 3.099(4) | 3.105(4) |
| -O10 |  | 3.113(16) | 3.060(6) | 3.067(7) | 3.062(16) | 3.012(11) | 3.012(8) | 3.038(8) | 3.005(7) |
| Distances M1,2 |  |  |  |  |  |  |  |  |  |
| Al1-O1 |  | 1.987(11) | 1.996(5) | 1.987(6) | 1.978(13) | 1.955(9) | 1.969(7) | 1.974(6) | 1.965(7) |
| Al1-O3 |  | 1.934(12) | 1.869(5) | 1.872(7) | 1.877(14) | 1.869(10) | 1.859(7) | 1.863(7) | 1.869(7) |
| Al1-O4 |  | 1.833(10) | 1.811(4) | 1.832(5) | 1.833(12) | 1.803(8) | 1.826(6) | 1.849(6) | 1.806(6) |
| Al1-O5 |  | 1.956(11) | 1.922(4) | 1.950(6) | 1.929(13) | 1.954(9) | 1.930(6) | 1.921(6) | 1.937(6) |
| Al1-O6 |  | 1.831(11) | 1.934(5) | 1.948(6) | 1.901(14) | 1.926(10) | 1.963(7) | 1.952(7) | 1.964(7) |
| Al1-O10 |  | 1.817(10) | 1.839(4) | 1.854(5) | 1.803(11) | 1.836(8) | 1.874(6) | 1.836(6) | 1.856(6) |
|  | Mean (6) | 1.89 | 1.90 | 1.91 | 1.89 | 1.89 | 1.90 | 1.90 |  |
| Distances M3 |  |  |  |  |  |  |  |  |  |
| Al2-O1 | x2 | 2.063(12) | 2.111(5) | 2.128(7) | 2.105(14) | 2.097(10) | 2.096(7) | 2.115(6) | 2.124(7) |
| Al2-O2 | x2 | 1.994(13) | 1.979(5) | 1.962(6) | 1.958(13) | 2.010(10) | 1.978(7) | 1.966(6) | 1.954(6) |
| Al2-O4 |  | 1.914(17) | 1.846(8) | 1.831(9) | 1.816(21) | 1.847(15) | 1.848(10) | 1.876(10) | 1.840(9) |
| Al2-O8 |  | 1.715(18) | 1.701(8) | 1.756(9) | 1.684(23) | 1.706(16) | 1.747(11) | 1.706(11) | 1.717(10) |
|  | Mean (6) | 1.96 | 1.95 | 1.96 | 1.94 | 1.96 | 1.96 | 1.96 |  |
| Distances T1 |  |  |  |  |  |  |  |  |  |
| Si1-O1 | x2 | 1.657(10) | 1.642(4) | 1.649(5) | 1.670(11) | 1.652(8) | 1.661(6) | 1.670(5) | 1.652(6) |
| Si1-O7 |  | 1.569(14) | 1.575(7) | 1.538(8) | 1.599(17) | 1.567(14) | 1.538(10) | 1.553(9) | 1.507(9) |
| Si1-O9 |  | 1.678(15) | 1.592(7) | 1.607(9) | 1.506(20) | 1.567(13) | 1.638(9) | 1.600(9) | 1.595(9) |
|  | Mean (4) | 1.64 | 1.61 | 1.61 | 1.61 | 1.61 | 1.62 | 1.62 |  |
| Distances T2 |  |  |  |  |  |  |  |  |  |
| Si2-O3 | x2 | 1.562(12) | 1.594(5) | 1.598(6) | 1.572(13) | 1.590(9) | 1.600(7) | 1.597(6) | 1.574(6) |
| Si2-O8 |  | 1.625(18) | 1.661(8) | 1.606(9) | 1.698(22) | 1.661(16) | 1.649(10) | 1.668(11) | 1.669(10) |
| Si2-O9 |  | 1.592(15) | 1.667(7) | 1.675(9) | 1.742(20) | 1.710(13) | 1.663(9) | 1.676(9) | 1.724(9) |
|  | Mean (4) | 1.59 | 1.63 | 1.62 | 1.65 | 1.64 | 1.63 | 1.63 |  |
| Distances T3 |  |  |  |  |  |  |  |  |  |
| Si3-O2 | x2 | 1.539(13) | 1.577(5) | 1.583(5) | 1.547(11) | 1.558(8) | 1.573(6) | 1.592(5) | 1.592(5) |
| Si3-O5 |  | 1.618(17) | 1.638(6) | 1.604(8) | 1.620(20) | 1.571(13) | 1.652(9) | 1.640(8) | 1.632(9) |
| Si3-O6 |  | 1.820(17) | 1.700(7) | 1.684(8) | 1.742(18) | 1.728(13) | 1.662(9) | 1.660(9) | 1.641(9) |
|  | Mean (4) | 1.63 | 1.62 | 1.61 | 1.61 | 1.60 | 1.62 | 1.62 |  |

Table A2: Interatomic angels in zoisite [°]

| Run no. |  | Au32 | Au40 | Au45 | Pt4 | Au31 | Au34 | Au30 | Pt3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| XSrzo |  | 0.06 | 0.13 | 0.16 | 0.22 | 0.25 | 0.24 | 0.32 | 0.42 |
| Angles M1,2 |  |  |  |  |  |  |  |  |  |
| O1-Al1-O4 |  | 83.2(4) | 83.2(4) | 82.2(4) | 82.48(24) | 85.4(5) | 84.3(1) | 83.8(0) | 82.96(27) |
| O1-Al1-O5 |  | 87.1(5) | 87.4(4) | 87.0(5) | 86.95(24) | 87.6(5) | 86.2(1) | 85.7(0) | 86.57(25) |
| O1-Al1-O6 |  | 94.6(5) | 94.3(4) | 95.2(5) | 92.66(24) | 95.5(5) | 95.1(1) | 93.9(0) | 92.44(25) |
| O1-Al1-O10 |  | 91.2(5) | 91.0(4) | 91.8(5) | 90.73(26) | 89.6(6) | 90.3(2) | 90.0(0) | 89.94(27) |
| O3-Al1-O4 |  | 92.1(5) | 93.1(4) | 92.5(5) | 93.12(27) | 90.0(6) | 92.0(1) | 92.7(1) | 92.59(29) |
| O3-Al1-O5 |  | 90.4(5) | 89.3(5) | 89.5(5) | 90.35(26) | 87.8(5) | 88.0(1) | 90.1(1) | 90.31(28) |
| O3-Al1-O6 |  | 87.9(4) | 89.1(4) | 88.2(5) | 90.18(24) | 88.8(5) | 90.5(1) | 90.4(1) | 90.92(25) |
| O3-Al1-O10 |  | 93.4(5) | 92.6(4) | 93.5(5) | 93.60(25) | 94.6(6) | 93.2(1) | 93.2(0) | 94.42(26) |
| O4-Al1-O5 |  | 95.2(4) | 96.0(4) | 94.6(4) | 96.20(27) | 92.9(5) | 95.4(2) | 96.3(1) | 96.21(27) |
| O4-Al1-O6 |  | 84.7(4) | 85.85(33) | 84.4(4) | 85.62(21) | 85.0(4) | 84.1(1) | 84.1(1) | 86.52(23) |
| O5-Al1-O10 |  | 83.2(4) | 82.26(31) | 83.0(4) | 82.28(20) | 82.6(4) | 82.7(2) | 81.8(1) | 82.16(25) |
| O6-Al1-O10 |  | 97.1(4) | 96.0(4) | 98.3(5) | 95.84(26) | 99.8(5) | 98.1(1) | 97.8(1) | 94.97(29) |
|  | Mean(12) | 90.0 | 90.0 | 90.0 | 90.0 | 90.0 | 90.0 | 90.0 | 90.0 |
| ## Angles M3 |  |  |  |  |  |  |  |  |  |
| O1-Al2-O1 |  | 84.2(5) | 85.2(4) | 85.2(5) | 82.79(26) | 85.1(5) | 85.6(2) | 85.8(1) | 83.74(31) |
| O1-Al2-O2 | x2 | 89.37(32) | 89.26(26) | 88.34(31) | 89.11(16) | 88.11(35) | 87.6(2) | 87.6(1) | 88.76(17) |
| O1-Al2-O4 | x2 | 80.3(4) | 81.22(33) | 79.8(4) | 79.24(22) | 81.5(4) | 79.4(3) | 79.7(0) | 79.72(25) |
| O1-Al2-O8 | x2 | 99.6(5) | 98.9(4) | 99.6(5) | 99.00(25) | 100.5(6) | 100.1(4) | 99.0(0) | 99.94(28) |
| O2-Al2-O2 |  | 95.8(5) | 95.5(5) | 96.7(5) | 97.90(31) | 97.2(6) | 97.8(2) | 98.0(1) | 97.5(4) |
| O2-Al2-O4 | x2 | 90.8(4) | 91.85(34) | 90.9(4) | 92.04(23) | 89.0(5) | 91.0(1) | 91.7(0) | 91.29(25) |
| O2-Al2-O8 | x2 | 89.3(5) | 88.0(4) | 89.7(5) | 89.52(23) | 89.2(5) | 89.5(1) | 89.4(0) | 89.01(25) |
|  | Mean(12) | 89.9 | 89.9 | 89.9 | 89.9 | 89.9 | 89.9 | 89.9 | 89.9 |
| ## Angles T1 |  |  |  |  |  |  |  |  |  |
| O1-Si1-O1 |  | 114.0(7) | 114.4(6) | 113.4(7) | 115.6(4) | 112.4(7) | 110.9(1) | 111.7(1) | 114.8(4) |
| O1-Si1-O7 | x2 | 107.5(4) | 108.49(33) | 107.6(4) | 110.20(22) | 107.9(5) | 109.8(1) | 109.3(1) | 111.22(26) |
| O1-Si1-O9 | x2 | 108.37(34) | 107.41(31) | 107.9(4) | 104.96(21) | 107.8(4) | 106.8(1) | 106.8(0) | 104.86(26) |
| O7-Si1-O9 |  | 111.1(7) | 110.6(6) | 112.4(7) | 110.6(4) | 113.2(8) | 112.6(3) | 112.8(1) | 109.3(5) |
|  | Mean (6) | 109.5 | 109.5 | 109.5 | 109.4 | 109.5 | 109.5 | 109.5 | 109.4 |
| Angles T2 |  |  |  |  |  |  |  |  |  |
| O3-Si2-O3 |  | 109.0(7) | 111.0(6) | 109.1(7) | 109.5(4) | 108.4(7) | 115.1(3) | 111.6(1) | 110.3(4) |
| O3-Si2-O8 | x2 | 112.8(4) | 111.1(4) | 112.8(4) | 110.67(24) | 111.8(5) | 110.9(4) | 111.4(1) | 111.00(27) |
| O3-Si2-O9 | x2 | 105.3(4) | 105.9(4) | 105.4(4) | 105.81(24) | 105.4(5) | 104.4(4) | 105.8(0) | 105.07(29) |
| O8-Si2-O9 |  | 111.0(8) | 111.6(7) | 111.0(9) | 114.1(4) | 113.6(10) | 110.7(3) | 110.5(1) | 114.1(5) |
|  | Mean (6) | 109.4 | 109.4 | 109.4 | 109.4 | 109.4 | 109.4 | 109.4 | 109.4 |
| ## Angles T3 |  |  |  |  |  |  |  |  |  |
| O2-Si3-O2 |  | 113.6(6) | 111.0(5) | 110.2(6) | 109.01(31) | 112.8(7) | 110.4(1) | 110.7(1) | 108.2(4) |
| O2-Si3-O5 | x2 | 111.0(4) | 111.5(4) | 111.3(5) | 110.96(26) | 111.7(5) | 110.6(1) | 111.15(1) | 111.13(31) |
| O2-Si3-O6 | x2 | 111.9(4) | 113.1(4) | 113.2(4) | 114.19(25) | 112.1(5) | 113.7(1) | 113.23(1) | 114.07(28) |
| O5-Si3-O6 |  | 96.3(6) | 95.8(5) | 97.2(6) | 97.07(35) | 95.2(6) | 97.2(1) | 96.64(1) | 97.9(4) |
|  | Mean (6) | 109.3 | 109.3 | 109.4 | 109.4 | 109.3 | 109.4 | 109.4 | 109.4 |

(continued)

Table A2, continued

| Run no. |  | Au42 | Pt36 | Pt2 | Au23 | Au22 | Au33 | Au44 | Au21 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| XSrzo |  | 0.37 | 0.52 | 0.63 | 0.66 | 0.77 | 0.86 | 0.87 | 1 |
| Angles M1,2 |  |  |  |  |  |  |  |  |  |
| O1-Al1-O4 |  | 84.6(6) | 82.89(28) | 82.85(32) | 81.6(8) | 83.2(5) | 83.1(4) | 83.33(33) | 82.97(33) |
| O1-Al1-O5 |  | 86.3(6) | 88.11(25) | 86.78(29) | 86.1(7) | 86.0(5) | 87.9(4) | 86.27(32) | 86.07(32) |
| O1-Al1-O6 |  | 94.5(6) | 91.88(24) | 92.09(29) | 93.3(6) | 91.6(4) | 92.86(33) | 92.33(30) | 93.10(31) |
| O1-Al1-O10 |  | 90.1(7) | 91.11(25) | 90.59(30) | 91.8(6) | 93.0(5) | 92.60(34) | 91.60(32) | 91.50(32) |
| O3-Al1-O4 |  | 90.2(7) | 93.46(30) | 93.48(35) | 93.1(8) | 91.9(5) | 92.7(4) | 92.15(34) | 94.11(34) |
| O3-Al1-O5 |  | 89.3(6) | 89.56(27) | 90.16(33) | 90.5(8) | 91.4(5) | 89.9(4) | 91.56(35) | 92.46(35) |
| O3-Al1-O6 |  | 89.7(6) | 90.61(26) | 91.12(32) | 90.2(7) | 91.1(5) | 89.50(34) | 90.02(32) | 88.55(32) |
| O3-Al1-O10 |  | 94.9(7) | 92.52(25) | 93.02(31) | 93.4(7) | 91.8(5) | 91.66(34) | 92.85(33) | 91.40(33) |
| O4-Al1-O5 |  | 94.7(6) | 97.03(22) | 95.42(28) | 96.2(7) | 96.4(5) | 96.66(33) | 95.95(30) | 97.15(32) |
| O4-Al1-O6 |  | 83.0(5) | 85.18(22) | 86.55(26) | 84.7(6) | 85.0(4) | 86.45(30) | 86.21(27) | 86.17(29) |
| O5-Al1-O10 |  | 82.9(5) | 82.34(22) | 83.24(28) | 81.0(6) | 82.2(4) | 83.07(32) | 82.23(28) | 81.97(30) |
| O6-Al1-O10 |  | 99.5(6) | 95.43(22) | 94.64(29) | 98.0(6) | 96.3(5) | 93.86(33) | 95.47(31) | 94.60(33) |
|  | Mean(12) | 90.0 | 90.0 | 90.0 | 90.0 | 90.0 | 90.0 | 90.0 |  |
| Angles M3 |  |  |  |  |  |  |  |  |  |
| O1-Al2-O1 |  | 85.7(6) | 83.62(28) | 82.88(35) | 84.2(7) | 84.3(5) | 83.8(4) | 83.57(35) | 84.0(4) |
| O1-Al2-O2 | x2 | 86.7(4) | 88.16(15) | 88.23(20) | 85.8(4) | 87.53(27) | 87.46(22) | 87.55(19) | 86.77(21) |
| O1-Al2-O4 | x2 | 80.6(5) | 78.96(23) | 79.02(28) | 78.5(6) | 78.3(4) | 79.10(32) | 78.92(29) | 77.86(29) |
| O1-Al2-O8 | x2 | 100.2(6) | 99.92(26) | 98.13(32) | 99.1(7) | 99.0(5) | 98.34(34) | 97.99(32) | 98.05(33) |
| O2-Al2-O2 |  | 99.6(8) | 98.49(31) | 99.2(4) | 102.5(9) | 99.0(6) | 99.9(5) | 99.7(4) | 101.0(4) |
| O2-Al2-O4 | x2 | 90.0(6) | 90.79(24) | 91.11(28) | 90.7(6) | 91.2(4) | 91.28(30) | 90.51(27) | 91.99(28) |
| O2-Al2-O8 | x2 | 89.3(6) | 90.20(25) | 91.37(30) | 91.3(7) | 91.2(5) | 90.96(34) | 92.20(31) | 91.56(30) |
|  | Mean(12) | 89.9 | 89.8 | 89.8 | 89.8 | 89.8 | 89.8 | 89.8 |  |
| Angles T1 |  |  |  |  |  |  |  |  |  |
| O1-Si1-O1 |  | 112.6(9) | 114.2(4) | 113.7(5) | 111.5(10) | 114.2(7) | 114.6(6) | 112.3(5) | 113.0(5) |
| O1-Si1-O7 | x2 | 109.9(5) | 110.80(24) | 110.91(29) | 108.9(6) | 110.1(4) | 110.70(32) | 110.74(29) | 110.36(33) |
| O1-Si1-O9 | x2 | 107.0(5) | 105.42(23) | 104.62(28) | 107.4(6) | 106.6(4) | 106.57(30) | 106.77(29) | 106.45(32) |
| O7-Si1-O9 |  | 110.4(8) | 109.9(4) | 111.7(5) | 112.6(11) | 108.9(9) | 107.3(6) | 109.3(5) | 110.1(6) |
|  | Mean (6) | 109.5 | 109.4 | 109.4 | 109.5 | 109.4 | 109.4 | 109.4 |  |
| Angles T2 |  |  |  |  |  |  |  |  |  |
| O3-Si2-O3 |  | 115.1(11) | 110.1(4) | 110.8(5) | 110.6(12) | 106.7(8) | 108.8(6) | 109.4(5) | 109.3(5) |
| O3-Si2-O8 | x2 | 110.9(6) | 110.73(23) | 111.52(30) | 111.6(6) | 112.2(4) | 111.02(32) | 110.73(29) | 110.94(33) |
| O3-Si2-O9 | x2 | 104.0(6) | 106.24(24) | 104.78(32) | 104.8(7) | 105.4(5) | 106.25(35) | 106.70(31) | 106.30(35) |
| O8-Si2-O9 |  | 111.6(11) | 112.6(4) | 113.1(5) | 112.9(12) | 114.3(8) | 113.2(6) | 112.4(5) | 112.8(5) |
|  | Mean (6) | 109.4 | 109.4 | 109.4 | 109.4 | 109.4 | 109.4 | 109.4 |  |
| Angles T3 |  |  |  |  |  |  |  |  |  |
| O2-Si3-O2 |  | 109.8(10) | 109.3(4) | 109.8(5) | 109.5(11) | 108.5(7) | 109.3(5) | 108.8(4) | 108.5(5) |
| O2-Si3-O5 | x2 | 110.9(7) | 111.46(26) | 111.01(33) | 109.8(7) | 112.0(5) | 111.1(4) | 109.98(32) | 109.3(4) |
| O2-Si3-O6 | x2 | 113.6(7) | 113.63(24) | 113.64(30) | 113.9(7) | 112.8(5) | 113.25(34) | 113.57(30) | 114.31(34) |
| O5-Si3-O6 |  | 97.6(8) | 96.9(4) | 97.2(4) | 99.5(10) | 98.6(7) | 98.4(5) | 100.6(4) | 100.8(4) |
|  | Mean (6) | 109.4 | 109.4 | 109.4 | 109.4 | 109.5 | 109.4 | 109.4 |  |

Table A3: Conventional valence bond calculations for positions A1 and A2 in zoisite, based on bond valence data of  Brown & Altermatt (1985)

| ## Run no. |  | Au32 | Au40 | Au45 | Pt4 | Au31 | Au34 | Au30 | Pt3 | Au42 | Pt36 | Pt2 | Au23 | Au22 | Au33 | Au44 | Au21 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| XSrzo |  | 0.06 | 0.13 | 0.16 | 0.22 | 0.25 | 0.24 | 0.32 | 0.42 | 0.37 | 0.52 | 0.63 | 0.66 | 0.77 | 0.86 | 0.87 | 1 |
| XSr A1 |  | 0.02 | 0.04 | 0.03 | 0.03 | 0.06 | 0.00 | 0.04 | 0.13 | 0.09 | 0.20 | 0.38 | 0.41 | 0.61 | 0.76 | 0.82 | 1 |
| XSr A2 |  | 0.09 | 0.22 | 0.29 | 0.40 | 0.44 | 0.48 | 0.59 | 0.72 | 0.67 | 0.84 | 0.89 | 0.92 | 0.93 | 0.96 | 0.92 | 1 |
| Valence bond parameters* |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Ro† (A1) |  | 1.970 | 1.973 | 1.972 | 1.972 | 1.976 | 1.967 | 1.973 | 1.987 | 1.981 | 1.997 | 2.024 | 2.029 | 2.059 | 2.082 | 2.091 | 2.118 |
| Ro† (A2) |  | 1.981 | 2.000 | 2.011 | 2.027 | 2.033 | 2.039 | 2.056 | 2.076 | 2.068 | 2.094 | 2.101 | 2.106 | 2.107 | 2.112 | 2.106 | 2.118 |
| B |  | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 |
| ## Valence bond strength for A1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| A1-O1 | 2x | 0.223 | 0.215 | 0.211 | 0.222 | 0.217 | 0.206 | 0.215 | 0.225 | 0.220 | 0.233 | 0.255 | 0.234 | 0.255 | 0.281 | 0.283 | 0.301 |
| A1-O3 | 2x | 0.279 | 0.289 | 0.271 | 0.282 | 0.277 | 0.296 | 0.267 | 0.293 | 0.279 | 0.275 | 0.293 | 0.290 | 0.289 | 0.299 | 0.306 | 0.301 |
| A1-O5 |  | 0.198 | 0.212 | 0.208 | 0.195 | 0.231 | 0.206 | 0.190 | 0.193 | 0.199 | 0.228 | 0.214 | 0.211 | 0.218 | 0.261 | 0.239 | 0.260 |
| A1-O6 |  | 0.185 | 0.193 | 0.180 | 0.203 | 0.180 | 0.176 | 0.191 | 0.210 | 0.179 | 0.217 | 0.225 | 0.207 | 0.256 | 0.223 | 0.237 | 0.237 |
| A1-O7 |  | 0.395 | 0.463 | 0.406 | 0.446 | 0.418 | 0.411 | 0.414 | 0.461 | 0.506 | 0.501 | 0.460 | 0.520 | 0.521 | 0.506 | 0.547 | 0.447 |
| A1-O9 | 2x | 0.077 | 0.079 | 0.079 | 0.081 | 0.080 | 0.079 | 0.079 | 0.085 | 0.084 | 0.086 | 0.095 | 0.095 | 0.104 | 0.109 | 0.112 | 0.121 |
| Total bond strength A1 |  | 1.934 | 2.036 | 1.914 | 2.014 | 1.975 | 1.955 | 1.919 | 2.070 | 2.048 | 2.134 | 2.186 | 2.176 | 2.293 | 2.369 | 2.423 | 2.39 |
| Reference value |  | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 |
| Valence bond strength for A2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| A2-O2 | 2x | 0.216 | 0.231 | 0.218 | 0.222 | 0.213 | 0.208 | 0.211 | 0.230 | 0.204 | 0.223 | 0.227 | 0.202 | 0.219 | 0.214 | 0.219 | 0.213 |
| A2-O2 | 2x | 0.106 | 0.119 | 0.125 | 0.137 | 0.132 | 0.140 | 0.148 | 0.164 | 0.157 | 0.163 | 0.164 | 0.161 | 0.156 | 0.163 | 0.155 | 0.163 |
| A2-O3 | 2x | 0.251 | 0.279 | 0.271 | 0.265 | 0.291 | 0.313 | 0.314 | 0.277 | 0.327 | 0.305 | 0.306 | 0.292 | 0.294 | 0.306 | 0.314 | 0.321 |
| A2-O7 |  | 0.362 | 0.381 | 0.423 | 0.381 | 0.401 | 0.395 | 0.431 | 0.345 | 0.355 | 0.374 | 0.394 | 0.405 | 0.368 | 0.356 | 0.367 | 0.382 |
| A2-O8 | 2x | 0.056 | 0.062 | 0.060 | 0.068 | 0.066 | 0.067 | 0.069 | 0.076 | 0.072 | 0.075 | 0.074 | 0.073 | 0.071 | 0.072 | 0.068 | 0.069 |
| A2-O10 |  | 0.055 | 0.060 | 0.059 | 0.060 | 0.052 | 0.059 | 0.063 | 0.061 | 0.059 | 0.073 | 0.074 | 0.075 | 0.087 | 0.088 | 0.081 | 0.091 |
| Total bond strength A2 |  | 1.675 | 1.823 | 1.832 | 1.826 | 1.857 | 1.911 | 1.979 | 1.899 | 1.933 | 1.979 | 2.010 | 1.937 | 1.935 | 1.954 | 1.959 | 2.004 |
| Reference value |  | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 |

*Bond length from table A1

†Ro = RoCa+((RoSr-RoCa)*XSr(A1,A2)); RoCa=1.967, RoSr=2.118

Table A4: Calculated polyhedra volume [Å3] for A1, A2, M1,2, M3, T1, T2, T3 with quadratic elongation and variance for zoisite

| Run no. | Au32 | Au40 | Au45 | Pt4 | Au31 | #### Au34 | Au30 | Au42 | Pt3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| VA1[7] | 19.81 | 19.49 | 19.96 | 19.67 | 19.83 | 19.57 | 19.91 | 19.71 | 19.86 |
| VA2[7] | 23.46 | 23.06 | 23.30 | 23.66 | 23.54 | 23.36 | 23.54 | 23.84 | 24.32 |
| VM1,2 | 8.87 | 8.93 | 8.85 | 8.97 | 8.90 | 8.88 | 8.83 | 8.93 | 9.03 |
| quad | 1.00818 | 1.00821 | 1.00959 | 1.00844 | 1.00872 | 1.00896 | 1.01026 | 1.00991 | 1.00777 |
| variance | 22.5696 | 21.71959 | 26.72909 | 22.50972 | 24.52246 | 24.58820 | 26.77836 | 27.1855 | 21.03378 |
| VM3 | 9.23 | 9.49 | 9.30 | 9.65 | 9.66 | 9.77 | 9.80 | 9.71 | 9.77 |
| quad | 1.02266 | 1.01708 | 1.02254 | 1.02173 | 1.02218 | 1.02109 | 1.01998 | 1.02027 | 1.02016 |
| variance | 40.5455 | 34.74556 | 42.42622 | 47.12962 | 41.23824 | 47.39537 | 43.36998 | 47.17551 | 46.66571 |
| VT1 | 2.21 | 2.14 | 2.11 | 2.12 | 2.08 | 2.16 | 2.09 | 2.26 | 2.15 |
| quad | 1.00299 | 1.0025 | 1.00306 | 1.0049 | 1.00291 | 1.00219 | 1.00252 | 1.00203 | 1.00521 |
| variance | 6.72736 | 7.29725 | 7.23252 | 16.17863 | 6.62983 | 5.22204 | 6.16956 | 4.73104 | 15.44221 |
| VT2 | 2.15 | 2.20 | 2.23 | 2.13 | 2.16 | 2.18 | 2.15 | 1.98 | 2.10 |
| quad | 1.00477 | 1.00195 | 1.00354 | 1.00281 | 1.00454 | 1.00445 | 1.00254 | 1.00536 | 1.00341 |
| variance | 11.90902 | 7.63337 | 11.63823 | 10.24526 | 15.700081 | 17.51716 | 7.95131 | 20.48916 | 13.05005 |
| VT3 | 2.14 | 2.18 | 2.17 | 2.17 | 2.14 | 2.15 | 2.13 | 2.18 | 2.15 |
| quad | 1.01247 | 1.01193 | 1.01123 | 1.01101 | 1.0155 | 1.01141 | 1.01285 | 1.01613 | 1.00979 |
| variance | 41.1068 | 44.98664 | 36.95821 | 40.64444 | 47.73619 | 37.78345 | 39.98624 | 35.87196 | 36.48328 |
| Run no. | Pt36 | Au43 | Pt2 | Au23 | Au22 | Au33 | Au44 | #### Au21 |  |
| VA1[7] | 19.80 | 19.96 | 20.04 | 20.30 | 20.52 | 20.69 | 20.65 | 21.41 |  |
| VA2[7] | 24.40 | 24.44 | 24.49 | 24.92 | 25.06 | 25.08 | 24.90 | 25.12 |  |
| VM1,2 | 8.98 | 8.76 | 9.17 | 8.83 | 8.91 | 9.11 | 9.04 | 9.04 |  |
| quad | 1.00801 | 1.01394 | 1.00666 | 1.01049 | 1.00832 | 1.00641 | 1.00706 | 1.00844 |  |
| variance | 21.69545 | 34.23686 | 17.9355 | 30.35174 | 22.73402 | 17.91309 | 20.15701 | 23.2133 |  |
| VM3 | 9.68 | 9.57 | 9.80 | 9.39 | 9.77 | 9.74 | 9.74 | 9.63 |  |
| quad | 1.0244 | 1.01963 | 1.02216 | 1.02787 | 1.02435 | 1.02121 | 1.02259 | 1.0256 |  |
| variance | 51.05659 | 51.23664 | 47.44314 | 59.85964 | 51.41402 | 48.36439 | 48.19829 | 55.75985 |  |
| VT1 | 2.14 | 2.17 | 2.13 | 2.13 | 2.12 | 2.19 | 2.18 | 2.09 |  |
| quad | 1.00394 | 1.00303 | 1.00495 | 1.00408 | 1.00383 | 1.00442 | 1.00309 | 1.00394 |  |
| variance | 11.79461 | 8.57276 | 14.89172 | 4.54559 | 7.94464 | 10.14814 | 5.21533 | 6.46747 |  |
| VT2 | 2.21 | 2.15 | 2.16 | 2.12 | 2.23 | 2.20 | 2.23 | 2.23 |  |
| quad | 1.00269 | 1.00505 | 1.00364 | 1.00728 | 1.00594 | 1.00269 | 1.00245 | 1.00458 |  |
| variance | 6.8798 | 14.12947 | 13.40125 | 16.70919 | 15.74913 | 7.94769 | 5.40128 | 7.11989 |  |
| VT3 | 2.16 | 2.25 | 2.12 | 2.13 | 2.09 | 2.13 | 2.16 | 2.14 |  |
| quad | 1.01119 | 1.01912 | 1.0106 | 1.01045 | 1.0105 | 1.00834 | 1.00597 | 1.00636 |  |
| variance | 40.26778 | 62.63542 | 37.89872 | 27.61253 | 30.63564 | 31.38462 | 22.50358 | 24.47464 |  |

Table A5: Interatomic distances in clinozoisite [Å]

| ## Run no. |  | Au32 | Au45 | Au35 | Au34 | Pt8 | Au42 | Au43 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| XSrcz |  | 0.078 | 0.150 | 0.248 | 0.248 | 0.292 | 0.349 | 0.513 |
| Distances A1 |  |  |  |  |  |  |  |  |
| A1-O1 | X 2 | 2.502(11) | 2.533(14) | 2.528(12) | 2.554(15) | 2.541(8) | 2.523(11) | 2.559(11) |
| -O3 | X 2 | 2.339(10) | 2.313(13) | 2.355(12) | 2.375(14) | 2.376(8) | 2.406(10) | 2.415(11) |
| -O5 |  | 2.532(15) | 2.546(20) | 2.401(15) | 2.432(16) | 2.456(11) | 2.457(13) | 2.511(14) |
| -O6 |  | 2.640(28) | 2.649(29) | 2.731(21) | 2.755(25) | 2.718(12) | 2.717(12) | 2.700(16) |
| -O7 |  | 2.164(15) | 2.137(21) | 2.120(18) | 2.054(21) | 2.241(11) | 2.199(16) | 2.211(19) |
| Mean (7) |  | 2.43 | 2.43 | 2.43 | 2.44 | 2.46 | 2.46 | 2.48 |
| -O9 | X 2 | 2.933(6) | 2.933(7) | 2.922(6) | 2.904(7) | 2.915(4) | 2.908(5) | 2.911(5) |
| Distances A2 |  |  |  |  |  |  |  |  |
| A2-O2 | X 2 | 2.807(9) | 2.772(11) | 2.770(9) | 2.781(12) | 2.783(7) | 2.778(10) | 2.810(11) |
| -O2 | X 2 | 2.493(9) | 2.600(11) | 2.589(9) | 2.608(11) | 2.602(7) | 2.615(9) | 2.647(9) |
| -O3 | X 2 | 2.493(10) | 2.493(12) | 2.517(9) | 2.521(12) | 2.584(7) | 2.605(9) | 2.619(11) |
| -O7 |  | 2.449(17) | 2.394(22) | 2.414(19) | 2.421(23) | 2.381(13) | 2.396(16) | 2.417(17) |
| -O10 |  | 2.638(16) | 2.579(26) | 2.676(18) | 2.637(24) | 2.698(12) | 2.643(15) | 2.664(18) |
| Mean (8) |  | 2.58 | 2.59 | 2.61 | 2.61 | 2.63 | 2.63 | 2.65 |
| -O8 | X 2 | 3.024(6) | 2.957(6) | 3.015(7) | 3.041(10) | 3.024(5) | 3.037(7) | 3.068(7) |
| Distances M1 |  |  |  |  |  |  |  |  |
| Al1-O1 | X 2 | 1.896(10) | 1.955(12) | 1.924(10) | 1.887(13) | 1.949(6) | 1.878(9) | 1.917(11) |
| Al1-O4 | X 2 | 1.776(9) | 1.808(11) | 1.839(10) | 1.847(13) | 1.834(7) | 1.827(9) | 1.827(8) |
| Al1-O5 | X 2 | 1.922(11) | 1.900(14) | 1.959(12) | 1.958(12) | 1.981(9) | 1.940(10) | 1.969(10) |
| Mean (6) |  | 1.86 | 1.89 | 1.91 | 1.90 | 1.92 | 1.88 | 1.90 |
| Distances M2 |  |  |  |  |  |  |  |  |
| Al2-O3 | X 2 | 1.895(9) | 1.898(11) | 1.906(10) | 1.932(13) | 1.855(8) | 1.926(10) | 1.912(13) |
| Al2-O6 | X 2 | 1.980(22) | 1.917(26) | 1.953(17) | 1.988(20) | 1.973(8) | 1.977(9) | 1.986(11) |
| Al2-O10 | X 2 | 1.927(15) | 1.867(20) | 1.804(13) | 1.786(17) | 1.824(8) | 1.826(10) | 1.841(11) |
| Mean (6) |  | 1.93 | 1.89 | 1.89 | 1.90 | 1.88 | 1.91 | 1.91 |
| Distances M3 |  |  |  |  |  |  |  |  |
| Al3-O1 | X 2 | 2.175(12) | 2.156(15) | 2.127(13) | 2.067(16) | 2.152(9) | 2.129(12) | 2.111(13) |
| Al3-O2 | X 2 | 1.969(11) | 1.924(13) | 1.966(10) | 1.993(13) | 1.942(8) | 1.959(10) | 1.949(10) |
| Al3-O4 |  | 1.931(17) | 1.921(19) | 1.893(14) | 1.963(18) | 1.827(11) | 1.908(13) | 1.954(15) |
| Al3-O8 |  | 1.806(19) | 1.934(23) | 1.774(20) | 1.696(26) | 1.755(13) | 1.762(20) | 1.685(22) |
| Mean (6) |  | 2.00 | 2.00 | 1.98 | 1.96 | 1.96 | 1.97 | 1.96 |
| Distances T1 |  |  |  |  |  |  |  |  |
| Si1-O1 | X 2 | 1.664(12) | 1.683(15) | 1.690(13) | 1.750(16) | 1.638(8) | 1.727(11) | 1.686(12) |
| Si1-O7 |  | 1.549(17) | 1.585(22) | 1.610(19) | 1.642(23) | 1.539(13) | 1.585(17) | 1.584(18) |
| Si1-O9 |  | 1.652(21) | 1.655(27) | 1.653(21) | 1.651(25) | 1.681(13) | 1.642(17) | 1.544(18) |
| Mean (4) |  | 1.63 | 1.65 | 1.66 | 1.70 | 1.62 | 1.67 | 1.63 |
| ## Distances T2 |  |  |  |  |  |  |  |  |
| Si2-O3 | X 2 | 1.613(9) | 1.614(11) | 1.600(10) | 1.566(12) | 1.616(7) | 1.521(9) | 1.545(11) |
| Si2-O8 |  | 1.596(18) | 1.576(21) | 1.653(18) | 1.657(25) | 1.657(12) | 1.630(18) | 1.653(20) |
| Si2-O9 |  | 1.594(21) | 1.562(24) | 1.592(19) | 1.548(22) | 1.563(13) | 1.568(16) | 1.660(17) |
| Mean (4) |  | 1.60 | 1.59 | 1.61 | 1.58 | 1.61 | 1.56 | 1.60 |
| Distances T3 |  |  |  |  |  |  |  |  |
| Si3-O2 | X 2 | 1.621(8) | 1.629(10) | 1.611(9) | 1.608(10) | 1.617(6) | 1.605(9) | 1.596(9) |
| Si3-O5 |  | 1.681(16) | 1.698(20) | 1.693(16) | 1.658(18) | 1.628(13) | 1.649(14) | 1.598(16) |
| Si3-O6 |  | 1.599(28) | 1.66(4) | 1.621(24) | 1.587(27) | 1.599(12) | 1.635(14) | 1.651(16) |
| Mean (4) |  | 1.63 | 1.65 | 1.63 | 1.62 | 1.62 | 1.62 | 1.61 |

Table A6. Selected interatomic angles in clinozoisite [°]

| Run no. |  | Au32 | Au45 | Au35 | Au34 | Pt8 | Au42 | Au43 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| XSrcz |  | 0.078 | 0.150 | 0.248 | 0.248 | 0.292 | 0.349 | 0.513 |
| Angles M1 |  |  |  |  |  |  |  |  |
| O1-Al1-O4 | X 2 | 86.1(6) | 86.1(7) | 85.3(5) | 85.7(7) | 83.3(4) | 85.0(5) | 85.5(6) |
| O1-Al1-O4 | X 2 | 93.9(6) | 93.9(7) | 94.7(5) | 94.3(7) | 96.7(4) | 95.0(5) | 94.5(6) |
| O1-Al1-O5 | X 2 | 89.8(5) | 89.7(7) | 93.2(5) | 92.7(6) | 90.0(4) | 91.7(5) | 89.7(5) |
| O1-Al1-O5 | X 2 | 90.2(5) | 90.3(7) | 86.8(5) | 87.3(6) | 90.0(4) | 88.3(5) | 90.3(5) |
| O4-Al1-O5 | X 2 | 81.7(5) | 82.3(6) | 84.9(5) | 85.3(6) | 85.2(4) | 83.9(4) | 84.8(4) |
| O4-Al1-O5 | X 2 | 98.3(5) | 97.7(6) | 95.1(5) | 94.7(6) | 94.8(4) | 96.1(4) | 95.2(4) |
| Mean (12) |  | 90 | 90 | 90 | 90 | 90 | 90 | 90 |
| Angels M2 |  |  |  |  |  |  |  |  |
| O3-Al2-O6 | X 2 | 86.8(8) | 86.5(9) | 89.9(7) | 91.4(8) | 89.7(4) | 90.1(4) | 89.2(5) |
| O3-Al2-O6 | X 2 | 93.2(8) | 93.5(9) | 90.1(7) | 88.6(8) | 90.3(4) | 89.9(4) | 90.8(5) |
| O3-Al2-O10 | X 2 | 89.0(6) | 85.9(9) | 86.9(7) | 85.2(8) | 89.0(4) | 88.0(5) | 87.8(6) |
| O3-Al2-O10 | X 2 | 91.0(6) | 94.1(9) | 93.1(7) | 94.8(8) | 91.0(4) | 92.0(5) | 92.2(6) |
| O6-Al2-O10 | X 2 | 88.6(7) | 84.4(9) | 83.6(6) | 83.6(8) | 84.95(34) | 84.7(4) | 85.3(4) |
| O6-Al2-O10 | X 2 | 91.4(7) | 95.6(9) | 96.4(6) | 96.4(8) | 95.05(34) | 95.3(4) | 94.7(4) |
| Mean (12) |  | 90 | 90 | 90 | 90 | 90 | 90 | 90 |
| Angles M3 |  |  |  |  |  |  |  |  |
| O1-Al3-O1 |  | 79.7(7) | 79.9(9) | 81.1(7) | 82.3(10) | 82.4(5) | 80.9(6) | 83.1(7) |
| O2-Al3-O2 |  | 97.2(6) | 102.8(8) | 98.8(7) | 96.9(8) | 98.5(5) | 99.1(7) | 98.0(7) |
| O1-Al3-O2 | X 2 | 91.11(32) | 88.5(4) | 89.65(34) | 89.5(4) | 89.09(24) | 89.19(33) | 88.2(4) |
| O1-Al3-O4 | X 2 | 75.0(5) | 78.0(6) | 78.5(5) | 78.1(6) | 77.9(4) | 76.4(4) | 77.3(5) |
| O1-Al3-O8 | X 2 | 99.4(5) | 100.3(7) | 101.4(6) | 102.9(8) | 100.3(4) | 101.7(5) | 101.3(7) |
| O2-Al3-O4 | X 2 | 96.3(5) | 96.3(6) | 93.8(5) | 91.1(7) | 93.8(4) | 92.9(5) | 90.1(5) |
| O2-Al3-O8 | X 2 | 88.6(5) | 85.1(6) | 86.3(5) | 88.0(8) | 87.8(4) | 88.8(5) | 91.1(7) |
| Mean (12) |  | 89.8 | 89.9 | 89.9 | 89.9 | 89.9 | 89.8 | 89.8 |
| Angles T1 |  |  |  |  |  |  |  |  |
| O7-Si1-O9 |  | 101.8(10) | 107.1(12) | 107.2(10) | 109.1(13) | 110.5(7) | 112.3(9) | 111.4(11) |
| O1-Si1-O1 |  | 113.8(9) | 113.0(11) | 112.5(9) | 109.5(11) | 113.5(6) | 109.2(8) | 111.2(10) |
| O1-Si1-O7 | X 2 | 113.3(6) | 109.8(7) | 111.9(6) | 111.7(7) | 111.5(4) | 111.1(5) | 109.1(6) |
| O1-Si1-O9 | X 2 | 106.8(5) | 108.5(6) | 106.4(6) | 107.4(7) | 104.7(4) | 106.4(5) | 108.0(6) |
| Mean (6) |  | 109.3 | 109.5 | 109.4 | 109.5 | 109.4 | 109.4 | 109.5 |
| Angles T2 |  |  |  |  |  |  |  |  |
| O8-Si2-O9 |  | 113.1(10) | 117.8(13) | 114.8(11) | 114.5(14) | 116.1(7) | 114.0(10) | 112.5(10) |
| O3-Si2-O3 |  | 114.0(8) | 115.0(9) | 113.9(9) | 112.8(11) | 108.4(6) | 111.1(9) | 109.3(11) |
| O3-Si2-O8 | X 2 | 109.2(5) | 107.5(6) | 109.5(5) | 110.6(7) | 110.8(4) | 111.6(5) | 112.3(6) |
| O3-Si2-O9 | X 2 | 105.6(6) | 104.7(8) | 104.6(6) | 104.1(8) | 105.1(4) | 104.1(6) | 105.0(7) |
| Mean (6) |  | 109.5 | 109.5 | 109.5 | 109.5 | 109.4 | 109.4 | 109.4 |
| Angles T3 |  |  |  |  |  |  |  |  |
| O5-Si3-O6 |  | 96.2(11) | 99.8(13) | 96.6(9) | 97.8(11) | 97.9(6) | 97.8(7) | 97.0(9) |
| O2-Si3-O2 |  | 107.9(7) | 104.0(9) | 107.0(8) | 107.6(10) | 109.2(5) | 108.1(8) | 111.8(10) |
| O2-Si3-O5 | X 2 | 113.0(5) | 110.5(7) | 114.0(5) | 114.8(6) | 112.0(4) | 114.0(5) | 112.3(6) |
| O2-Si3-O6 | X 2 | 113.3(6) | 116.1(7) | 112.6(6) | 110.9(7) | 112.7(4) | 111.3(5) | 111.4(6) |
| Mean (6) |  | 109.5 | 109.5 | 109.5 | 109.5 | 109.4 | 109.4 | 109.4 |
| Other Angles |  |  |  |  |  |  |  |  |
| Si1-O9-Si2 |  | 164.58 | 165.66 | 169.7 | 173.99 | 172.93 | 172.65 | 171.64 |
| Si2-O8-Al3 |  | 150.41 | 141.22 | 146.97 | 150.215 | 147.62 | 150.8 | 153.023 |
| O5-O6-O10 |  | 156.19 | 154.24 | 148.46 | 146.15 | 150.4 | 149.61 | 152.06 |
| O7-O9-O8 |  | 124.32 | 127.53 | 121.13 | 116.37 | 121.22 | 120.45 | 119.88 |

Table A7: Conventional valence bond calculations for positions A1 and A2 in clinozoisite, based on bond valence data of  Brown & Altermatt (1985)

| Run no |  | Au32 | Au45 | Au35 | Au34 | Pt8 | Au42 | Au43 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| XSrcz |  | 0.078 | 0.15 | 0.248 | 0.248 | 0.292 | 0.349 | 0.513 |
| XSr A1 |  | 0.029 | 0 | 0.034 | 0 | 0.058 | 0 | 0.148 |
| XSr A2 |  | 0.128 | 0.3 | 0.462 | 0.496 | 0.526 | 0.698 | 0.878 |
| Valence bond parameters* |  |  |  |  |  |  |  |  |
| Ro† A1 |  | 1.971 | 1.967 | 1.972 | 1.967 | 1.976 | 1.967 | 1.989 |
| Ro† A2 |  | 1.986 | 2.012 | 2.037 | 2.042 | 2.046 | 2.072 | 2.100 |
| B |  | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 | 0.37 |
| Valence bond strength for A1 |  |  |  |  |  |  |  |  |
| Ca1-O1 | 2x | 0.238 | 0.217 | 0.223 | 0.205 | 0.217 | 0.223 | 0.214 |
| Ca1-O3 | 2x | 0.370 | 0.393 | 0.355 | 0.332 | 0.339 | 0.305 | 0.317 |
| Ca1-O5 |  | 0.220 | 0.209 | 0.314 | 0.285 | 0.273 | 0.266 | 0.244 |
| Ca1-O6 |  | 0.164 | 0.158 | 0.129 | 0.119 | 0.135 | 0.132 | 0.147 |
| Ca1-O7 |  | 0.594 | 0.632 | 0.671 | 0.790 | 0.488 | 0.534 | 0.549 |
| Ca1-O9 | 2x | 0.074 | 0.073 | 0.077 | 0.079 | 0.079 | 0.079 | 0.083 |
| Total bond strength A1 |  | 2.34 | 2.36 | 2.42 | 2.43 | 2.17 | 2.14 | 2.17 |
| Reference value |  | 2 | 2 | 2 | 2 | 2 | 2 | 2 |
| Valence bond strength for A2 |  |  |  |  |  |  |  |  |
| Ca2-O2 | 2x | 0.109 | 0.128 | 0.138 | 0.136 | 0.137 | 0.149 | 0.147 |
| Ca2-O2 | 2x | 0.254 | 0.204 | 0.225 | 0.217 | 0.223 | 0.231 | 0.228 |
| Ca2-O3 | 2x | 0.254 | 0.273 | 0.273 | 0.274 | 0.234 | 0.237 | 0.246 |
| Ca2-O7 |  | 0.286 | 0.356 | 0.361 | 0.359 | 0.405 | 0.417 | 0.424 |
| Ca2-O8 | 2x | 0.061 | 0.078 | 0.071 | 0.067 | 0.071 | 0.074 | 0.073 |
| Ca2-O10 |  | 0.172 | 0.216 | 0.178 | 0.200 | 0.172 | 0.214 | 0.218 |
| Total bond strength A2 |  | 1.814 | 1.939 | 1.952 | 1.946 | 1.906 | 2.011 | 2.028 |
| Reference value |  | 2 | 2 | 2 | 2 | 2 | 2 | 2 |

*Bond length from table 9

†Ro = RoCa+((RoSr-RoCa)*XSr(A1,A2)); RoCa=1.967, RoSr=2.118

Table A8: Calculated polyhedra volume[Å3]  for A1, A2, M1, M2, M3, T1, T2, T3 with quadratic elongation and variance for clinozoisite

| Run no. | ## Au32 | Au45 | Au35 | Au34 | Pt8 | Au42 | Au43 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Volume A1[7] | 18.15 | 18.14 | 18.24 | 18.39 | 19.13 | 18.91 | 19.41 |
| Volume A2[8] | 28.13 | 28.25 | 28.62 | 28.82 | 29.36 | 29.64 | 30.26 |
| Volume M1 | 8.52 | 8.85 | 9.16 | 9.04 | 9.34 | 8.79 | 9.13 |
| quad | 1.01104 | 1.00979 | 1.00717 | 1.00583 | 1.0092 | 1.00776 | 1.00678 |
| variance | 30.6728 | 27.15581 | 21.37043 | 17.27255 | 24.83691 | 23.89955 | 17.27171 |
| Volume M2 | 9.62 | 8.98 | 8.89 | 9.05 | 8.86 | 9.23 | 9.28 |
| quad | 1.00196 | 1.0062 | 1.0074 | 1.10096 | 1.00501 | 1.00542 | 1.0047 |
| variance | 4.64458 | 22.18364 | 18.55096 | 23.82497 | 9.62043 | 11.57355 | 9.98549 |
| Volume M3 | 10.05 | 9.94 | 9.61 | 9.45 | 9.50 | 9.57 | 9.48 |
| quad | 1.02955 | 1.02718 | 1.02506 | 1.02426 | 1.02637 | 1.02769 | 1.02537 |
| variance | 77.89204 | 75.1301 | 63.49569 | 64.06396 | 57.51065 | 71.49942 | 59.8722 |
| Volume T1 | 2.21 | 2.31 | 2.34 | 2.51 | 2.19 | 2.21 | 2.20 |
| quad | 1.00812 | 1.00234 | 1.00314 | 1.00258 | 1.00436 | 1.00812 | 1.00308 |
| variance | 24.31766 | 3.94579 | 8.92979 | 3.82534 | 14.13191 | 24.31766 | 2.2352 |
| Volume T2 | 2.11 | 2.04 | 2.13 | 2.02 | 2.14 | 1.93 | 2.09 |
| quad | 1.00344 | 1.00833 | 1.00571 | 1.00717 | 1.00557 | 1.00679 | 1.00558 |
| variance | 12.77299 | 30.69957 | 18.8788 | 19.30594 | 17.67768 | 17.98549 | 12.86811 |
| Volume T3 | 2.18 | 2.29 | 2.20 | 2.13 | 2.13 | 2.16 | 2.11 |
| quad | 1.0124 | 1.01063 | 1.0124 | 1.01113 | 1.00885 | 1.00952 | 1.00967 |
| variance | 46.39472 | 42.7078 | 46.64687 | 40.08846 | 33.43891 | 37.16529 | 36.88566 |