Appendices

Appendix I: The Table below give the most well-developed XRD peaks from which the minerals were identified and peaks from corresponding XRD reference patterns.

| Miller Indices | APS 800 (° C) talc pattern d-spacing | I (%) | 13-558 Reference 25 (°C) Talc I >15% d-spacing | I (%) |
| --- | --- | --- | --- | --- |
| 002 | 9.46 | 100 | 9.35 | 100 |
| 004 | 4.59 | 12 | 4.59 | 45 |
| 006 | 3.14 | 10 | 3.12 | 40 |
| 130 | 2.648 | 3 | 2.635 | 18 |
| 132 | 2.609 | 6 | 2.597 | 20 |
| 133 | forsterite |  | 2.496 | 20 |
| 132 | forsterite |  | 2.479 | 30 |
| 060 | 1.53 | 17 | 1.529 | 55 |
| Miller Indices | APS 800 (°C) tridymite-like pattern d-spacing | I (%) | 18-1170 Reference 25 (°C) tridymite I >15% d-spacing | I (%) |
| 040 | forsterite |  | 4.328 | 90 |
| 211 | 4.12 | 100 | 4.107 | 100 |
| 221 | Missing |  | 3.867 | 20 |
| 041 | Missing |  | 3.818 | 50 |
| 042 | Missing |  | 2.975 | 25 |
| 341 | Missing |  | 2.5 | 16 |
| 043 | Missing |  | 2.308 | 16 |
| Miller Indices | APS 800 (°C) anthophylite d-spacing | I (%) | 9-455 Reference 25 (°C) anthophyllite I >15% d-spacing | I (%) |
| 020 | 9.03 | 100 | 8.9 | 30 |
| 210 | 8.317 | 75 | 8.26 | 55 |
| 400 | 4.499 | 7 | 4.5 | 25 |
| 321 | 3.671 | 25 | 3.65 | 35 |
| 421 | 3.252 | 18 | 3.24 | 60 |
| 610 | 3.084 | 9 | 3.05 | 100 |
| 260 | 2.845 | 16 | 2.84 | 40 |
| 640 | 2.565 | 25 | 2.54 | 40 |
| Miller Indices | APS 800 (°C) Enstatite d-spacing | I (%) | 22-714 Reference 25 (°C) Enstatite I >15% d-spacing | I (%) |
| 420 | 3.193 | 100 | 3.18 | 100 |
| 030 | forsterite |  | 2.946 | 16 |
| 610 | 2.9235 | 21 | 2.878 | 55 |
| 131 | forsterite |  | 2.54 | 25 |
| 710 | forsterite |  | 2.497 | 18 |
| 430 | forsterite |  | 2.477 | 18 |
| 440 | 1.9827 | 18 | 1.988 | 10 |
| 133 | forsterite |  | 1.488 | 25 |
| 060 | forsterite |  | 1.473 | 18 |

Appendix II. Starting materials, heating time, temperature, and Phases Observed.

| Sample | Temperature (°C) | Heating Time | log min | Mineral Assemblage |
| --- | --- | --- | --- | --- |
| Jeffrey 6D | 450 | 30 days | 4.635 | chrysotile |
| Thetford | 450 | 30 days | 4.635 | chrysotile |
| Jeffrey 6D | 450 | 30 days | 4.635 | chrysotile |
| Jeffrey 6D | 475 | 30 days | 4.635 | chrysotile + possible forsterite |
| Thetford | 500 | 30 days | 4.635 | forsterite + 10+/talc like |
| Thetford | 500 | 24 h | 3.158 | chrysotile |
| Jeffrey 6D | 550 | 12 min | 1.079 | chrysotile |
| Jeffrey 6D | 550 | 22 min | 1.342 | chrysotile + 10A+ |
| Jeffrey 6D | 550 | 37 min | 1.568 | chrysotile + 10A+ |
| Jeffrey 6D | 550 | 55 min | 1.74 | chrysotile + 10A+ |
| Jeffrey 6D | 550 | 63 min | 1.799 | chrysotile + 10A+ |
| Jeffrey 6D | 550 | 76 min | 1.881 | chrysotile + 10A+ |
| Jeffrey 6D | 550 | 104 min | 2.021 | chrysotile + 10A+ + |
| Thetford | 550 | 8 h | 2.682 | chrysotile |
| Thetford | 550 | 20 h | 3.079 | forsterite + 10A+ + chrysotile |
| Thetford | 550 | 16 h | 2.982 | forsterite + chrysotile |
| Thetford | 575 | 8 h | 2.682 | chrysotile |
| Thetford | 575 | 24 h | 3.158 | forsterite + 10A+ + chrysotile |
| Thetford | 587 | 4 h | 2.38 | forsterite + 10A+ + chrysotile |
| Thetford | 587 | 24 h | 3.158 | forsterite + talc |
| Thetford | 600 | 4 h | 2.38 | forsterite + talc |
| Thetford | 600 | 20 h | 3.079 | forsterite + talc |
| Thetford | 600 | 24 h | 3.158 | forsterite + talc |
| New Idria | 600 | 46 min | 1.663 | chrysotile |
| New Idria | 600 | 139 min | 2.143 | none |
| Jeffrey CP | 600 | 9 min | 0.954 | chrysotile |
| Jeffrey CP | 600 | 14 min | 1.146 | talc + chrysotile |
| Jeffrey CP | 600 | 23 min | 1.362 | talc + chrysotile+ forsterite |
| Jeffrey CP | 600 | 30 min | 1.477 | talc + chrysotile+ forsterite |
| Jeffrey CP | 600 | 42 min | 1.623 | talc + chrysotile+ forsterite |
| Jeffrey CP | 600 | 62 min | 1.792 | talc + chrysotile+ forsterite |
| Jeffrey CP | 600 | 79 min | 1.898 | talc + chrysotile+ forsterite |
| Jeffrey CP | 600 | 94 min | 1.973 | talc + chrysotile+ forsterite |
| Jeffrey CP | 600 | 122 min | 2.013 | talc + chrysotile+ forsterite |
| Jeffrey CP | 600 | 137 min | 2.086 | talc + forsterite |
| Jeffrey 6D | 600 | 2 min | 0.301 | chrysotile + forsterite |
| Jeffrey 6D | 600 | 9 min | 0.954 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 14 min | 1.146 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 24 min | 1.38 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 30 min | 1.477 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 36 min | 1.556 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 43 min | 1.633 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 52 min | 1.716 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 59 min | 1.771 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 66 min | 1.82 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 73 min | 1.863 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 82 min | 1.914 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 92 min | 1.964 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 117 min | 2.068 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 120 min | 2.079 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 137 min | 2.137 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 154 min | 2.188 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 171 min | 2.232 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 186 min | 2.27 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 201 min | 2.303 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 216 min | 2.334 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 231 min | 2.364 | chrysotile + forsterite + talc |
| Jeffrey 6D | 600 | 246 min | 2.391 | chrysotile + forsterite + talc |
| Thetford | 600 | 9 min | 0.954 | chrysotile |
| Thetford | 600 | 22 min | 1.342 | chrysotile + forsterite |
| Thetford | 600 | 42min | 1.623 | 10+ + forsterite + chrysotile |
| Thetford | 600 | 54 min | 1.732 | 10+ + talc + forsterite + chrysotile |
| Thetford | 600 | 64 min | 1.806 | 10+ + forsterite + chrysotile |
| Thetford | 600 | 72 min | 1.857 | 10+ + forsterite + chrysotile |
| Thetford | 600 | 84 min | 1.924 | 10+ + forsterite + chrysotile |
| Thetford | 600 | 101 min | 2.004 | 10+ + talc + forsterite + chrysotile |
| Thetford | 600 | 114 min | 2.057 | 10+ + talc + forsterite + chrysotile |
| Thetford | 600 | 136 min | 2.134 | 10+ + talc + forsterite + chrysotile |
| Thetford | 600 | 153 min | 2.185 | 10+ + talc + forsterite + chrysotile |
| Thetford | 600 | 182 min | 2.26 | 10+ + forsterite + chrysotile |
| Thetford | 650 | 4 h | 2.38 | forsterite + talc |
| Thetford | 650 | 8 h | 2.681 | forsterite + talc |
| Thetford | 650 | 16 h | 2.982 | forsterite + talc |
| Thetford | 650 | 20 h | 3.079 | forsterite + talc |
| Thetford | 650 | 24 h | 3.158 | forsterite + talc |
| Jeffrey 6D | 650 | 2 min | 0.301 | chrysotile |
| Jeffrey 6D | 650 | 8 min | 0.903 | chrysotile + forsterite + talc |
| Jeffrey 6D | 650 | 17 min | 1.23 | chrysotile + forsterite + talc |
| Jeffrey 6D | 650 | 25 min | 1.398 | chrysotile + forsterite + talc |
| Jeffrey 6D | 650 | 32 min | 1.505 | chrysotile + forsterite + talc |
| Jeffrey 6D | 650 | 71 min | 1.851 | chrysotile + forsterite + talc |
| Jeffrey 6D | 650 | 79 min | 1.898 | chrysotile + forsterite + talc |
| Jeffrey 6D | 650 | 96 min | 1.982 | chrysotile + forsterite + talc |
| Jeffrey 6D | 650 | 118 min | 2.072 | forsterite + talc |
| Thetford | 700 | 4 h | 2.38 | talc + forsterite |
| Thetford | 700 | 8 h | 2.681 | talc + forsterite |
| Thetford | 700 | 16 h | 2.982 | talc + forsterite |
| Thetford | 700 | 20 h | 3.079 | talc + forsterite |
| Thetford | 700 | 24 h | 3.158 | talc + forsterite |
| Jeffrey 6D | 700 | 2 min | 0.301 | chrysotile + forsterite + talc |
| Jeffrey 6D | 700 | 9 min | 0.954 | forsterite + talc |
| Jeffrey 6D | 700 | 16 min | 1.204 | forsterite + talc |
| Jeffrey 6D | 700 | 28 min | 1.447 | forsterite + talc |
| Jeffrey 6D | 700 | 37 min | 1.568 | forsterite + talc |
| Jeffrey 6D | 700 | 43 min | 1.633 | forsterite + talc |
| Jeffrey 6D | 700 | 51 min | 1.708 | forsterite + talc |
| Jeffrey 6D | 700 | 58 min | 1.763 | forsterite + talc |
| Jeffrey 6D | 700 | 63 min | 1.799 | forsterite + talc |
| Jeffrey 6D | 700 | 70 min | 1.845 | forsterite + talc |
| Jeffrey 6D | 700 | 88 min | 1.944 | forsterite + talc |
| Jeffrey 6D | 700 | 118 min | 2.012 | forsterite + talc |
| Jeffrey 6D | 700 | 151 min | 2.179 | forsterite + talc |
| Jeffrey 6D | 700 | 181 min | 2.258 | forsterite + talc |
| Jeffrey 6D | 700 | 211 min | 2.324 | forsterite + talc |
| Jeffrey 6D | 700 | 241 min | 2.382 | forsterite + talc |
| Thetford | 700 | 2 min | 0.301 | forsterite + chrysotile |
| Thetford | 700 | 9 min | 0.954 | forsterite |
| Thetford | 750 | 4 h | 2.38 | forsterite |
| Thetford | 800 | 1 min | 0 | forsterite + chrysotile |
| Thetford | 800 | 3 min | 0.477 | forsterite |
| Jeffrey 6D | 800 | 2 min | 0.301 | forsterite + talc |
| Jeffrey 6D | 800 | 9 min | 0.954 | forsterite + talc |
| Jeffrey 6D | 800 | 16 min | 1.204 | forsterite + talc |
| Jeffrey 6D | 800 | 23 min | 1.362 | forsterite + talc |
| Jeffrey 6D | 800 | 29 min | 1.462 | forsterite + talc + enstatite |
| Jeffrey 6D | 800 | 37 min | 1.568 | forsterite + talc + enstatite |
| Jeffrey 6D | 800 | 42 min | 1.623 | forsterite + talc + enstatite |
| Thetford | 800 | 5 min | 0.699 | forsterite + talc |
| Thetford | 800 | 10 min | 1 | forsterite + talc + tridymite-like |
| Thetford | 800 | 17 min | 1.23 | forsterite + talc + tridymite-like |
| Thetford | 800 | 42 min | 1.623 | forsterite + talc + tridymite-like + enstatite |
| Thetford | 800 | 60 min | 1.778 | forsterite + talc + tridymite-like + enstatite + anthophyllite |
| Thetford | 800 | 90 min | 1.954 | forsterite + tridymite-like + enstatite + anthophyllite |
| Thetford | 800 | 103 min | 2.013 | forsterite + tridymite-like + enstatite + anthophyllite |
| Thetford | 800 | 113 min | 2.053 | forsterite + enstatite + anthophyllite |
| Thetford | 800 | 151 min | 2.179 | forsterite + enstatite + anthophyllite |
| Thetford | 800 | 173 min | 2.238 | forsterite + enstatite + anthophyllite |
| Thetford | 800 | 209 min | 2.32 | forsterite + enstatite + anthophyllite |
| Thetford | 800 | 229 min | 2.36 | forsterite + enstatite + anthophyllite |
| Thetford | 800 | 245 min | 2.389 | forsterite + enstatite + anthophyllite |
| Thetford | 800 | 265 min | 2.423 | forsterite + chrysotile |
| New Idria | 800 | 2 min | 0.301 | forsterite + enstatite |
| New Idria | 800 | 8 min | 0.903 | forsterite + enstatite |
| Thetford | 900 | 4 h | 2.38 | forsterite + enstatite |
| Thetford | 1000 | 4 h | 2.38 | forsterite + enstatite |

Appendix III. Thetford Gradual Heating Experiment: Heat times, phases, and area intensity sums as a percentage of maximum intensity of each phase.

| Heating Time |  | Percent Maximum Intensity |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Min | Chrysotile | Forsterite | Talc | Tridymite-like | Enstatite | Anthophyllite |
| 0 | 100 | 0 |  |  |  |  |
| 1 | 25 | 80 |  |  |  |  |
| 3 | <1 | 79 | 0 |  |  |  |
| 5 | 0 | 76 | 95 | 0 |  |  |
| 10 |  | 91 | 100 | 3 |  |  |
| 17 |  | 92 | 95 | 86 | 0 |  |
| 42 |  | 100 | 95 | 100 | 1 | 0 |
| 60 |  | 87 | 89 | 99 | 2 | <1 |
| 90 |  | 88 | 0 | 78 | 61 | <1 |
| 103 |  | 79 |  | 5 | 94 | 20 |
| 113 |  | 90 |  | 58 | 78 | 50 |
| 151 |  | 92 |  | 0 | 82 | 92 |
| 173 |  | 96 |  |  | 90 | 100 |
| 209 |  | 93 |  |  | 91 | 96 |
| 229 |  | 85 |  |  | 71 | 54 |
| 245 |  | 94 |  |  | 66 | 42 |
| 265 |  | 77 |  |  | 100 | 43 |