Table 2. Thermodynamic properties for various SiO2 phases given with respect to

quartz for one mol of SiO2

| SiO2 Phase | DSt2r9a8nsK | DHt2r9a8nsK | DGt2r9a8nsK |
| --- | --- | --- | --- |
|  | J/(mol·K) | kJ/mol | kJ/mol |
| quartz | 0.0 | 0.0 | 0.0 |
| cristobalite | 1.9 | 2.8 | 2.3 |
| melanophlogite | 6.7 | 9.5 | 7.5 |
| silica glass | 7.0 | 9.1 | 7.0 |
| ZSM-5 | 3.6 | 6.8 | 5.7 |
| ZSM-23 | 4.2 | 6.7 | 5.4 |
| zeolite beta | 3.4 | 9.3 | 8.0 |
| silica faujasite | 3.2 | 13.6 | 12.6 |

Notes: The first three listed phases are minerals and the last four are synthetic

crystalline phases. All data, except for melanophlogite, are from Piccione et al.

(2001). The enthalpy value for melanophlogite is from Navrotsky et al. (2003)

and the entropy and free-energy values from this study. The entropy for quartz at

298 K was taken from Robie and Hemingway (1995).