Jenkins AM-13-031, American Mineralogist April 2013

David M. Jenkins, Giancarlo Della Ventura, Roberta Oberti, Krassimir Bozhilov

Synthesis and characterization of amphiboles along the tremolite–glaucophane join.

Table 6 – Supplementary crystallographic data.  Single-crystal refinements (SREF) of samples WIN 9-1 and WIN 4-2

WIN 9-1

a = 9.8076(9) b = 18.0004(17) c = 5.2804(5) Å beta = 104.575(2)°  V = 902.21 Å3

Atom coordinates, refined site-scattering values (ss, epfu), atomic-displacement parameters (Beq, Å2; ii)

Site    ss      x/a     y/b     z/c    Beq      11     22     33      12     13      23

O(1)  32.00  0.11079 0.08660 0.21658  0.88  0.0020 0.0008 0.0080 -0.00012 0.0010 -0.0001

O(2)  32.00  0.11901 0.17091 0.72730  0.97  0.0029 0.0009 0.0079  0.00019 0.0020  0.0002

O(3)  16.00  0.10967 0.00000 0.71368  1.12  0.0027 0.0009 0.0117  0.00000 0.0012  0.0000

O(4)  32.00  0.36549 0.24850 0.79236  1.24  0.0042 0.0009 0.0103 -0.00020 0.0023 -0.0001

O(5)  32.00  0.34739 0.13453 0.09805  1.15  0.0029 0.0011 0.0092  0.00001 0.0012  0.0008

O(6)  32.00  0.34379 0.11802 0.58993  1.05  0.0030 0.0009 0.0086  0.00016 0.0015 -0.0007

O(7)  16.00  0.33697 0.00000 0.28829  1.14  0.0036 0.0004 0.0145  0.00000 0.0011  0.0000

T(1)  55.80  0.28068 0.08468 0.29671  0.71  0.0020 0.0006 0.0064 -0.00002 0.0013 -0.0001

T(2)  56.00  0.28869 0.17169 0.80393  0.82  0.0024 0.0007 0.0070 -0.00016 0.0011 -0.0000

M(1)  24.00  0.00000 0.08826 0.50000  0.78  0.0024 0.0006 0.0066  0.00000 0.0013  0.0000

M(2)  24.06  0.00000 0.17748 0.00000  0.84  0.0024 0.0008 0.0072  0.00000 0.0018  0.0000

M(3)  24.00  0.00000 0.00000 0.00000  0.83  0.0028 0.0005 0.0081  0.00000 0.0014  0.0000

M(4)  34.56  0.00000 0.27719 0.50000  1.08  0.0035 0.0009 0.0101  0.00000 0.0036  0.0000

A2     2.38  0.00000 0.47927 0.00000  3.20

H      2.00  0.20284 0.00000 0.76357  1.89

R3σ   = 3.51 ( 806  refl.)   R5σ  = 2.69 ( 614 refl.)   Rall  = 7.20 (1369 refl.) F(000)= 805.58     limited to θ = 30°

Selected interatomic distances (Å) and angles (o). Values of tetrahedral (T) and octahedral (O) quadratic elongation (QE) and angular variance (AV) are calculated according to Robinson et al. (1971). DELTA is calculated according to Brown and Shannon (1973)

| T(1)-O(1) 1.613 | T(2)-O(2) 1.611 | M(4)-O(2) 2.400 | M(1)-O(1) 2.059 | M(2)-O(1) 2.131 | M(3)-O(1) 2.072 |
| --- | --- | --- | --- | --- | --- |
| -O(5) 1.637 | -O(4) 1.583 | -O(4) 2.316 | -O(2) 2.076 | -O(2) 2.073 | -O(3) 2.064 |
| -O(6) 1.630 | -O(5) 1.656 | -O(5) 2.770 | -O(3) 2.084 | -O(4) 1.997 | H-O(3) 0.885 |
| -O(7) 1.626 | -O(6) 1.676 | -O(6) 2.549 | <M(1)-O> 2.073 | <M(2)-O> 2.067 | <M(3)-O> 2.069 |
| <T(1)-O> 1.626 | <T(2)-O> 1.631 | <M(4)-O> 2.508 | VOL. 11.685 | VOL. 11.642 | VOL. 11.557 |
| VOL. 2.205 | VOL. 2.212 |  | OQE 1.0112 | OQE 1.0082 | OQE 1.0148 |
| TQE 1.0010 | TQE 1.0053 |  | OAV 36.83 | OAV 25.61 | OAV 48.23 |
| TAV 4.13 | TAV 21.70 |  | DELTA 0.254 | DELTA 6.963 | DELTA 0.031 |

| A -O(5) 2.958 | A(2)-O(5) 2.664 | T(1)-T(2)-T(1) 118.58 |
| --- | --- | --- |
| -O(6) 3.143 | -O(6) 2.904 | T(1)-O(5)-T(2) 136.25 |
| -O(7) 2.469 | -O(7) 2.498 | T(1)-O(6)-T(2) 137.95 |
| <A -O> 2.934 | <A(2)-O> 2.688 | T(1)-O(7)-T(1) 139.34 |
|  |  | M(1)-M(2) 3.090 |

WIN 4-2

a = 9.7739(11) b = 17.9636(20) c = 5.2659(6) Å beta = 104.423(3)°  V = 895.42 Å3

Atom coordinates, refined site-scattering values (ss, epfu), atomic-displacement parameters (Beq, Å2; ii)

Site    ss      x/a      y/b      z/c    Beq      11     22    33      12     13      23

O(1)  32.00  0.11062  0.08673  0.21645  0.65  0.0021 0.0007 0.0034 -0.0001 0.0008  0.0001

O(2)  32.00  0.11904  0.17120  0.72635  0.72  0.0019 0.0006 0.0063  0.0002 0.0009  0.0001

O(3)  16.00  0.10974  0.00000  0.71485  0.76  0.0021 0.0007 0.0059  0.0000 0.0014  0.0000

O(4)  32.00  0.36571  0.24868  0.79115  0.94  0.0037 0.0005 0.0088 -0.0004 0.0023 -0.0001

O(5)  32.00  0.34784  0.13441  0.09800  0.94  0.0032 0.0009 0.0057  0.0001 0.0015  0.0010

O(6)  32.00  0.34347  0.11794  0.58877  0.86  0.0027 0.0010 0.0034  0.0001 0.0009 -0.0010

O(7)  16.00  0.33775  0.00000  0.28706  0.96  0.0029 0.0005 0.0129  0.0000 0.0024  0.0000

T(1)  56.00  0.28063  0.08459  0.29511  0.46  0.0018 0.0004 0.0029  0.0000 0.0009 -0.0001

T(2)  55.80  0.28941  0.17146  0.80351  0.49  0.0020 0.0004 0.0025 -0.0001 0.0008  0.0001

M(1)  24.00  0.00000  0.08830  0.50000  0.57  0.0026 0.0004 0.0024  0.0000 0.0012  0.0000

M(2)  24.33  0.00000  0.17747  0.00000  0.65  0.0022 0.0005 0.0053  0.0000 0.0011  0.0000

M(3)  12.31  0.00000  0.00000  0.00000  0.63  0.0027 0.0003 0.0046  0.0000 0.0009  0.0000

M(4)  34.26  0.00000  0.27693  0.50000  0.95  0.0037 0.0008 0.0078  0.0000 0.0040  0.0000

A      2.90  0.00000  0.50000  0.00000  6.17

H      2.00  0.19245  0.00000  0.74231  1.31

R3σ   = 4.38 (1020 refl.)   R5σ  = 3.82 (  863 refl.)   Rall  = 6.34 (1837 refl.) F(000)= 805.58      limited to θ = 35°

Selected interatomic distances (Å) and angles (o). Values of tetrahedral (T) and octahedral (O) quadratic elongation (QE) and angular variance (AV) are calculated according to Robinson et al. ( 1971). DELTA is calculated according to Brown and Shannon (1973)

| T(1)-O(1) 1.610 | T(2)- (O2) 1.613 | M(4)- (O2) 2.386 | M(1)-O(1) 2.050 | M(2)-O(1) 2.124 | M(3)-O(1) 2.069 |
| --- | --- | --- | --- | --- | --- |
| -O(5) 1.628 | -O(4) 1.584 | -O(4) 2.299 | -O(2) 2.074 | -O(2) 2.068 | -O(3) 2.051 |
| -O(6) 1.629 | -O(5) 1.653 | -O(5) 2.768 | -O(3) 2.084 | -O(4) 1.993 | H-O(3) 0.785 |
| -O(7) 1.623 | -O(6) 1.667 | -O(6) 2.546 | <M(1)-O> 2.069 | <M(2)-O> 2.062 | <M(3)-O> 2.063 |
| <T(1)-O> 1.622 | <T(2)-O> 1.629 | <M(4)-O> 2.500 | VOL. 11.618 | VOL. 11.559 | VOL. 11.452 |
| VOL. 2.188 | VOL. 2.205 |  | OQE 1.0113 | OQE 1.0081 | OQE 1.0150 |
| TQE 1.0011 | TQE 1.0047 |  | OAV 37.17 | OAV 25.22 | OAV 48.71 |
| TAV 4.69 | TAV 18.79 |  | DELTA 0.462 | DELTA 6.748 | DELTA 0.169 |

| A -O(5) 2.948 | A(2)-O(5) 3.005 | T(1)-T(2)-T(1) 118.62 |
| --- | --- | --- |
| -O(6) 3.141 | -O(6) 3.619 | T(1)-O(5)-T(2) 136.02 |
| -O(7) 2.448 | -O(7) 5.476 | T(1)-O(6)-T(2) 138.38 |
| <A -O> 2.925 | <A(2-O> 4.034 | T(1)-O(7)-T(1) 138.86 |
|  |  | M(1)-M(2) 3.082 |